## Slide 2
Use of Nanotechnology in Remediation of Heavy Metals Polluted Soils
by
Dr. Mohamed . I. D. Helal
Prof. Soil Sci. Dept., Fac. of Agric.,
Cairo University

## Slide 3: Contents
- Remediation Techniques: - Methods of production of nano particles - Characteristics of the prepared nano particles
- Immobilization of Cd and Pb in polluted soils - Distribution of Cd and Pb among soil fractions
- Conclusion
Scientific Definitions
Properties of Nano Materials
General Methods for Preparation of Nano Materials
Introduction
Remediation of Heavy Metals Polluted Soils

## Slide 4: INTRODUCTION

## Slide 5
Nano-science :
is an emerging science which comprises the world of atoms, molecules, macromolecules, quantum dots, and macromolecular assemblies.

## Slide 6: Nano-technology
Nanotechnology is the technology for design, fabrication and manipulation of nanometre scale systems, in the scale of 1-100 nm.
Is any technology which exploits phenomena and structures that can only occur at nanometer scale.

## Slide 7: What is Nanotechnology?
Nanotechnology deals with the creation of USEFUL materials, devices and systems using the particles of nanometer length scale and exploitation of NOVEL properties (physical, chemical, biological) at that length scale

## Slide 8: Nanomaterials
NMs are materials have at least one dimension of size ~ 70nm (1-100 nm).

## Slide 9: Classification of Nanomaterials
1- Nanomaterials are categorized according to their Dimensions.
Example | Nanomaterial dimension
Nano films, layers and coatings | One dimension < 100 nm
Nanowires, Nanotubes, fibres | Two dimensions < 100 nm
Nanoparticles, quantum dots, nanoshells , nanorings , microcapsules | Three dimensions < 100 nm

## Slide 10: Properties of Nano materials

## Slide 11
Properties of Nano materials
Familiar materials can have completely different properties at nanoscale.
The familiar classical physics guideposts of magnetism and electricity are no longer dominant.
The applicable laws of physics shift as Newtonian mechanics give way to quantum mechanics.

## Slide 12
- Nanoscale sizes can lead to different physical and chemical properties:
  Melting point
  Boiling point
  Band gap
  Optical properties
  Electrical properties
  Magnetic properties
Properties of Nano materials
For example, metals with a so-called grain size of around 10 nanometers are as much as seven times harder and tougher than their ordinary counterparts with grain sizes in the micro meter range.

## Slide 13
The vastly increased ratio of surface area to volume opens new possibilities in surface-based science, such as catalysis.
Interactions of individual atoms and molecules take place
Surface effects such as Van der Waals force attraction, hydrogen bonding, electric charge, ionic bonding, covalent bonding, hydrophobicity, hydrophilicity and quantum mechanical tunneling.

## Slide 14
The melting point of gold particles decreases dramatically as the particle size gets below 5 nm
Source: Nanoscale Materials in Chemistry, Wiley, 2001
Melting Point
Properties of Nano materials

## Slide 15
Properties of Nano materials
  Optical properties – color changes with size

## Slide 16
Properties of Nano materials Surface area dependence on particle size

## Slide 17: Importance of Nano Materials - Nano particles are of interest because of the new properties (such as chemical reactivity and optical behavior) that they exhibit compared with larger particles of the same materials.

## Slide 18
Methods of Production
of Nanoparticles

## Slide 19
General Methods:
First : (top-down) method
Start from bulk until you reach the nano-cutting through the following:
1 – Milling method
2 - Scratching or etching method :
This method is used to produce particles of silicon nano particles

## Slide 20
3- Laser ablation method : use of a laser pulse with a high-energy focused on the goal of the heart
4- (Sputtering) method :
Used to make thin film

## Slide 21
Second : (Bottom-up) method
This method starts from the bottom of any of the atoms begin to separate them and then aggregated up to the level of nano scale methods used :
1 - (sol-gel) method
2- Aerosol method
3- Chemical vapor deposition method ( CVD )

## Slide 22
Iron Nano Particle

## Slide 23: Remediation of Heavy Metals Polluted Soil

## Slide 24: Remediation of Heavy Metals Polluted Soil
Definition:
Heavy metals are widely defined as metallic elements
that have a specific gravity of 5.0 g/cm3 or more.
Heavy metals are the most toxic inorganic pollutants
exist in soils.
They can be of natural or anthropogenic origin
(Bradl, 2004 and Sedgwick, 2005).
- There are about 50 elements can be classified as heavy metals, but only 17 are considered to be very toxic, e.g., Hg,, Pb, Cd, Ni and Cr.

## Slide 25: Remediation of Heavy Metals Polluted Soil
Remediation technologies are scientific techniques used to remove pollutants and/or rehabilitate polluted natural materials.

## Slide 26
Remediation techniques
Removing of pollutants
Stabilization/ immobilization
Soil leaching
Phytoremediation
Ex situ
Or
In situ
Water or suitable solution
Extremly
Expensive
cause pollution of the ground water (in situ
Hyper accumulators
Environmental safe
Need long time
Chemi- Remediation
Chemical Reactions, Absorption, Ion exchange, Precipitation.
Conventional
Reagents (cement, phosphate, rock,…..)
Nano materials

## Slide 27: EXPERIMENTAL & RESULTS

## Slide 28: Nano Immobilizing Materials - Several nano particles are prepared and used for immobilization of Cd and Pb in polluted soils; 1- nZVI 2 - Bentonite supported nZVI (Bent-nZVI), 3 - Nano carbon 4 - Nano alginit

## Slide 29
Methods of production of Nano Particles

## Slide 30: Methods of production of Nano Particles
Nano particles used in our research are prepared using either:
1 - Chemical Methods
(nZVI and bent-nZVI)
II - Physical Methods
(nano alginit)

## Slide 31: Methods of production of Nano Particles
I - Chemical Methods:
A - Nano-scale Zero Valent Iron (nZVI):
Synthesis of nZVI is based on reduction of Fe (II) using borohydride (Wang and Zhang, 1997 and Wang et al., 2006).
FeCl2. 4H2O and NaBH4 are used. The proposed reaction is:
Fe+2 + 2BH- + 6H2O → Fe0 + 2B(OH)3 + 4H2 ↑
- Sample of the product was inspected using TEM, and the particle size ranged from 13- 103 nm.

## Slide 32
a
Figure1.Transmission Electron Microscopy “TEM” images of nZVI.

## Slide 33: B - Bentonite Supported nZVI (bent-nZVI): - 5.34 g FeCl2.4H2O was dissolved in a 4:1 (v/v) ethanol/water mixture (24 ml ethanol + 6 ml deion. H2O), then 1.5 g bentonite was added. -The mixture was held on a magnetic stirrer to be mixed. - Solid particles were washed three times with 25 ml portions of absolute ethanol to remove all water. - Drying the synthesized nanoparticles overnight at 45 C°. - TEM showed that particle size ranged from 28-110 nm

## Slide 34
Methods of production of Nano Particles
II- Physical methods:
Nano alginite: Alginite is a naturally occurring rock. It is greyish-green, it has high specific surface area, high number of functional groups and high CEC.
Nano alginit was prepared in lab by ball-milling (Photon company, Egypt). Portions of alginit were placed in a stainless steel canister with metal balls of different three sizes, and stirred for 27 hours at speed of 1000 rpm.
A sample of milled alginite was inspected using TEM, and the size of the alginite particle ranged from 13 – 23nm.

## Slide 35: Nano Carbon : Thermal Preparation - Nano carbon was collected from ovens of bread in Iraq. - TEM showed that particle size ranged from 12.9-23.9 nm

## Slide 36
Table 1. Important characteristics of nanoparticles |  |  | 
Reagents | Particle Size Range (nm) | Surface area (m2/g) | CEC (Cmol(c)/kg)
Nanoalginite | 53.5 – 63.1 | 194.2 | 47.7
nZVI | 12.7 – 103 | 235.7 | 42.5
Bent-nZVI | 27.8 – 110 | 225.4 | 47.7
nano carbon | 12.9 – 23.9 | 259.7 | -

## Slide 37: Reaction Mechanisms of Nanoscale Zero Valent Iron (nZVI)

## Slide 38: Reduction Power of nZVI
nZVI has been used extensively to reduce (dehalogenate) chlorinated solvents and sequester metals.
The small particle size and high surface area make iron nano particles highly reactive and extremely versatile.
Nano-particles can remediate more material at a higher rate and with a lower generation of hazardous byproducts (Zhang, 2003).

## Slide 39: Oxidation of Organic Contaminants using Nanoparticles Zero Valent Iron (ZVI)
In an experiment with the pesticide molinate and ZVI, no change was observed in the concentrations of either one when bubbling nitrogen gas through the solution.
Air showed a marked reduction in molinate.

## Slide 40: Oxidative Power of nZVI
Oxygen reacts with ZVI in two fashions.
In the useful pathway : Fe0 reacts with O2 to form Fe+2 and O2-2. The O2-2 reacts with hydrogen to form hydrogen peroxide which reacts with Fe+2 to form Fe+3 and hydroxyl radicals (Fenton's reaction) that are highly reactive oxidants.
The usefulness of the reaction depends on the efficiency of the branching process to favor hydroxyl radical formation.

## Slide 42: IMMOBILIZATION OF Cd and Pb IN POLLUTED SOIL

## Slide 43: Remediation of Heavy Metals Polluted Soil
The concept of immobilization technique based on:
The soluble/mobile form of an element in soil is considered to be a better indicator of the risk associated with heavy metals (e.g. leaching, bio-uptake) than the total metal concentration.
- Heavy metals are immobilized in soil through different processes, e.g., specific adsorption, cation-exchange and precipitation (carbonates, phosphates, sulfides, ….).

## Slide 44: Immobilization of Cd and Pb in polluted soil
Heavy metals polluted soils are treated with nano materials at different ratios, 0, 0.1, 0.5 and 1%, and incubated for one month. During this period the samples were submitted to four cycling of wetting and drying.
The samples were extracted using DTPA before and after treating with nano materials.
DTPA solution consists of 0.005 M DTPA “Diethylene-triamine-penta acetic acid”, 0.01 M CaCl2 and 0.1 M TEA “Tri ethanolamine” at pH 7.3.
DTPA solution is recommended to extract amount of metal represent the so called “ plant available Cd and Pb” in polluted soil

## Slide 45
Table 2 : Initial contents of plant available (DTPA), and total Cd and Pb (mg/kg), and their ratios in polluted soils |  |  |  |  |  | 
Soil | DTPA-Cd | Total - Cd | Ratio (DTPA/ Total)% | DTPA-Pb | Total - Pb | Ratio (DTPA/ Total)%
1 | 3.2 | 8.9 | 36.6 | 52.7 | 180.0 | 29.3
2 | 19.9 | 47.5 | 42.0 | 47.3 | 275.0 | 17.2
3 | 3.7 | 8.7 | 43.0 | 41.5 | 150.0 | 27.7
4 | 7.6 | 21.0 | 36.3 | 33.6 | 135.0 | 24.9

## Slide 46
Table 3 : Plant available Cd (mg/kg) in polluted soils before and after treating with Nano particles |  |  |  |  | 
DTPA- extractable Cd (mg/kg ) |  |  |  |  | 
Treatment | Rate of addition % | Soil 1 | Soil 2 | Soil 3 | Soil 4
nZVI | 0.0 | 3.24 | 19.9 | 3.74 | 7.61
 | 0.1 | 1.71 | 9.36 | 1.66 | 3.21
 | 0.5 | 0.91 | 4.73 | 1.04 | 2.65
 | 1.0 | 0.23 | 2.01 | 0.11 | 2.17
Level of non polluted soil (Aboulroos et al,1988) |  | 0.06 | 0.06 | 0.06 | 0.06

## Slide 47
Table 4 : Plant available Cd (mg/kg) in polluted soils before and after treating with Nano particles |  |  |  |  | 
DTPA- extractable Cd (mg/kg ) |  |  |  |  | 
Treatment | Rate of addition % | Soil 1 | Soil 2 | Soil 3 | Soil 4
Bent-nZVI | 0.0 | 3.24 | 19.9 | 3.74 | 7.61
 | 0.1 | 1.56 | 10.05 | 1.48 | 3.14
 | 0.5 | 0.78 | 5.83 | 0.62 | 2.39
 | 1.0 | 0.15 | 3.79 | 0.15 | 1.51
Level of non polluted soil (Aboulroos et al,1988) |  | 0.06 | 0.06 | 0.06 | 0.06

## Slide 48
Table 5: Plant available Pb (mg/kg) of polluted soils before and after treating with nano particles |  |  |  |  | 
DTPA- extractable Pb (mg/kg ) |  |  |  |  | 
Treatment | Rate of addition % | Soil 1 | Soil 2 | Soil 3 | Soil 4
nZVI | 0.0 | 52.7 | 47.3 | 41.5 | 33.6
 | 0.1 | 24.6 | 25.1 | 21.5 | 11.5
 | 0.5 | 8.7 | 9.8 | 8.44 | 3.4
 | 1.0 | 3.2 | 3.5 | 2.9 | 1.62
Level of non polluted soil (Aboulroos et al, 1988) |  | 2.2 | 2.2 | 2.2 | 2.2

## Slide 49
Table 6: Plant available Pb (mg/kg) of polluted soils before and after treating with nano particles |  |  |  |  | 
DTPA- extractable Pb (mg/kg ) |  |  |  |  | 
Treatment | Rate of addition % | Soil 1 | Soil 2 | Soil 3 | Soil 4
Bent-nZVI | 0.0 | 52.7 | 47.3 | 41.5 | 33.6
 | 0.1 | 21.8 | 22.2 | 21.5 | 11.6
 | 0.5 | 7.3 | 8.2 | 8.4 | 2.9
 | 1.0 | 3.2 | 3.5 | 2.9 | 0.9
Level of non polluted soil (Aboulroos et al, 1988) |  | 2.2 | 2.2 | 2.2 | 2.2

## Slide 50
Chart: Soil 3/Cd
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 42.7814 | 23.6557 | 5.623 | 43.0546 | 26.1148 | 0.70492 | 38.4098 | 14.9126 | 2.071 | 43.3279 | 29.1202 | 25.8415 | 38.1366 | 32.1257 | 15.7322
0.5 | 1
1 | 1
Chart: Soil 1/Cd
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 56.9873 | 29.7722 | 7.3038 | 51.6076 | 26.2911 | 4.7722 | 47.1772 | 22.4937 | 2.557 | 56.038 | 54.1392 | 46.2278 | 51.6076 | 40.2152 | 13.6329
0.5 | 1
1 | 1
Chart: Soil 2/Cd
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 56.7353 | 49.3743 | 46.3986 | 49.1394 | 36.3751 | 22.906 | 46.7901 | 29.4056 | 21.2616 | 60.1026 | 57.7533 | 54.7776 | 45.3023 | 25.3336 | 17.816
0.5 | 1
1 | 1
Chart: Soil 4/Cd
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 43.6109 | 32.3227 | 28.8699 | 41.6189 | 34.1819 | 27.8074 | 40.822 | 30.8619 | 19.1753 | 38.9628 | 34.7131 | 29.1355 | 42.6813 | 39.3612 | 24.089
0.5 | 1
1 | 1
Fig. 2. DTPA extractable-Cd expressed as percentages of the initial values of the studied samples after treating with three rates of nano immobilizing materials.

## Slide 51
Chart: Soil 1/ Pb
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 51.9231 | 39.1026 | 27.0833 | 48.5577 | 34.1346 | 25 | 43.4295 | 29.0064 | 16.3462 | 61.6987 | 60.0962 | 50.1603 | 61.0577 | 47.9167 | 46.4744
0.5 | 1
1 | 1
Chart: Soil 2/Pb
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 56.5141 | 43.662 | 33.4507 | 54.5775 | 42.4296 | 31.5141 | 48.5915 | 35.7394 | 17.7817 | 57.0423 | 54.5775 | 48.0634 | 42.2535 | 19.7183 | 16.0211
0.5 | 1
1 | 1
Chart: Soil 3/Pb
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 39.8438 | 32.0312 | 23.763 | 35.4818 | 27.2135 | 21.6146 | 32.8776 | 23.112 | 21.224 | 51.237 | 43.099 | 39.974 | 40.2995 | 38.0859 | 29.6224
0.5 | 1
1 | 1
Chart: Soil 4/Pb
| Nano-Algi. | ZVI | ZVI-Bento | Nano Carbon | Dendrimers
Ctrl. | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1 | 0.1 | 0.5 | 1
0.1 | 100 | 39.5466 | 28.9673 | 13.3501 | 35.2645 | 20.1511 | 12.5945 | 36.0202 | 17.6322 | 7.0529 | 54.6599 | 63.728 | 69.7733 | 57.1788 | 38.539 | 21.6625
0.5 | 1
1 | 1
Fig. 3. DTPA extractable-Pb expressed as percentages of the initial values of the studied samples after treating with three rates of nano immobilizing materials.

## Slide 52: PARTIONING OF Cd AND Pb AMONG DIFFERENT SOIL FRACTIONS

## Slide 53
Partitioning of Cd and Pb among different soil fractions:
A sequential extraction procedure was employed to study the effect of nano immobilizing materials on the distribution of Cd and Pb among various soil chemical forms;
1- exchangeable (EXCH),
2- bound with carbonate (CARB),
3- organic matter (OM),
4- oxides (OX) and
5- residual (RES).

## Slide 54
Table 7 : Sum of all all fractions of Cd and Pb, total contents (mg/kg), and their ratios in soils |  |  |  |  |  | 
Soil | Cd |  |  | Pb |  | 
 | Sum of fractions | Total | Ratio (SUM/Total)% | Sum of fractions | Total | Ratio (SUM/Total)%
1 | 8.2 | 8.9 | 93.0 | 179.2 | 180.0 | 99.6
2 | 44.7 | 47.5 | 94.1 | 267 | 275.0 | 97.1
3 | 8.4 | 8.7 | 96.6 | 149.7 | 150.0 | 99.8
4 | 19.6 | 21.0 | 93.3 | 132 | 135.0 | 97.8

## Slide 55
Table 8. Different fractions of Cd sequentially extracted from soil (1) before and after treating with nano particles |  |  |  |  |  |  | 
Treatment |  | Cd fractions (mg/kg) |  |  |  |  | 
 |  | EXCH | CARB | OX | OM | RES | SUM
 | Initial | 2.8 | 0.8 | 1.3 | 0.6 | 2.7 | 8.2
 | nZVI | 0.4 | 1.9 | 2.5 | 0.6 | 3.0 | 8.4
 | Bent-nZVI | 0.6 | 2.7 | 1.4 | 0.7 | 3.2 | 8.6

## Slide 56
Table 9. Different fractions of Cd sequentially extracted from soil (2) before and after treating with nano particles |  |  |  |  |  |  | 
Treatment |  | Cd fractions (mg/kg) |  |  |  |  | 
 |  | EXCH | CARB | OX | OM | RES | SUM
 | Initial | 23.3 | 5.2 | 7.3 | 2.4 | 6.5 | 44.7
 | nZVI | 3.2 | 11.9 | 8.6 | 4.0 | 15.1 | 42.7
 | Bent-nZVI | 3.1 | 10.3 | 8.1 | 3.8 | 22.2 | 47.5

## Slide 57
Table 10: Different fractions of Pb sequentially extracted from soil (1) before and after treating with nano particles |  |  |  |  |  |  | 
Treatment |  | Pb fractions (mg/kg) |  |  |  |  | 
 |  | EXCH | CARB | OX | OM | RES | SUM
 | Initial | 22.3 | 29.6 | 36.0 | 17.5 | 73.8 | 179.2
 | nZVI | 9.8 | 22.4 | 70.5 | 20.3 | 54.6 | 177.6
 | Bent-nZVI | 9.1 | 36.2 | 67.5 | 20.3 | 47.7 | 180.8

## Slide 58
Table 11: Different fractions of Pb sequentially extracted from soil (2) before and after treating with nano particles |  |  |  |  |  |  | 
Treatment |  | Pb fractions (mg/kg) |  |  |  |  | 
 |  | EXCH | CARB | OX | OM | RES | SUM
 | Initial | 20.3 | 26.7 | 44.9 | 103.6 | 71.6 | 267.0
 | nZVI | 10.1 | 66.4 | 82.1 | 60.3 | 55.8 | 274.7
 | Bent-Nzvi | 10.1 | 68.4 | 78.3 | 65.8 | 51.2 | 27.0

## Slide 59: Conclusion
All immobilizing nano materials efficiently reduced the contents of plant available Cd and Pb in polluted soils as extracted in DTPA solution.
The magnitude of the reduction of plant available Cd and Pb varied as the immobilizing nano materials and its rate of application varied.
Increasing application rate of immobilizing nano materials significantly decreased DTPA extractable-Pb of all tested soils.
The immobilizing nano materials could be arranged in descending order according to their efficiency in immobilizing Cd and Pb as follows:
bent-nZVI > dendrimers > nZVI > nano alginite > nano carbon.

## Slide 60: Conclusion
Regarding partitioning of soil-Cd and -Pb among different factions;
the exchangeable Cd was the dominant one in all soils, followed by carbonate one, which indicates the high mobility of soil Cd.
Whereas a great potion of soil Pb exists in immobile fractions, e.g., residual and oxide ones.
All immobilizing nano materials significantly reduced the contents of exchangeable Cd and Pb in polluted soils, whereas those of other fractions; carbonate, oxide, organic and residual; significantly increased, indicating high efficiency of nano immobilizing materials to alter Cd and Pb form mobile to immobile fraction.
All immobilizing nano materials, particularly nZVI and bent-nZVI, are recommended to be used for remediation of Cd and Pb polluted soils due to their high efficiency, low cost, and safety to environment and human hygiene.

## Slide 61
THANK YOU

## Slide 62
Optical Properties