## Slide 1
Boundary element analysis of a piezoelectric ceramic with an interfacial crack subjected to in-plane mechanical and electrical loading
Characterisation of pellets and beams from barium titanate perovskite granulates
M. Gromada
Institute of Power Engineering, Ceramic Department CEREL, Boguchwała, Poland
M. Biglar, F. Stachowicz, T. Trzepieciński
Rzeszow University of Technology, Rzeszów, Poland

## Slide 2
Piezoelectric Materials
Motivation

## Slide 3
XRD patterns of BaTiO3 powder after first, second and third activation and calcination
Synthesis of BaTiO3 (BT) perovskite

## Slide 4
XRD pattern of BaTiO3 powder after second mechanical activation and calcination
Synthesis of BaTiO3 (BT) perovskite

## Slide 5
SEM microstructure of BaTiO3 powder in two different magnifications
Synthesis of BaTiO3 (BT) perovskite

## Slide 6
TEM morphology of BaTiO3 powder
Synthesis of BaTiO3 (BT) perovskite

## Slide 7
The particle size distribution of BaTiO3 powder
Synthesis of BaTiO3 (BT) perovskite

## Slide 8
Fabrication of BaTiO3 perovskite granulates
XRD pattern of BaTiO3 granulate

## Slide 9
SEM microstructure of BaTiO3 granulate in two different magnifications
Fabrication of BaTiO3 perovskite granulates

## Slide 10
Photos of discs and beams after forming by isostatic pressing
Preparation and characterisation of pellets

## Slide 11
Preparation and characterisation of pellets
The dilatometric curve of beam before sintering

## Slide 12
Material | The water absorbability, % | The apparent density, g/cm3 | The apparent porosity, % | The relative density, %
BT_0 | 0.03 | 5.84 | 0.19 | 97.01
BT_1 | 0.05 | 5.82 | 0.28 | 96.68
BT_2 | 0.06 | 5.83 | 0.37 | 96.84
BT_3 | 0.07 | 5.80 | 0.38 | 96.35
BT_4 | 0.09 | 5.87 | 0.50 | 97.51
The apparent density, water absorbability and apparent porosity of sintered pellets
Preparation and characterisation of pellets
XRD patterns of BaTiO3 pellets sintered in three different maximal temperature

## Slide 13
Preparation and characterisation of pellets
SEM microstructure of BT_1 pellet surface in two different magnifications
SEM microstructure of BT_1 pellet fracture surface

## Slide 14
SEM microstructure (BSE and SE) of BT_2 pellet surface in two different magnifications
SEM microstructure (SE and BSE) of BT_2 pellet fracture surface
Preparation and characterisation of pellets

## Slide 15
BT_0
BT_5
BT_6
BT_7
SEM microstructure of BT_0, BT_5, BT_6 and BT_7 pellets surface in the same magnification
Preparation and characterisation of pellets

## Slide 16
Thank You For Your Attention