## Slide 1: Comparative study of enzymatic and chemical denaturation of wheat gluten and their cellulosic nanocomposites By Nahla A. El-Wakil Cellulose & Paper Dept. National Research Center Cairo, Egypt
Recycling Expo-2015

## Slide 2: Protein-Based nanocomposites for Food Packaging Academy of Scientific Research and Technology, Egypt & Campus France
Recycling Expo-2015
International Project (Imhotep) (2013/2015)

## Slide 3: Objective The purpose is to examine the role of nanocellulose (CNC and MFC) as a reinforcing agent on the chemically and enzymatically denatured wheat gluten films.
Recycling Expo-2015

## Slide 4: Introduction
Recycling Expo-2015

## Slide 5: Cellulose
Recycling Expo-2015

## Slide 6: Nanocellulose
Recycling Expo-2015
TEM of nanofibers isolated from rice straw (a) and bagasse (b) (Hassan et al., 2010 & 2012)
Microfibrillated cellulose

## Slide 7: Cellulose nanocrystals
Recycling Expo-2015
The nanostructure of (a) bagasse and rice straw (b) (Hassan et al., 2009)

## Slide 8: Wheat gluten
Recycling Expo-2015
The structure of wheat gluten

## Slide 9
Recycling Expo-2015
Denaturation of protein
Enzymatic denaturation
Chemical denaturation
Heat denaturation

## Slide 10
Chemical denaturation of wheat gluten
Development of wheat gluten/nanocellulose/titanium dioxidenanocomposites for active food packaging. Nahla A. El-Wakil, Enas A. Hassan, Ragab E. Abou-Zeid, Alain Dufresne. Carbohydrate Polymers 124(2015) 337–346.
Recycling Expo-2015

## Slide 11: Charcterization
Recycling Expo-2015
Scanning electron microscopy (SEM)
Water sensitivity
Contact angle
Water vapor uptake (WVU)
Water vapor permeability (WVP)
Mechanical testing
    Tensile strength and Young’s modulus
Antimicrobial activity

## Slide 12
Recycling Expo-2015
SEM micrographs of surfaces and cross sections of neat WG (a and b), WG/CNC 7.5% (c and d), WG/CNC 12.5% (e and f) and WG/CNC 7.5%/0.6%TiO2(g and h).
Scanning electron microscopy (SEM)

## Slide 13
Recycling Expo-2015
Contact angle of WG, WG / CNC and WG/CNC/ TiO2
WG/CNC |  | WG/CNC 7.5%/TiO2 | 
Sample | Contact angle | Sample | Contact angle
WG | 45.10 ± 1.18 | WG/CNC 7.5% | 64.04 ± 2.84
2.5% CNC | 58.88 ± 0.74 | 0.2% TiO2 | 67.10 ± 0.11
5% CNC | 62.00 ± 0.38 | 0.4% TiO2 | 68.86 ± 0.41
7.5% CNC | 64.04 ± 2.84 | 0.6%TiO2 | 74.63 ± 0.66
10% CNC | 75.19 ± 0.25 | 0.8% TiO2 | 85.6 ± 2.31
12.5% CNC | 78.48 ± 1.18 | 1.0% TiO2 | 89.70 ± 0.14
Contact angle

## Slide 14
Recycling Expo-2015
Dependence of WVU on CNC content (a) and TiO2 content (b).
Water vapor uptake test (WVU)

## Slide 15
Recycling Expo-2015
Dependence of WVP on CNC content (a) and TiO2 content (b).
Water vapor permeability (WVP)

## Slide 16: Mechanical testing
Recycling Expo-2015
Typical stress-strain curves obtained from tensile tests for neat WG and WG filled with CNC (a) and WG with 7.5% CNC filled with TiO2 (b).

## Slide 17
Recycling Expo-2015
The colony-forming units (CFU/ml) and the reduction % of surviving number of the tested bacteria of the coated paper with and without TiO2 nanoparticles
 |  |  | S. aureus |  |  |  |  |  |  | E. coli |  |  | 
 |  |  |  |  |  | Time of UVA light exposure (h) |  |  |  |  |  |  | 
 | 1/2 |  | 1 |  | 2 |  |  | 1/2 |  | 1 |  | 2 | 
Sample | CFU/ml | R (%) | CFU/ml | R (%) | CFU/ml |  | R (%) | CFU/ml | R (%) | CFU/ml | R (%) | CFU/ml | R (%)
Blank | 2.4×105 | - | 3.7×105 | - | 3.1×105 |  | - | 3.2×105 | - | 6.0×105 | - | 6.6×105 | -
I layer | 1.0×105 | 58.3 | 8.0×104 | 78.4 | 0 |  | 100 | 2.5×105 | 21.9 | 2.9×105 | 51.7 | 1.0×105 | 84.9
II layers | 3.7×104 | 84.6 | 1.0×104 | 97.3 | 0 |  | 100 | 1.9×105 | 40.6 | 1.0×105 | 83.8 | 3.0×104 | 95.5
III layers | 2.9×104 | 87.9 | 3.0×103 | 98.2 | 0 |  | 100 | 1.5×105 | 53.1 | 6.0×104 | 90.0 | 1.0×104 | 98.5
Antimicrobial activity

## Slide 18
Recycling Expo-2015
Enzymatic denaturation of wheat gluten (EWG)
Effect of time on solubility of wheat gluten obtained with different percent of Alcalase enzyme

## Slide 19
Recycling Expo-2015
Chart: MFC
| 0 | 5.0000000000000031E-2 | 0.1 | 0.15000000000000008 | 0.2 | 0.25 | 0.30000000000000016
 | 11.7268 | 14.1435 | 15.3962 | 15.9963 | 16.4696 | 10.3246 | 8.5467
 | 3.6784 | 4.9011 | 6.4058 | 6.8726 | 7.5667 | 4.5678
Mechanical testing
Tensile strength of WG/MFC and EWG/MFC films

## Slide 20: Water vapor permeability (WVP)
Recycling Expo-2015
Chart: MFC %
| 0 | 5 | 10 | 15 | 20 | 25 | 30
Enzymaticaly | 2.1506e-09 | 2.4429e-09 | 2.1217e-09 | 1.6783e-09 | 1.6245e-09 | 1.454e-09
Chemically | 7.89e-10 | 9.9197e-10 | 9.2348e-10 | 4.9042e-10 | 3.4516e-10 | 3.1009e-10 | 3.2044e-10
WVP of WG/MFC and EWG/MFC films

## Slide 21: Contact angle measurment
Recycling Expo-2015
WG/MFC | 
Sample | Contact angle
5 % MFC 10 % MFC 15 % MFC 20 % MFC 25 % MFC 30 % MFC | 30.85 34.77 38.22 39.33 40.5 38.4
Contact angle of EWG/MFC films

## Slide 22: Scanning electrone microscopy
Recycling Expo-2015
SEM micrographs of EWG/20% MFC (a and b) and EWG/30% MFC (c and d) surface and cross section.

## Slide 23: Conclusion
Recycling Expo-2015
Filling of chemically and enzymatically denatured wheat gluten with MFC enhanced the mechanical and barrier properties of the prepared nanocomposites. However, this enhancement is significant in case of chemical denaturation specially for MFC content > 15%.
Attempts to develop thermoplastic films from wheat gluten to replace synthetic polymer based films need more extensive studies to achieve the target

## Slide 24: Acknowledgement
Recycling Expo-2015
I would to acknowledge my colleagues:
Dr. Enas A. Hassan assistant prof. and Dr. Ragab Abou-Zeid Researcher.
The authors acknowledge the Academy of Scientific Research and Technology, Egypt (National Research Center) & Scientific sector of the French institute of Egypt (Grenoble Institute of Technology, Pagora, Grenoble , France) for their financial support.

## Slide 25
Recycling Expo-2015