## Slide 1
A fundamental understanding
of the microwave properties in commercial ceramic dielectrics
Nathan Newman
Materials Department, ASU
Students: Shengke Zhang, Justin Gonzales, Siddhesh Gajare, & Alex Devonport
Collaborators: Hasin Sahin (U. Antwerp) & Dinish Martien (Quantum Design)
Q1: Can solid state physics methods provide a fundamental understanding?
A1: Yes, electronic & phonon band theory predicts dielectric properties of interest
Q2: What causes microwave loss?
A2: Spin-losses- a surprising result!!!!!
  Q3: Can the materials properties that determine tF (i.e. αL, τµ and τe) be predicted
A3: Yes 
Our approach: Use modern solid-state methods

## Slide 2
http://wwwen.zte.com.cn
Bandpass
filter
Cell phone base stations and their bandpass filters
15 cm x 8 cm
www.trans-techinc.com
Microwave dielectrics
60,000
35,000
25,000
24,000
Q @2 GHz
Cell phone bandpass filter
Cell phone base station
Bandpass filter characteristics

## Slide 3
Motivation
Future wireless systems will
  handle voice, audio , video and other data simultaneously at very fast rates
  require simultaneous operation in bands from hundreds of MHz to tens of GHz
  Need multiband, broadband and narrowband functionality, power handling, dynamic range, selectivity
  Require simultaneous transmission & reception over multiple bands
To bridge gap between current technology & future needs requires miniaturization
  PATHS: Novel design and/or low-loss high-dielectric-constant materials

## Slide 4
Microwave properties of Ba(Zn1/3Ta2/3)O3
for resonators and filters
l/2
E

## Slide 5: Critical Device Parameters for Resonators and Filters, Q & tf
Goal: High Q-factor to improve filter performance
  Low insertion loss
  Sharp roll-off
1st derivative
Q =
f0
Df
=1/tan δ (loss tangent)
Goal: Near-Zero Temperature Coefficient of Resonant Frequency (τf )
http://www.sengpielaudio.com/calculator-bandwidth.htm
A resonant peak
  Transition-metal additives are added to “tune” τf

## Slide 6
Perovskite Ba(Zn1/3Ta2/3)O3 (BZT)
Compact devices: l ∞ e-½ at specific device frequency, ε=30
tan d = 1/Q = ~1.6 x 10-5 @ 2 GHz, Q = ~60,000
Ba+2 Zr+4 O3-2
one Zn2+ and two Ta5+ results in average valence of
(1 x 2) + (2 x 5) = 4
Ba2+
O2-
+2 +5
e of ~30
tan d = 1/Q = ~2x10-5 @ 2 GHz
Devices w/ Q = ~55,000 (i.e. low-loss & sharp bandwidth)
Compact devices: (l/2 =2 cm, rather than 4 cm with e = 7.5)

## Slide 7
Ba(Zn1/3Ta2/3)O3 band structure
Band Structure shows d-electron “covalent” bonding - rigid & directional
This arises from charge transfer from
emptying out Ta-5d (lower conduction band) to filled Zn-3d (upper valence band) levels
angularly rigid bonds → ↓ anharmonicity phonon → ↓ microwave loss
Zn
O
O
Ba
Empty Ta (d)
Full Zn (d)

## Slide 8
Directional covalent bonds
strong like covalent diamond
Non-directional ionic bonds
weak like ionic NaCl
Low melt temperatures
Weak angular rigidity,
with soft phonon modes
High microwave loss
High melt temperatures
Strong angular rigidity,
with rigid phonon modes
Low microwave loss

## Slide 9
Ni-doping gives zero temp.-coefficient of resonant frequency
  offsets thermal expansion w/ T-dependence of e
l/2
E
Zr-doping minimizes anneal times to attain high Quality Factors (Q)
τf = 0 ppm/K
T. Negas et al, Proceedings of the International Conference, Jackson, WY, July 17–20, 1990
Transition-metal Additives are Commonly Added to “Tune” τf to Zero

## Slide 10: Approach
We will vary the temperature &magnetic field to identify the loss mechanism in practical microwave dielectric materials
Intrinsic loss
  Anharmonic phonons
Extrinsic loss
  a) Electrical carrier conduction
  b) Softened anharmonic phonons from defects
  c) Electron paramagnetic “spin-flip” loss
  d) 2-level systems from electric dipoles precession
Prior to this work, no direct measurement!
No proof!

## Slide 11: Temperature dependence of commercial materials (from Trans-Tech Inc.)
Ba(Ni0.04Zr0.03Zn0.29Ta0.64)O3
Ba(Zn0.13Co0.20Nb2/3)O3
Decrease of Q at low temperature
General effect in commercial microwave dielectric materials!
Quality factor (scaled to 10 GhZ)

## Slide 12
Unloaded Q factor of BZT doped w/ various impurities @ 4.2K
4.2K
“Magnetic” transition metal impurities influence loss
Spin mechanism involved; Not phonons or free carriers!

## Slide 13: Magnetic-field dependence of Ni-doped samples at 4.2K
We can improve Q by orders of magnitude with applied field
Shows is spin related
Magnetic dependence: Rule out the possibility of phonon & free carrier conductive losses
Practical importance??
(% is fraction of Ni substitution on Zn-site, 15% corresponds to 1 atomic % Ni)
Commercial Ni-doping concentration is ~12%

## Slide 14: Electron Paramagnetic Resonance (EPR)
3.8% Mn-doped BZT
6 peaks due to hyper fine structure
from I=5/2 Mn nuclear spins
i.e. I = -5/2, -3/2, -½ , ½, 3/2, 5/2
T=300K
E=mBgB
Zeeman
E=hn
Microwave
photon
40 mV
Resonance
3400 G
B
Zeeman
Resonance
Applied Magnetic Field

## Slide 15: Electron Paramagnetic Resonance (EPR)
3.8% Mn-doped BZT
6 peaks due to hyper fine structure
from I=5/2 Mn nuclear spins
i.e. I = -5/2, -3/2, -½ , ½, 3/2, 5/2
T=300K
E=mBgB
Zeeman
E=hn
Microwave
photon
40 mV
Resonance
3400 G
B
Zeeman
Resonance
Applied Magnetic Field
g=2.01

## Slide 16: It is spin flips! Identify as EPR spin-flip mechanism!
Microwave-induced Spin flips in exchange-coupled clusters!
Isolated defects
Plotting 1/Q (i.e. loss tangent ∞absorption)
B
Loss tangent (1/Q)

## Slide 17: Best properties in a magnetic-field- so far
 ALLOWS TUNING OF MICROWAVE PROPERTIES
Co-doped Ba(Zn1/3Nb2/3)O3

## Slide 18
Ba(Zn1/3Ta2/3)O3
Q>40,000
Q<15,000
Degraded microwave properties at room temperature

## Slide 19
Photon energy (eV)
Color Centers!!!! High Q, yellow. Low Q, brown.
Ba(Zn1/3Ta2/3)O3
Optical measurements of Ba(Zn1/3Ta2/3)O3.
Enhanced background from optically active point defects for lower Q materials Correlates microwave loss to point defect concentrations.
Ba(Zn1/3Ta2/3)O3
Q>40,000
Q<15,000

## Slide 20
EPR finds free-carrier conduction loss peak (i.e. g=2)
correlates with Q at 300 K

## Slide 21: τf = - (αL + ½ τµ+ ½ τε)
MHz
L. Miller, RF filters applications for dummies, a Wiley brand, 2015
Why is Zero/Near-Zero τf So Important?
We will independently determine τf, αL, τµ and τe
Use of experiment and simulation will be used to understand the fundamental mechanism for each factor!

## Slide 22
Kramers-Kronig (KK) of complex dielectric constant
-indicates that a change in e is associated with a loss mechanism
\
amicrowave loss
e
Loss tangent
40 mV 30 mV 1 eV
Microwave phonon electronic
loss absorption transitions

## Slide 23
If there are EPR losses, then there are also changes to the magnetic permeability (μr)!
KK equations:
11
μr(B) = μr’(B) - jμr’’(B)
Loss tangent=μr’’(B)/μ r’(B)
Magnetic field (Gauss)
Magnetic field (Gauss)
0.05 at.% Mn-BZT, 50K
0.05 at.%
Mn-BZT, 50K
Black dots: Measurement
Red line: KK transformed
Black dots: Measurement
Red line: KK transformed
g=2.0

## Slide 24: Phonon Dispersion Curves from Density Functional Theory Calculations
Ba(Zn1/3Ta2/3)O3
Ba(Ni1/3Ta2/3)O3
Black is for 0 K and Red is for 300 K, a 0.2% expanded lattice

## Slide 25: Thermal expansion coefficient measurement with dilatometer Good agreement between experimental results and Density Functional Calculations!
 | Avg. Gruneisen parameter (γ) | Bulk Modulus (B) (GPa)
BZT | 4.11 | 359 GPa
BNT | 2.57 | 235 GPa

## Slide 26: Measurements of Temperature Dependence of Magnetic Permeability (τµ)
µ of BNT (3.3 – 300 K) and 0.8 at.% Ni-BZT accurately fit by Curie-Weiss law
TNeel = 3.3 K is observed.
TNeel=3.3K

## Slide 27: Inferred Temperature Dependence of Dielectric Constant (τε)
τε = - (2 τf + 2 αL + τµ)
ε is the integration of τε
At low T, τε scales with the Ni concentration.
Surprisingly, ε can be fit with equation, Constant/T + ε∞ at low T, resulting from the paraelectric defects.

## Slide 28: Summary
Transition metal impurities dominate loss tangent at cryogenic temperature in high performance microwave dielectrics
  From resonant spin excitations of unpaired transition metal d-electrons in exchange-coupled clusters
The room temperature loss is tentatively associated with electrical conduction, even in commercially produced material
We are exploring the potential to use magnetic fields to improve Q and tune the microwave performance
First principle electron and phonon band structure calculations can be used to understand relevant properties of interest to the microwave dielectric community
  including e, τf, αL, τµ and τe
  additional work is needed to predict anharmonic phonon loss in complex dielectrics (Wu and Ceder, 2001)
Microwave loss in the high performance dielectric Ba(Zn1/3Ta2/3)O3 at 4.2K, Phys. Rev. Letters 109, 257601 (2012)
Dominance of paramagnetic loss in microwave dielectric s at cryogenic temperatures Appl. Phys. Lett. 101, 252901 (2012)
Main source of loss in Ba(Zn1/3Ta2/3)O3 and Ba(Zn1/3Nb2/3)O3 at low temperatures J. Am. Ceram. Soc. (2015)

## Slide 29
1 cm
HP 8510
Microwave dipping probe measurement system
Parallel plate & dielectric cavity
Schematic
Picture
Dip into 2-400 K 0-9 T Dewar

## Slide 30: 8% Ni Species 1
B ┴ to z plane
8% Ni Species 2
B || to z axis
(no transition in this range)
B || to z axis
Nate Newman Materials Program
Pictures from Bruker website
H=mBgBS+1/2J(S(S+1)-2s(s+1))+D(Sz2-1/3S(S+1))
Zeeman
Exchange interaction
Zero field splitting