## Slide 1
  A part of Sustainable recycling of “green” plastics project
  Recycling of bio/petro blends

## Slide 2
The focus is on highlighting challenges with new bio- petro blends as a new class of materials, identification, compatibility and recyclability.
  The aim of this work was to study reprocessing of some commercial blends, evaluation of properties and degradation.
Aim of the work

## Slide 3
  Choice of materials
  Investigation of the effects of repeated extrusion on material´s degradation
  Thermal and mechanical analysis for determination of miscibility
  Simulation of ”service life & recycling” using combination of repeated extrusion and ageing. Study of the effects on material degradation
Work plan

## Slide 4: Commercial polymer blends used in the study
PLA (Poly Lactic Acid) pure and blends:
  PLA 3051D injection moulding grade from Nature Work
  PLA/HDPE (39%) renewable- RTP2099X115382C from Nature Work
  PLA/PC (32%) renewable- RTP2099X126213 from Nature Work

## Slide 5
Processing and ageing of the materials
In-Lab
  PLA Granule, pressed material
  PLA/HDPE Granule, pressed material, extruded 1- 6 times
  PLA/PC Granule, pressed material, extruded 1- 6 times, pressed and aged, extruded and aged, extruded, aged and extruded again, extruded and aged 2 times
At-Industry
  PLA Granule
  PLA/HDPE Granule, extruded 3 times
  PLA/PC Granule, pressed material, extruded 2 times

## Slide 6
Simulation of pre-consumer recycling ”At Laboratory”
Extrusion
Material for testing
Bio/petro material (with additives)
Drying
FTIR
DSC
Mechanical testing
Notes: Bearbetning (extruderad och pressad)
Granulat och sex cyklar bearbetad material har granskat i syfte med nedbrytning av materialet under processbetingelse för både PLA/HDPE och PLA/PC.

## Slide 7
Extrusion
Material for testing
Bio/petro material (with additives)
Drying
FTIR
DSC
Mechanical testing
Simulation of pre-consumer recycling ”At industry”
Notes: Materialen bearbetads i form av en produkt (kniv) två gånger på industri (Hammarplast) för att simulera återvinning av produktionspill.

## Slide 8
”Life cycle”
Extrusion
Material for evaluation
Bio/petro material (with additives)
Drying
FTIR
DSC
Mechanical testing
Ageing
Material for evaluation
70 ºC & 50 % RH
Period 7 weeks
Simulation of post-consumer recycling ”At Laboratory”
Notes: Bearbetning och termiskåldring
Materialens livscykel (bearbetning + service life) simuleras med både bearbetning och termisk accelererad åldring i 3 omgångar

## Slide 9: Evaluation of simulated pre- and post-consumer recycling
E-modulus at tensile insignificantly decreased with the number of extrusions.
Double ageing period caused decrease of E-modulus in PLA/PC
Processing | E-modulus PLA/HDPE [MPa] | E-modulus PLA/PC [MPa]
0 Extrusion ( pressed) | 1417 | 2269
Extrusion 1 time | 1401 | 2250
Extrusion 2 times | 1387 | 2261
Extrusion 3 times | 1441 | 2279
Extrusion 4 times | 1349 | 2265
Extrusion 6 times | 1358 | 2280
Extrusion 1 time +1 ageing | - | 2075
Extrusion 1 time+1 ageing + Extrusion again | - | 2132
Extrusion 1 time+1 ageing + ageing again | - | 1503

## Slide 10
DSC: Tg, Tc and Tm for PLA/PC blend after repeated extrusion
Material | Tg | Tc | Tm
Pressed , non-extruded | 58,8 | 109.6 | 170,1
Extruded 1 time | 58,9 | 107,8 | 170,2
Extruded 2 times | 58,6 | 106,2 | 169,5
Extruded 3 times | 58,7 | 103,6 | 169,7
Extruded 6 times | 58,6 | 102,6 | 169,2
Glass transition temperature for PLA and PC has not changed after repeated extrusion.
Crystallization temperature of PLA has decreased.
Melt temperature has changed slightly.

## Slide 11
Material | Tg | Tc | Tg | Tm
Pressed , non-extruded | 58,8 | 109.6 |  | 170,1
Extruded 1 time | 58,9 | 107,8 |  | 170,2
Extruded 6 times | 58,6 | 102,6 |  | 169,2
Extruded 1 time + ageing | 56,4 | 104,7 | 144,2 | 167,4
DSC: Tg, Tc and Tm for PLA/PC after
repeated extrusion and combination of extrusion and ageing
Ageing causes degradation of PLA/PC
(lower Tg ,Tc and Tm)

## Slide 12
Material | Tg | Tc | Tg | Tm
Pressed , non-extruded | 58,8 | 109.6 | 147,3 | 170,1
Extruded 1 time | 58,9 | 107,8 | 147,2 | 170,2
Extruded 6 times | 58,6 | 102,6 | 146,5 | 169,2
Extruded 1 time + ageing | 56,4 | 104,7 | 144,2 | 167,4
Extruded 1 time + ageing + Extruded again | 55,3 | 104,9 | 144,0 | 167,0
Extruded 1 time + ageing + Ageing again | ? | 73,6 | 128 | 148,5
DSC: Tg, Tc and Tm for PLA/PC after
repeated extrusion and combination of extrusion and ageing
Ageing has a significant effect on degradation of PLA/PC

## Slide 13
Red: Virgin PLA
Light blue: PC-PLA pressed
Blue: PC-PLA Extruded 1 time
Green: PC-PLA Extruded 6 times
FTIR spectra of PLA and PLA/PC blend after repeated extrusion
No obvious change due to repeated extrusion

## Slide 14
Increasing of Bis Phenol A by aging of PC / PLA
Material | Concentration of Bis Phenol A [mg/g]
Non extrusion/granule | 0,13
Extrusion 6 times | 0,61
Extrusion once + ageing + ageing + ageing (B1A3) | 2,3
Concentration of Bis Phenol A increases almost 20 times by combination of extrusion and ageing

## Slide 15
Material | Tg1 | Tc | Tm1 | Tm2
Pressed/ Non extruded | 59,4 | 107,1 | 132,8 | 168,8
Extruded 1 time | 59,8 | 108,1 | 133,9 | 169,5
Extruded 2 times | 59,8 | 107,6 | 133,8 | 169,2
Extruded 3 times | 59,9 | 106,7 | 133,8 | 169,2
Extruded 6 times | 59,8 | 105,2 | 134,3 | 168,8
DSC thermogram and changing of Tg, Tc and Tm för PLA/HDPE
Small effect on crystallization temperature

## Slide 16
Blue: Virgin PLA
Red: HDPE-PLA pressed
Purple: HDPE-PLA Extrud 1 time
Green: HDPE-PLA Extrud 6 times
FTIR spectra for PLA and PLA/HDPE blend
No obvious change due to repeated extrusion

## Slide 17
Acknowledgements
Organizing committee for the opportunity to present our results
MISTRA for the financial support
My co-workers for the fruitful collaboration
Thank you for your kind attention !