## Slide 1: Optical Properties and Crystallization kinetic of Tellurite Glass–Ceramics Presented by
Dr. Nehal Elkhoshkhany,
Ass.Prof., Department of Material Science, Institute of Graduate Studies and Researches, Alexandria University

## Slide 2
Outline
Outline
Introduction.
EXPERIMENTAL WORK
Results and discussion.
Conclusion

## Slide 3
Introduction.

## Slide 4
The Rare earth-doped tellurite glass systems are very attractive materials. It have attracted a great attention in the last years because of their interesting properties, which made him ideal materials for applications in many important fields like telecommunication technology, laser and optical fiber technology, optical device technology.
Why we study tellurite glass system ?

## Slide 5: Aim
The aim of this research work is to investigate the influence of adding Er2O3 from 0 to 2.5 mol % on the Thermal and Optical properties and the network structure of (TeO2 – Na2O – ZnO) glasses, using DSC, X-Ray, SEM, and UV-Vis Spectroscopy.

## Slide 6: EXPERIMENTAL WORK

## Slide 7
Samples preparation
Quaternary tellurite glass systems in the form ((75-x) TeO2 - 20ZnO-5Na2Co3 - xEr2O3) glass samples with 0≤ x≤ 2.5 mol %) have been prepared by the melt quenching technique.
Glass type | Chemical composition by mol percent
TZNE0 | 75TeO2 -20ZnO- 5 Na2CO3
TZNE.5 | 74.5TeO2 -20ZnO- 5 Na2CO3 - 0.5Er2O3
TZNE1 | 74TeO2 -20ZnO- 5 Na2CO3 –1Er2O3
TZNE1.5 | 73.5TeO2 -20ZnO- 5 Na2CO3 –1.5Er2O3
TZNE2 | 73TeO2 -20ZnO- 5 Na2CO3 –2Er2O3
TZNE2.5 | 72.5TeO2 -20ZnO- 5 Na2CO3 –2.5Er2O3

## Slide 8
Measurements
X-ray diffraction.
Density measurements & calculation of Molar volume.
Differential Scanning Calorimetry (DSC) have been carried out on the prepared glass systems in the temperature range 300-800 ºC at heating rate 10, 15, 20 oC/min
Kinetics parameters like activation energy of relaxation structure Et , activation energy of crystallization Ec and order of crystallization have been calculated for every glass composition.

## Slide 9
Optical absorption studies are carried out on the glassy system in the wavelength range of 300– 600 nm. The cut-off wavelength λc, optical band gap Eopt, Urbach energy ΔE and refractive index n values were calculated from optical absorption data.
glass ceramics were prepared by controlled one step heat treatment method.
The crystal structure was investigated by using X-ray diffraction (XRD) and scanning electron microscopy (SEM).

## Slide 10
Results and Discussion.

## Slide 11: X-ray diffraction of glasses samples.

## Slide 12: Density measurements & calculation of Molar volume
Chart: Er2O3 mol%
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5
Molar Volume | 27.2533 | 26.9486 | 26.4292 | 26.0164 | 25.9509 | 25.0777
Density | 5.184 | 5.3136 | 5.43 | 5.559 | 5.616 | 5.856

## Slide 13: Differential Scanning Calorimetry (DSC)
Tg
Tc1
Tc2
Tg
Tc1
Tc2
Heat Flow (W/g)
100
300
500
700
900
Temperature (°C)
Er = 2.5 mol%
–––––––
Er = 2% mol%
–––––––
Er = 1.5 mol%
–––––––
Er = 1% mol%
–––––––
Er = 0.5 mol%
–––––––
Er = Zero mol%
–––––––
Exo Up
Universal V4.5A TA Instruments
Er = 2.5 mol%
Er = 1.5 mol%
Er = 2.5 mol%
Er = 1.5 mol%
–––––––
Er = 2.5 mol%
Er = 2% mol%
Er = 1.5 mol%
Er = 2.5 mol%

## Slide 14
Tg (K)
Ln (α)
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5

## Slide 15
1000/Tg
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α)
3.15
3.20
3.25
3.30
3.35
3.40
2.2
2.4
2.6
2.8
3.0
3.2
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α/Tg2)
1000/Tg
Glass Transition Activation Energy (Et)
The formula of [Kissinger’s], The formula of Moynihan C.
Ln(α / Tg 2) = (-Et / R Tg ) + const. Ln(α ) = (-Et / R Tg ) + const.
1000/Tg
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α)
3.15
3.20
3.25
3.30
3.35
3.40
2.2
2.4
2.6
2.8
3.0
3.2
Glass Transition Activation Energy (Et)
The formula of [Kissinger’s], The formula of Moynihan C.
Ln(α / Tg 2) = (-Et / R Tg ) + const. Ln(α ) = (-Et / R Tg ) + const.
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α/Tg2)
1000/Tg
1000/Tg
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α)
3.15
3.20
3.25
3.30
3.35
3.40
2.2
2.4
2.6
2.8
3.0
3.2
Glass Transition Activation Energy (Et)
The formula of [Kissinger’s], The formula of Moynihan C.
Ln(α / Tg 2) = (-Et / R Tg ) + const. Ln(α ) = (-Et / R Tg ) + const.

## Slide 16
Order of the crystallization reaction (n)
Deduce by using Ozawa method, ln[-ln(1-χ)] = n ln(α)
where  is (volume fraction crystallized in time (t) obtained from the crystallization exothermic peaks at the same temperature taken at different heating rates.

## Slide 17
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α)
1000/Tc1
TZNE 0
TZNE 0.5
TZNE 1
TZNE 1.5
TZNE 2
TZNE 2.5
Ln (α/Tc12)
1000/Tc1
Crystallization Activation Energy (Ec1)
The Kissinger model The Ozawa-Chen model
ln(α/T2) = (m/n)(Ec /RTc) + const ln(α) = (m/n)(Ec /RTc) + const

## Slide 18
TZNE 0
TZNE 0.5
TZNE 1
TZNE 2
TZNE 2.5
Ln (α)
1000/Tc2
TZNE 0
TZNE 0.5
TZNE 1
TZNE 2
TZNE 2.5
Ln (α/Tc22)
1000/Tc2
Crystallization Activation Energy (Ec2)
The Kissinger model The Ozawa-Chen model
ln(α/T2) = (m/n)(Ec /RTc) + const ln(α) = (m/n)(Ec /RTc) + const

## Slide 19
Sample | n |  | Eg (kJ/mol) | Eg (kJ/mol) | Ec1 (kJ/mol) | Ec1 (kJ/mol) | Ec1 (kJ/mol) | Ec2 (kJ/mol) | Ec2 (kJ/mol) | Ec2 (kJ/mol)
 | 1st peak | 2nd peak |  |  |  |  |  |  |  | 
TZNE0 | 2.89 | 2.04 | 90 | 85 | 169 | 159 | 117 | 150 | 136 | 111
TZNE0.5 | 1.64 | 1.75 | 132 | 127 | 106 | 93 | 224 | 145 | 129 | 166
TZNE1 | 1.71 | 1.82 | 163 | 158 | 95 | 82 | 216 | 162 | 146 | 524
TZNE1.5 | 1.86 |  | 106 | 101 | 75 | 88 | 255 | - | - | -
TZNE2 | 1.61 | 1.69 | 114 | 109 | 57 | 87 | 179 | 398 | 382 | 540
TZNE2.5 | 1.77 | 1.92 | 110 | 104 | 108 | 97 | 125 | 186.3167 | 169 | 97
Thermal kinetics parameters of TZNE glasses

## Slide 20: glass ceramics were prepared by controlled one step heat treatment method.
According to the DSC results, TZNE0 and TZNE2.5 as cast sample were heat treated at:-
Average Tg +50c for 4h and 22h
Average Onset temperature of 1st crystallization peak
Average crystallization temperature of 2nd crystallization peak
The crystal structure was investigated by using X-ray diffraction (XRD) and scanning electron microscopy (SEM).

## Slide 21
TZNE0.5 heat treated at average Tg +50c for 4h = (311 0c)
TZNE0.5 heat treated at average Tg +50c for 22h
= (311 0c)

## Slide 22
TZNE0.5 heat treated at Average Onset temperature of 1st crystallization peak
For 4h = (3500c)
TZNE0.5 heat treated at Average Onset temperature
of 1st crystallization peak For 4h = (3500c)

## Slide 23
TZNE0.5 heat treated at Average crystallization temperature of 2nd crystallization peak for 4h =(4600c)

## Slide 24
TZNE2.5 heat treated at average
Tg + 50c for 4h = (339 0c)
TZNE2.5 heat treated at average
Tg +50c for 22h = (339 0c)

## Slide 25
TZNE2.5 heat treated at average Onset temperature of 1st crystallization peak For 4h = (3550c)
TZNE2.5 heat treated at average Onset temperature of 1st crystallization peak For 8h = (3550c)

## Slide 26
TZNE2.5 heat treated at Average crystallization temperature of 2nd crystallization peak for 4h =(5200c)

## Slide 27
The Legend Phase | Particle Size (nm) | Annealing Time (hrs.) | Annealing Temperature | Sample
Er2TeO6 (210) | 55.58 | 8h | 350 | TZNE0.5
TeO2 (012) | 42.82 |  |  | 
ZnO (200) | 74.13 |  |  | 
Zn2 Te3O8 (100) | 46.86 | 4h | 460 | TZNE0.5
Zn2 Te3O8 (002) | 36.49 |  |  | 
Te O2 (110) | 54.04 |  |  | 
Te O2 (102) | 58.21 |  |  | 
Te O2 (212) | 36.52 |  |  | 
Er2TeO6 (202) | 71.02 | 8h | 355 | TZNE2.5
Er6Te5O19.2 (211) | 71.25 |  |  | 
Er6Te5O19.2 (111) | 71.35 |  |  | 
ZnO (111) | 47.37 | 4h | 520 | TZNE2.5
Er2O3 (111) | 30.47 |  |  | 
TeO2 (101) | 30.5 |  |  | 
TeO2(211) | 47.37 |  |  | 
The Legend Phase | Particle Size (nm) | Annealing Time (hrs.) |  | Sample
Er2TeO6 (210) | 55.58 | 8h |  | TZNE0.5
TeO2 (012) | 42.82 |  |  | 
ZnO (200) | 74.13 |  |  | 
Zn2 Te3O8 (100) | 46.86 | 4h |  | TZNE0.5
Zn2 Te3O8 (002) | 36.49 |  |  | 
Te O2 (110) | 54.04 |  |  | 
Te O2 (102) | 58.21 |  |  | 
Te O2 (212) | 36.52 |  |  | 
Er2TeO6 (202) | 71.02 | 8h |  | TZNE2.5
Er6Te5O19.2 (211) | 71.25 |  |  | 
Er6Te5O19.2 (111) | 71.35 |  |  | 
ZnO (111) | 47.37 | 4h |  | TZNE2.5
Er2O3 (111) | 30.47 |  |  | 
TeO2 (101) | 30.5 |  |  | 
TeO2(211) | 47.37 |  |  | 

## Slide 28
Optical properties UV/VIS absorption spectra
The optical absorption coefficient of each curve is calculated by equation:

## Slide 29
The (λcutoff) shifts towards lower wavelength side with increasing Er2O3 mol% concentration. This shifting is attributed increase in the number of the bridging oxygen (BO) atoms. glass network to become more rigid than non bridging oxygen
Chart: Er2O3 mol %
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5
 | 352 | 351 | 350 | 348 | 346 | 344
The Fundamental absorption edge

## Slide 30
Optical energy band gap and Urbach energy
Where n is equal to 1/2 for direct allowed transitions and 2 for indirect allowed transitions )