## Slide 1: NV centers in diamond: from quantum coherence to nanoscale MRI
Nir Bar-Gill
Hebrew University, Jerusalem, Israel
Quantum Conference 2016, London, March 14th 2016

## Slide 2: Outline
Introduction to NV centers in diamond
Quantum information processing – dynamical decoupling for better qubits
Noise spectroscopy of shallow NVs
Nanoscale NMR
Summary and outlook

## Slide 3: NV Physical Structure
Staggered face-centered-cubic lattice of C
Nearest-neighbor pair of substitutional Nitrogen and lattice Vacancy (NV)
Recent advances in diamond growth and implantation allow control of defect concentrations
N
V

## Slide 4
532 nm light pumps into the state
State read out from a fluorescence measurement before optical pumping occurs
Coherent spin manipulation with microwave fields at ~3GHz
Zeeman shift allows magnetometry along NV axis
NV- electronic structure
qubit

## Slide 5: NV Spin Decoherence
NV spin decoherence is due to fluctuating dipolar fields from N electron and 13C nuclear spins in environment
Focus on N-induced decoherence
N
N
N
V
13C
NV spin environment:
13C
Substitutional Nitrogen paramagnetic impurities
N
13C nuclear spin impurities

## Slide 6: Fighting decoherence: Hahn echo and dynamical decoupling
Efficient for slow noise
Use more 180 pulses to suppress faster noise – increase T2

## Slide 7: Enhanced coherence time through dynamic decoupling
N = 1 T2 = 250 ms
N = 512 T2 = 2.2 ms
L. M. Pham, N. Bar-Gill et. al, PRB 86, 045214 (2012)

## Slide 8: Low temperature: Increase T2 by a factor of 1000
At 77K: 1000 fold increase in T1
  achieve T2 = 0.6s
Achieve ms at TEC temperature
Nir Bar-Gill et. al., Nat. Commun. 4, 1743 (2013)

## Slide 9: Optimized dynamical decoupling for arbitrary states
Modified control sequences:
CPMG:
XY8:
Concatenated XY8:
D. Farfurnik et. al., PRB 92, 060301(R) (2015)

## Slide 10: Optimized dynamical decoupling for arbitrary states
Fidelity of quantum state (contrast):
simulation
experiment

## Slide 11: Optimized dynamical decoupling for arbitrary states
Coherence time ():
Achieve ms coherence time with a fidelity of 0.5

## Slide 12: Noise experienced by shallow NVs
Study noise experienced by shallow NVs as a function of depth, temperature, surface coating, magnetic field
Related recent work
  Degen group Rosskopf et. al., PRL 112, 147602
  Jayich group Myers et. al., PRL 113, 027602
Y. Romach et. al., PRL 114, 017601 (2015)

## Slide 13: Probing the spin-bath in Bulk
Dynamical decoupling pulse sequences (CPMG) are periodic in time
Act as a “lock-in” detector
N
N
N
V
13C
N. Bar-Gill et. al, Nat. Commun. 3, 858 (2012)
In bulk, extract Lorentzian spectrum
Notes: 13

## Slide 14: Shallow NV noise spectrum
Use decoherence measurements on several NVs to extract noise spectrum and compare to commonly encountered spectra (Lorentzian, 1/f)
Best fit to a double-Loretzian
  2 distinct noise sources (fast and slow)

## Slide 15: Two noise sources
Noise spectrum is described by a double-Lorentzian
- the coupling strength between noise component and the NV
- correlation time of noise component
We find slow (large ) and fast (small ) noise components

## Slide 16: Noise vs. NV depth
Correlation time () is independent of depth
  Intrinsic to the bath

## Slide 17: Noise vs. NV depth
Coupling strength () strongly depends on depths
  Low frequency noise exhibits dependence – spin bath
  High frequency noise has dependence – surface-modified phonons?

## Slide 18: Surface noise analysis
Identify 2 distinct noise sources
  Slow – surface spins controlled by spin-spin interactions
  Fast – surface modified phonons (?)
Additional studies still needed
  Various surface terminations/coatings (N- termination)
  Theoretical analysis of modified phononic behavior near diamond surface
  Nanoscale structures

## Slide 19: NMR Spectroscopy
Inductive detection
Macro-scale sample volume
Thermal spin polarization
Perform spectroscopy on nuclear spin species to extract physical, chemical and biological properties (e.g., structure, dynamics, chemical environment, etc.) of atoms and molecules
Conventional NMR

## Slide 20: NMR Spectroscopy
Optical detection
Nano-, micro-scale sample volume
Statistical spin polarization
NV Diamond NMR
S. DeVience et. al., Nat. Nanotech.,10, 129-134 (2015)

## Slide 21: NV Diamond NMR detection scheme
XY8-n
τ
2
τ
τ
τ
( )
π
2
x
( )
π
x
( )
π
y
( )
π
x
( )
π
y
τ
τ
τ
( )
π
y
( )
π
x
( )
π
y
τ
( )
π
x
τ
2
x n
( )
π
2
x
NV coherence
Free precession time τ

## Slide 22: NV Diamond NMR detection scheme
NV coherence
Free precession time τ
XY8-n
τ
2
τ
τ
τ
( )
π
2
x
( )
π
x
( )
π
y
( )
π
x
( )
π
y
τ
τ
τ
( )
π
y
( )
π
x
( )
π
y
τ
( )
π
x
τ
2
x n
( )
π
2
x
In the presence of a fluctuating magnetic field with characteristic frequency fac

## Slide 23: NV Diamond NMR detection scheme
NV coherence
Free precession time τ
XY8-n
τ
2
τ
τ
τ
( )
π
2
x
( )
π
x
( )
π
y
( )
π
x
( )
π
y
τ
τ
τ
( )
π
y
( )
π
x
( )
π
y
τ
( )
π
x
τ
2
x n
( )
π
2
x
In the presence of a fluctuating magnetic field with characteristic frequency fac

## Slide 24: NV Diamond NMR detection scheme
XY8-n
τ
2
τ
τ
τ
( )
π
2
x
( )
π
x
( )
π
y
( )
π
x
( )
π
y
τ
τ
τ
( )
π
y
( )
π
x
( )
π
y
τ
( )
π
x
τ
2
x n
( )
π
2
x
In the presence of a fluctuating magnetic field with characteristic frequency fac
NV coherence
Free precession time τ
τ0 = 1/(2fac)

## Slide 25: Multi-species NMR
Spectrally identify three spin species (proton, fluorine and phosphorous) using high-order pulse sequences

## Slide 26: MRI of fluorine
Partially coat diamond with SiO2, and then introduce fluorine
Image optically on a CCD

## Slide 27: Summary and outlook
NVs present a promising new platform for spin physics research and applications
  Nanoscale magnetic imaging
  Quantum information and computing
  Integrated spintronic and photonic devices
Outlook
  Magnetic sensing of various samples (thin layer magnets, bio, …)
  Improved sensitivity at low temperatures
  Improved sensitivity and coherence time through surface termination
  Interaction dominated quantum dynamics in spin ensembles
  Quantum thermodynamics
Notes: 27

## Slide 28: Optical readout: not perfect…
Signal strength
  Low photon flux (radiative lifetime ns)
  Low collection efficiency
Signal contrast
  Branching ratio between radiative and non-radiative transitions in the excited states
L. Childress, PhD thesis (2007)

## Slide 29: Purcell enhancement for improved spin readout
Enhance fluorescence rate (photon flux) and directionality (collection efficiency)
Affect contrast?
  Could modify the branching ratio between radiative and non-radiative transitions
SNR definition
  Measure combining photon flux and contrast
S. Wolf et. al., PRB 92, 235410 (2015)

## Slide 30: Plasmonic nano-antenna
Demonstrated for quantum dots (Ronen Rapaport)
Achieve directional emission and enhanced collection efficiency
  Metallic dielectric bullseye structure
  Collection efficiency of 30% with NA=0.55
Livneh et. al., ACS Photonics 2, 1669 (2015)

## Slide 31: Different spin-mixing terms
It is known that spin mixing occurs in the presence of optical excitation
The physics mechanism is unclear
  Radiative
  Non-radiative
Radiative
Non-radiative

## Slide 32: SNR vs. Purcell factor
The effect of Purcell enhancement on the SNR strongly depends on the nature of the spin mixing
  For non-radiatve mixing, and enhanced collection, could reach single-shot readout at PF<10
  Could be used to identify the underlying mechanism
Radiative
Non-radiative

## Slide 33: Summary
NVs present a promising platform for quantum information processing and quantum sensing
  Advantage – optical initialization and readout of quantum state
  Disadvantage – Weak coupling to optical degree of freedom and low photon flux
Purcell enhancement of optical readout
  Could improve photon flux and collection efficiency
  Performance dependent on physical mechanism of spin-mixing transitions
  Experimental studies under way…
Notes: 33