## Slide 1
Influence of the InAs/GaSb superlattice period composition on the electro-optical performances of T2SL infrared photodiode
P. Christol, M. Delmas, R. Rossignol, J.B. Rodriguez
Institut d'Electronique et des Systèmes (IES)
UMR-CNRS, Université de Montpellier, FRANCE.
Work supported by the French DGA
2015 OPTICS Conference
Valencia, September 2015
Université de Montpellier

## Slide 2
Antimonide (Sb)-based materials
a (Å)
Photonic research group of IES
University of Montpellier (France)
MWIR Laser diodes MWIR detectors
30µm
GaSb or InSb substrate
III-Sb (p)
III-Sb (n)
h
active zone
nid (~3µm)
InSb & InAsSb photodiodes
InAs/GaSb Superlattice (T2SL) photodiodes
contact layer
substrate
active
zone
0.6µm
SEM image of IR mesa photodiode
GaSb Substrate
metal
( p)
( n)
oxyde
SEM image of IR Laser diode
Pixel pin Photodiode
Laser diode
InAs/AlSb QCL
GaInAsSb EELs & VCSELs
MBE machine
RIBER compact 21E
GaSb, InAs, AlSb, InSb, (Ga,In,Al,As,Sb)

## Slide 3
InAs/GaSb heterostructure :
Type-III or type-II broken gap
band alignment
(InAs CB lower than GaSb VB)
*
InAs/GaSb type-II superlattice (SL)
InAs
GaSb
*
Electron minband
Hole minbands
d
absorption
SL = a periodic stacking of InAs and GaSb layers with a period d of a few nm thick
SL = coupled MQW  energy minibands  Fundamental absorption between V1C1
suitable for Infrared detection (3-30µm)
Type-II Superlattice (T2SL) photodiode
Buffer GaSb (p)
InAs (n)
GaSb (p)
Iph
A
h
InAs/GaSb
SL
SL : active zone of a pin junction
 T2SL Photodiode to compete
InSb and MCT high performance IR detectors
T2SL FPA commercially available (2015) :
IRNOVA, SCD, IRcamera
BUT works have to be done
to improve performances…

## Slide 4
Outline
Our motivation : study the influence of SL period composition (flexibility) on the performances of MWIR T2SL photodetector
Pixel pin Photodiode
GaSb (p) substrate
InAs (n)
GaSb (p)
InAs/GaSb
SL
Influence of SL period composition
on material-rich structure
on dimensionality
on residual type of doping
on electrical & electro-optical
performances
SL period
composition

## Slide 5
BC
BV
P
R=
InAs(ML)
GaSb(ML)
Symmetrical
period
5
Choice of SL period for MWIR domain
T=77K
(3Å=1ML)
Fundamental C1V1 energy

## Slide 6
BC
BV
P
R=
InAs(ML)
GaSb(ML)
Symmetrical
period
6
Choice of SL period for MWIR domain
T=77K
10/10
7/7
 MWIR spectral domain addressed by the same SL thickness ratio R
Photoluminescence spectra
(3Å=1ML)
Fundamental C1V1 energy

## Slide 7
7
R=
InAs(ML)
GaSb(ML)
BC
BV
InAs
GaSb
P
Asymmetrical
period
InAs-rich
GaSb-rich
T=77K
T=77K
Choice of SL period for MWIR domain
Fundamental C1V1 energy

## Slide 8
 Same bandgap energy addressed by different SL thickness ratio R
8
R=
InAs(ML)
GaSb(ML)
BC
BV
InAs
GaSb
P
Asymmetrical
period
InAs-rich
GaSb-rich
For a given band gap  different material-rich structures
T=77K
T=77K
Choice of SL period for MWIR domain
Fundamental C1V1 energy

## Slide 9
10/10
InAs/GaSb SL
7/4
InAs/GaSb SL
R=
InAs(ML)
GaSb(ML)
10/19
InAs/GaSb SL
Choice of SL period for MWIR domain
10/19 SL
10/10 SL
7/4 SL
 Same bandgap energy addressed by different SL thickness ratio R
 for cut-off wavelength around 5µm (@77K)

## Slide 10
10/19 SL
10/10 SL
7/4 SL
SL pin photodiodes have been fabricated by MBE
with active zone thickness of 1µm
Choice of SL period for MWIR domain
GaSb
10 nm
MBE growth control of InAs/GaSb superlattice on GaSb substrate
Mesa diodes & photodiodes
 Same bandgap energy addressed by different SL thickness ratio R

## Slide 11
GaSb-rich
InAs-rich
Symmetric
Photoresponse spectra
Same cut-off (5µm @ 77K) but photoresponse spectra strongly different !
 Influence of SL period composition on PR spectra

## Slide 12
GaSb-rich
InAs-rich
Symmetric
Same cut-off but MQW versus SL behavior
GaSb-rich
Symmetric
InAs-rich
MQW behavior
SL behavior
Photoresponse spectra

## Slide 13
- Spectral absorption shape is relative to the joined density of states
Anisotropic situation
in 3D space
Isotropic situation
in a D space
In the framework of
fractional dimensional space
Joined density of states
Density of states D
Energy ()
Photoresponse spectra
 Influence on dimensionality
- Photoresponse spectrum is proportional to the excitonic absorption

## Slide 14
77 K
J(-50mV)= 0.2µA/cm2
R0A = 3x105 .cm2
J(-50mV)= 3µA/cm2
R0A = 2x104 .cm2
J(-50mV)= 0.04µA/cm2
R0A = 2x106 .cm2
10/19 SL
(~110 periods)
10/10 SL
(~170 periods)
7/4 SL
(~300 periods)
GaSb-rich
InAs-rich
Same cut-off but electrical performances strongly different !
Electrical measurements
J(V) results

## Slide 15
J(V) results
Electrical measurements
15
Different cut-off but same electrical behavior for each kind of structure

## Slide 16
J(V) results
Electrical measurements
16
Intrinsic carrier concentration ni
R=1
Symmetric
R=2
« InAs-rich »
R=0.5
« GaSb-rich »
ni = f (Eg, T, m*eff )
High coupling
 small masses
 ni 
 JGR 
 Low Jdark value of InAs-rich SL
Different cut-off but same electrical behavior for each kind of structure

## Slide 17
J(V) results
Different cut-off but same electrical behavior for each kind of structure
Electrical measurements
17
%GaSb   GR 
 high Jdark value of GaSb-rich SL
Symmetric
InAs-rich
GaSb-rich
ONERA
77K
Carrier lifetime GR

## Slide 18
J(V) results
Different cut-off but same electrical behavior for each kind of structure
Electrical measurements
18
%GaSb   GR 
 high Jdark value of GaSb-rich SL
Symmetric
InAs-rich
GaSb-rich
 Ga-free InAs/InAsSb SL diode
Electrical performances of InAs/GaSb SL diode are strongly dependant on GaSb-content
ONERA
77K
Carrier lifetime GR

## Slide 19
Transport  type of SL material
Electrical measurements
Change in type of apparent conductivity
µn >> µP
Symmetric SL is p-type !!

## Slide 20
Transport  type of SL material
 | GaSb-rich (R=0.5) | Symmetric (R=1) | InAs-rich (R=2)
Residual carrier concentration (cm-3) | 3.5x1015 P-type | 2.5x1015 P-type | 8x1014 N-type
T = 77K
Electrical measurements
 Influence on type of doping

## Slide 21
2D
3D
Minority carriers : holes
Very low dark current
3D spectral shape
InAs-rich SL
N-type structure
Minority carriers : electrons (high QE)
High dark current
2D spectral shape
GaSb-rich SL
P-type structure
Influence of SL period composition
- same cut-off for different SL periods with different properties/performances
- same cut-off with n-type or p-type residual SL doping
21
Summary of results  Conclusion

## Slide 22
Minority carriers : holes
Very low dark current
3D spectral shape
InAs-rich SL
N-type structure
Minority carriers : electrons (high QE)
High dark current
2D spectral shape
GaSb-rich SL
P-type structure
Combine the advantages of each structure
Active zone
P-side of the junction
N-side of the junction
P+ contact
N+ contact
InAs-rich
Residual N-type
GaSb-rich
Residual P-type
22
Conclusion  Combined structure
 pn junction without doping the junction !

## Slide 23
Active zone P-side
N-side
Gradual periods
(%GaSb ↘)
P+ contact
N+ contact
InAs-rich
Residual N-type
GaSb-rich
Residual P-type
Cap InAs n+=5.1017cm-3 20nm
SL 7ML InAs/4ML GaSb N.i.D 200nm
GaSb (P) Substrate
SL 11ML InAs/20ML GaSb N.i.D 1.5μm
SL 11ML InAs/16ML GaSb N.i.D 50nm
SL 11ML InAs/20ML GaSb p+=5.1017cm-3 130nm
SL 7ML InAs/4ML GaSb n+=5.1017cm-3 100nm
SL 9ML InAs/8ML GaSb N.i.D 50nm
SL 10ML InAs/12ML GaSb N.i.D 50nm
MWIR T2SL photodiode combining SL properties
Conclusion  Combined structure

## Slide 24
GaSb (P) Substrate
Cap InAs n+=5.1017cm-3 20nm
SL 7ML InAs/4ML GaSb N.i.D 200nm
SL 11ML InAs/20ML GaSb N.i.D 1.5μm
SL 11ML InAs/16ML GaSb N.i.D 50nm
SL 7ML InAs/4ML GaSb n+=5.1017cm-3 100nm
SL 9ML InAs/8ML GaSb N.i.D 50nm
SL 10ML InAs/12ML GaSb N.i.D 50nm
HR-XRD spectrum
SL 11ML InAs/20ML GaSb p+=5.1017cm-3 130nm
MWIR T2SL photodiode combining SL properties
Conclusion  Combined structure

## Slide 25
- 2D spectral shape (as GaSb-rich SL)
- Dark current is lower than the GaSb-rich period but slightly higher than the InAs-rich period
        … in progress
MWIR T2SL photodiode combining SL properties
Conclusion  Combined structure

## Slide 26
Thank you for your attention
Our recent publications on T2SL photodiodes
M. Delmas et al “Midwave infrared InAs/GaSb superIattice photodiode with a dopant-free p-n junction”
Infrared Physics & Technology, 70, 76 (2015)
E. Giard, et al “ Influence of the p-type doping on the radiometric performances of MWIR T2SL photodiodes”
Infrared Physics & Technology, 70, 103 (2015)
M. Delmas et al “Electrical modeling of InAs/GaSb superlattice mid-wavelength infrared pin photodiode to analyze experimental dark current characteristics”
Journal of Applied Physics 116, 113101-7 (2014)
E. Giard, et al “Quantum efficiency investigations of type-II InAs/GaSb MWIR superlattice photodetectors”
Journal of Applied Physics 116, 043101-6 (2014)
R. Taalat et al “Influence of the period thickness and composition on the electro-optical properties of type-II InAs/GaSb midwave infrared superlattice photodetector”.
Journal of Physics D : Applied Physics 47, 015101-7 (2014)