## Slide 1: About Omics Group
OMICS Group International through its Open Access Initiative is committed to make genuine and reliable contributions to the scientific community. OMICS Group hosts over 400 leading-edge peer reviewed Open Access Journals and organize over 300 International Conferences annually all over the world. OMICS Publishing Group journals have over 3 million readers and the fame and success of the same can be attributed to the strong editorial board which contains over 30000 eminent personalities that ensure a rapid, quality and quick review process.

## Slide 2: About Omics Group conferences
OMICS Group signed an agreement with more than 1000 International Societies to make healthcare information Open Access. OMICS Group Conferences make the perfect platform for global networking as it brings together renowned speakers and scientists across the globe to a most exciting and memorable scientific event filled with much enlightening interactive sessions, world class exhibitions and poster presentations
Omics group has organised 500 conferences, workshops and national symposium across the major cities including SanFrancisco,Omaha,Orlado,Rayleigh,SantaClara,Chicago,Philadelphia,Unitedkingdom,Baltimore,SanAntanio,Dubai,Hyderabad,Bangaluru and Mumbai.

## Slide 3
Quantum interference effects and molecular electronics
Philippe Lafarge
Université Paris Diderot, CNRS, Paris, France
philippe.lafarge@univ-paris-diderot.fr
Optics 2014 - sept. 10, 2014

## Slide 4
R. A. Webb et al., Phys. Rev. Lett. 54, 2696 (1985)
Aharonov-Bohm effect in a metal ring
phase coherent transport
phase shift controlled by magnetic flux
= p F/F0
PQM = |A1 + A2|2
quantum interference
Quantum interference in mesoscopic systems

## Slide 5
MOLECULES
Nanoscale structures
chemically active
Cost-effective
Molecular electronics
Monolayer molecular junctions
Based on self assembled monolayers (SAMs)
Mechanically controlled break-junctions
One or a few molecules connected
Molecular junctions
Need to probe the electronic properties of molecules !
Electronic components made with molecules ?
M. L. Perrin et al. Nat Nano
2013, 8, 282-287
R. McCreery et al. Phys. Chem. Chem. Phys. 2013, 15, 1065
D. Fracasso et al. J. Am. Chem. Soc. 2011,133, 9556-9563
Solid state planar junction
Millions of molecules are connected thanks to electrografting
Molecular junctions
Quantum interference
Simulations
Experimental results
Conclusions and perspectives

## Slide 6
Quantum interference
Molecular junctions
Quantum interference
Simulations
Experimental results
Conclusions and perspectives
Electron transport through a single benzene molecule connected in
ortho, para or meta.
No QI
T. Markussen et al. Nano Lett. 10, 4260-4265 (2010)
Destructive QI
The connection between the molecule and the electrodes influences the
electronic properties described by the electronic transmission probability TLR(E)
TLR (EF) ≠ 0
TLR (EF) = 0
C. R. Arroyo et al. Ang.Chem., 125, 3234-3237 (2013)
P. Sautet, C. Joachim, Chem. Phys. Lett., 153, 511 (1988)
L
R
ortho
para
L
R
L
R
meta

## Slide 7
QI and molecular structure
linearly conjugated
cross conjugated
Only 1 path allowed
2 phase-opposed electronic paths
Constant transmission function at Ef
Antiresonance in the transmission function
T(Ef) = 0
Anthracene (AC)
Anthraquinone (AQ)
C.M.Guédon et al. Nat Nano. 7, 305-309 (2012)
(Localized Molecular Orbitals)
Energy diagrams
G. Solomon et al. ChemPhysChem, 10, 257-264 (2009)
MOLECULE
para
para
L
R
L
R
Destructive QI
No QI
Molecular junctions
Molecular junctions
Quantum interference
Simulations
Experimental results
Conclusions and perspectives

## Slide 8
First experimental evidences
In SAMs of AC and AQ arylethynylene thiolates with eutectic Ga-In top contacts
C.M.Guédon et al. Nat Nano. 7, 305-309 (2012)
D. Fracasso et al., JACS 133, 9556 (2011)
From an indirect measurement of AQ and AC based SAMs, statistical analysis
two-dimensional histograms
In AQ based molecular junctions from a direct measurement of the conductance curves
tunneling barrier model
30 x 30 mm2
300 K
4 K
Rabache et al., JACS 135, 10218 (2013)
AC-DT
AQ-MT
C-AFM
IAQ(V) < IAC(V)
dI/dV vs V
Molecular junctions
Quantum interference
Simulations
Experimental results
Conclusions and perspectives

## Slide 9
Transmission function calculation
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
C.W. Groth et al. a software package for quantum transport, arXiv: 1309.2926
Key role played by the way the molecules are connected to the electrodes.
Tight binding approach applied to charge transport (KWANT)
Para - anthracene
Meta-anthracene
Para-anthraquinone
Parameters
On site energies = 0eV / Coupling energies = -3eV / Coupling to the electrodes = -1eV

## Slide 10
Simulations for anthracene
para-para-para
para-para-meta
para-meta-para
QI
QI
no QI
C.W. Groth et al. a software package for quantum transport, arXiv: 1309.2926
para
para
para
meta
para
para
meta
para
para
One meta connection in a chain is enough to make QI occur
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives

## Slide 11
Recent theoretical predictions
Structures in the dI/dV curves
Influence of the temperature on QI effects
T. Markussen et al. Phys.Rev.B, 89, 085420 (2014)
No thermal activation
Dependence on the alignment of the transmission node and the Fermi level (blue and red lines)
el-ph interactions (solid lines)
T(E)
ΔEF
HOMO
LUMO
E
Steps visible a low T with el-ph interactions (solid blue line), not visible at RT (solid red line)
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
Bias voltage (V)
dI/dV (G0)

## Slide 12
Fabrication of the junctions
Si
SiO2
resist
Optical mask
UV light
Optical lithography
Development
Metallic deposition
Lift off
Postive resist with a positive mask
To carve the design of the electrode
Ti
Au
Au ~ 50nm
Ti ~ 2-3nm
Aceton bath
Bottom electrode
electrografting
Optical lithography
Development
Metallic deposition
+ lift off
Top electrode
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives

## Slide 13
Fabrication of the junctions
Profile view (schematic)
Crossed bar geometry junctions (optical image x 20)
Samples made with 24 junctions of 20x20μm2
Formation of organic film by reduction of diazonium salt
Final solid state planar junctions (cross bar geometry)
AQ
precursor
ACN
NBu4BF4
+e-
Au
9,10-dioxo-1-anthracenediazonium (AQD)
NH2
N2+
AQ
diazonium salt
junction
P. Martin, J.-C. Lacroix, ITODYS lab, Paris Diderot University
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
Au
Molecular layer
Au

## Slide 14
Conductance measurements
Antiresonance dip at 4K, lower visibility at 300K
Temperature dependent structures at low T
Au/ AQ /Au junctions
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
Junction 1
20x20μm2
G (V) vs bias voltage
Junction 2
20x20μm2
G (V = 0) vs bias voltage

## Slide 15
Conductance vs temperature
Experimental behaviour (blue line) similar to the one predicted for single molecule junctions with el-ph interactions (red line)
Decoherence by electron phonon coupling ?
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
G (V= 0) vs temperature
Vn = 2(ε + nhν)
Energy of the structures vs the position
T. Markussen, 2014 private communication
Experimental fit !

## Slide 16
Anthracene based junctions
Antiresonance dip at 4K, lower visibility at 300K as for the AQ-based junctions
Temperature dependent structures at low T
Au / AC /Au based junctions
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
Junction 3
Junction 4
20x20μm2
20x20μm2
G (V) vs bias voltage
G (V = 0) vs bias voltage

## Slide 17
Temperature dependence
Experimental behaviour similar to the one predicted for single and AQ based junctions
Decoherence by electron phonon coupling ?
Vn = 2(ε + nhν)
U (mV)
n° peak
Same vibrational modes as for the AQ excited
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
G (V= 0) vs temperature
Energy of the structures vs the position

## Slide 18
QI vs tunnel behaviour
Molecular junction and tunneling
Al (50nm)
Al (50nm)
Al2O3 (~ nm)
4K
Metallic tunnel junctions
Different shapes at low T
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
Al / Al2O3 /Al

## Slide 19
Conclusions and perspectives
Large area solid state molecules based junctions (with AQ, AC, oxides…)
Direct measurement of large antiresonance dip in dI/dV curves with a strong temperature dependence.
Additional structures at low T that could be the signatures of vibrational modes of the organic layer.
Giant thermoelectric effect predicted in molecular junctions where QI occur…
J.P. Bergfield and C.A. Stafford, NanoLett. 9, 3072 (2009)
J.P. Bergfield, M.A. Solis and C.A. Stafford, ACS Nano 4, 5314 (2010)
Molecular junctions
Quantum interferences
Simulations
Experimental results
Conclusions and perspectives
μ-μnode(eV)

## Slide 20
MPQ Lab, Paris Diderot University
Maria Luisa Della Rocca, Clément Barraud, Charlotte Bessis, Julien Chaste, Philippe Petit
ITODYS, Paris Diderot University
Pascal Martin, Jean-Christophe Lacroix
University of Alberta
Richard L. McCreery
Copenhagen, Quantum Wise
Troels Markussen
Thank you

## Slide 21: Let Us Meet Again
We welcome all to our future group conferences of Omics group international
Please visit:
www.omicsgroup.com
www.Conferenceseries.com
http://optics.conferenceseries.com/