## Slide 1: Effects of thermal cycles and immersion in different beverages on color, translucency and hardness of different composite resins
PINAR GUL
Atatürk University, School of Dentistry, Turkey

## Slide 2: INTRODUCTION
Resin-based composites (RBCs) are becoming more popular in restorative dentistry, particularly because of their superior esthetic outcomes.
RBCs typically consist of a methacrylate-based resin matrix, glass or ceramic fillers and a filler-matrix coupling agent. For the monomer matrix, bisphenol A glycol dimethacrylate (Bis-GMA), triethylene glycol dimethacrylate (TEGDMA), and urethane dimethacrylate (UDMA) are widely used in dental composites (Fong et al 2005; Sideridou et al 2005; Moszner et al 2001)

## Slide 3
In addition to these dimethacrylate based composite material, which are based on cross-linking dimethacrylates and inorganic fillers, a new type of inorganic-organic hybrid dental material, known as Ormocers, has been developed. A considerable widening of the adjustable properties is obtained through the possible incorporation of different fillers in the Ormocer composite (up to 67 vol %). The addition of fillers may bring an improvement of the mechanical and physical properties of this class of composites, such as small abrasion rate, low water absorption, and low water solubility (Cunha et al. 2003).

## Slide 4
It is noteworthy that the monomer matrix strongly influences the polymerization, reactivity, mechanical properties, and water sorption of RBCs. Under oral conditions, RBCs may be exposed either intermittently or continuously to chemical agents found in saliva, food, and beverages (Asmussen 1984; Wu et al 1982; Yap e al 2001). Consequently, the leaching of composite fillers and the disintegration of filler-resin interface (silane coupling agent) can also occur under oral conditions (Oysaed and Ruyter 1986).

## Slide 5
The silorane-based composite (SBC) exhibited low polymerization shrinkage due to the ring-opening oxirane monomer and increased hydrophobicity due to the presence of the siloxane species (Lee et al 1998). Compounds containing oxirane groups are reactive with water.

## Slide 6
On the other hand, like some other silicon-containing monomers, siloranes can be extremely hydrophobic, possibly making the oxirane groups inaccessible to attack by water or water-soluble species (Eick et al 2006).
Palin et al. reported that the silorane composite exhibited significantly lower water sorption, solubility and associated diffusion coefficient than the established methacrylate-based dental composites (Palin et al.2005)

## Slide 7
With MBCs, polymerization shrinkage and diffusion of moisture through the resin component lead to the initiation and propagation of microcracks in the resin matrix.
This process could provide a supply of chemical agents and a path for further diffusion into the restorative material, thereby resulting in more rapid degradation (Lee etal 1995).

## Slide 8
Clinically, this can lead to a loss of restoration contour, as well as an increase in surface roughness, and discoloration (Correr et al 2012; Bollen et al 1997). Generally, the optical and physical properties of resin composites are affected by the length of degradation (Moon et al 2015).

## Slide 9
Color plays an important role in obtaining optimum aesthetics. The increasing patient’s demand for improved esthetics has created greater demand restorative materials with excellent esthetic properties.

## Slide 10
In the present study, CIE L*a*b* color system was chosen to measure color differences.
ΔE values less than 3.3 were considered as clinically acceptable (Ruyter et al 1987) .

## Slide 11
Translucency is a property of a material that allows the passage of light but disperses the light so that objects cannot be seen clearly through the material. Therefore, translucency can be described as a state intermediate between complete opacity and transparency (Powers 2006).
The translucency of dental resin composites depends on their thickness as well as the scattering and absorption coefficients of the resin, filler particles, pigments and opacifiers. In addition, the water sorption of a resin monomer might lead to different translucency changes in composites (Johnston and Reisbick 1997; Kim and Lee 2007; Miyagawa et al 1981).

## Slide 12
Translucency of esthetic restorative materials has usually been determined with the translucency parameter (TP) (Johnston and Kienle 1995).

## Slide 13
Properties of resin composites were changed after thermocycling by thermal fatique, and the influence of thermal fatique was different by the properties of material (Yap et al 2004).
Color change of resin composite was perceivable after thermocycling (Lee et al 2001).

## Slide 14
Some authors (Mckenzie et al 2004; Pimenta et al 1997; Sarret et al 2000) believe that color alteration also occurs due to the weakening of the resin/load bond, resulting in a reduction in the translucency of the material due to the migration of colored products into the resin matrix, promoting change in the restoration color and leading to the need for its subsequent replacement.

## Slide 15
The surface microhardness of resin obtained after polymerization is an important physical property with regard to maintaining the color and degree of polymerization (Barghi et al 1994; Gouvea et al 1011).
The difference in hardness of the materials after immersion in different stain solutions may be attributed to their chemical composition and the effect the liquids had on different chemical components.

## Slide 16
In low pH drinks, resins show a high solubility and that solubility causes surface erosion and dissolution, which will affect the wear and hardness of the resins (Abu-Bakr et al 2000).

## Slide 17
The null hypothesis of the present study was that there was no significant difference in the changes of color, translucency and hardness of composite resins after thermocycling and immersion beverages.

## Slide 18: Aim
The aim of this study is to evaluate the color stability, translucency and hardness of eight different composite resins, after thermal cycling and immersion in beverages.

## Slide 19: MATERIALS AND METHODS
A total of 120 disk-shaped, composite resin specimens were prepared by using eight different composite materials (15 from each, 8x2 mm).
Details of the investigated restorative materials are presented in Table 1.

## Slide 20: Table. 1 Details of the investigated restorative materials.
Product | Manufacturer | Type | Content |  |  |  | Batch No.
 |  |  | Organic Matrix | Fillers | Particle Size | Filler Load (wt-v)% | 
Clearfil Majestry Esthetic | Kuraray Medical, Okayama, Japan | Nanohybrid | Bis-GMA, aromatic dimethacrylate | Silanated barium glass, filler, prepolymerized nano-organic filler | 0.7 μm, 20 nm | 78-66 | 00034A
Clearfil Majestry Posterior | Kuraray Medical | Nanosuperfilled | Bis-GMA, TEGDMA, aromatic dimethacrylate | Silanated glass ceramic filler, surfacetreated alümina microfiller | 1.5 μm, 20 nm | 92-82 | 0011OA
Grandio | VOCO GmbH Cuxhaven Germany | Nanohybrid | Bis-GMA, TEGDMA, UDMA | Glass-ceramic (microfiller) Si02 (nanofiller) | 1 µm 20-60 nm | 87-71.4 | 1117206
Grandio Flow | VOCO GmbH Cuxhaven Germany | Flowable Nanohybrid | Bis-GMA, TEGDMA, | silicium dioxide, glass ceramic particles | SiO2-nano particles (40 nm) glass fillers (1μm) | 80.2-65.7 | 1127403
Filtek Silorane | 3M ESPE, St. Paul, Minn. | Silorane | Siloranes | Quartz, yttrium fluoride | 0.47 μm | 76 | N132573
Admira | VOCO GmbH Cuxhaven Germany | Ormocer | Ormocer, Bis-GMA, UDMA | Ba-Al-B-silicate glass, SiO2 | 0.7 μm | 78-56 | 1034200
Arabesk Top | VOCO GmbH Cuxhaven Germany | Microhybrid | Bis-GMA, TEGDMA, UDMA | Bariumaluminiumsilicate glass, Lithium aluminium silicate glass ceramic, | 0.7 μm | 77-56 | 1051274
Valux Plus | 3M ESPE | Hybrid | Bis-GMA, TEGDMA | Silanetreated ceramic | 0.01-3.5 μm | 80-71 | N252857
Abbreviations: Bis-GMA: bisphenol A glycidyl methacrylate; TEGDMA: triethylene glycol dimethacrylate; UDMA: urethane dimethacrylate

## Slide 21
Colour was measured according to the CIELAB colour scale relative to standard illumination D65, against a standard white background
(L= 93.6 a= 1.5 b= -3.0) with a dental spectrophotometer (Shadepilot, DeguDent GmbH, Hanau, Germany).

## Slide 22
Color change values (ΔEab*) were analyzed for each restorative material with the following equation:
ΔEab*= [(ΔL*)2 +(Δa*)2 +(Δb*)2 ]1/2
The discoloration that is ΔE*ab > 3.3 was considered visually perceptible and clinically unacceptable (Ruyter et al 1987; Vichi et al 2004; Çelik et al 2009).

## Slide 23
In addition, the following equation was used to calculate the translucency parameter of the materials (Choi et al 2006; Woo et al 2008):
TP = [(L W- L B )2 + (a W-a B )2 + ( bW- bB)2]1/2
where the subscripts W and B are the CIELAB values of the materials on the white (L= 93.6 a= 1.5 b= -3.0) and black (L= 19.4 a= 0.5 b= 2.5) tiles, respectively.

## Slide 24
Then, baseline microhardness of specimens was measured. A Vickers diamond indenter was used in a microhardness tester (Micromet 2001, Buehler, Illinois, USA) for specimen indentation. For each microhardness test, two indentations were made randomly on the top and bottom surfaces of each specimen using a load of 10 g for 15 seconds.
All hardness values were expressed in Vickers hardness, where 1 HV=1.854 P/d2, with P being the indentation load and d the diagonal length.

## Slide 25
After the baseline color, translucency and hardness measurement, thermocycling was performed for 1000 cycles using distilled water (between 5 and 55°C), with a dwell time of 20 s.

## Slide 26
To evaluate the color stability in different solutions, 15 specimens from each composite resin were subdivided into three subgroups of five specimens each, which were immersed in two different solutions (Coffee and Red Wine). Distilled water served as a control solution.
The specimens of each composite resin were individually immersed in vials containing 10 ml of Coffee (2 g of coffee powder was dissolved in 200 ml of boiling water as per the manufacturer’s recommendations: Coffee (Nescafe Classic, Nestle, Turkey; pH 5.50), red wine (DLC Öküzgözü 2009, Doluca, Turkey: pH 3.28), for 3 hours a day at room temperature over a 30-days immersion period.

## Slide 27
After these daily immersion periods, the samples were washed with distilled water and then stored in distilled water at 37°C. The solutions were renewed daily.

## Slide 28
Color, translucency and hardness of each sample were re-measured baseline, after thermal cycles and after one-month staining periods.

## Slide 29
Statistical analysis was performed using statistical software, SPSS version 18.0 (SPSS Inc., Chicago, IL, USA). Repeated-measures analysis of variance (ANOVA) was performed to identify significant differences among the resins, the solutions and periods, and all interactions between them. The Bonferroni test was used for post-hoc analysis. All data were analyzed at a significance level of 0.05.

## Slide 30: RESULTS
Tables 2-4 show the interactions among color, translucency and hardness values of composite resins baseline, after thermal cycles and after coloration respectively.
Repeated-measures ANOVA revealed that there was significant differences among the periods, resins and the solutions used (distilled water, coffee and red wine) (P<0.05).

## Slide 31: Table 2. Repeated-measures analysis of variance (ANOVA) for color change (ΔE*ab) values of restorative materials and staining solutions
*P<.05 indicates statistically significant difference.

## Slide 32: Table 3. Significance of translucency parameter (TP) values among comparisons of restorative materials and staining solutions
*P<.05 indicates statistically significant difference.

## Slide 33: Table 4. Significance of hardness values among comparisons of restorative materials and staining solutions
*P<.05 indicates statistically significant difference.

## Slide 34
Red wine and coffee caused perceptible discolorations in all composite resin materials (△E>3.3). Discoloration was higher for Grandio Flow than other resins (Table 5, Figure 1.).

## Slide 35: Table 5. Mean (Standard Deviation) and multiple comparisons of ΔE*ab values baseline, after thermal cycles and coloration
Composite Materials | Solutions | Baseline | After TC | After Coloration | Mean Difference (Period 3-1)
Clearfil Majestry Esthetic | DW | 0.78 (0.50) | 0.74 (0.38) | 0.66 (0.23) | -0.12
 | CF | 0.62 (0.23) | 1.12 (0.28) | 4.06 (0.38)* | 3.44
 | RW | 0.72 (0.29) | 0.80 (0.16) | 19.84 (3.44)* | 19.12
Clearfil Majestry Posterior | DW | 0.52 (0.25) | 1.24 (0.42) | 0.70 (0.44) | 0.18
 | CF | 0.74 (0.31) | 0.96 (0.45) | 8.72 (0.70)* | 7.98
 | RW | 1.16 (0.71) | 1.36 (0.76) | 17.40 (1.34)* | 16.24
Grandio | DW | 0.80 (0.46) | 1.86 (0.51) | 1.30 (0.16) | 0.50
 | CF | 0.60 (0.10) | 1.34 (0.46) | 5.10 (0.58)* | 4.50
 | RW | 0.72 (0.27) | 1.56 (0.49) | 17.12 (0.71)* | 16.40
Grandio Flow | DW | 0.48 (0.16) | 1.30 (0.26) | 1.36 (0.11) | 0.88
 | CF | 0.58 (0.13) | 1.48 (0.28) | 9.26 (0.69)* | 8.68
 | RW | 0.90 (0.10) | 1.34 (0.72) | 24.36 (2.09)* | 23.46
Filtek Silorane | DW | 1.18 (0.55) | 2.38 (0.91) | 2.16 (0.51) | 0.98
 | CF | 0.86 (0.11) | 2.40 (0.65) | 3.76 (0.48)* | 2.74
 | RW | 0.82 (0.40) | 2.40 (0.48) | 13.58 (0.87)* | 12.76
Admira | DW | 0.40 (0.25) | 1.30 (0.42) | 1.28 (0.32) | 0.88
 | CF | 0.84 (0.43) | 1.38 (0.51) | 4.74 (0.69)* | 3.90
 | RW | 0.80 (0.35) | 1.56 (0.67) | 17.90 (0.85)* | 17.10
Arabesk Top | DW | 0.88 (0.66) | 1.94 (0.65) | 1.68 (0.81) | 0.80
 | CF | 0.54 (0.40) | 1.56 (0.63) | 3.56 (0.46)* | 3.02
 | RW | 0.40 (0.19) | 1.56 (0.48) | 17.52 (1.06)* | 17.12
Valux Plus | DW | 0.56 (0.21) | 2.22 (0.81) | 2.64 (0.76) | 2.08
 | CF | 0.66 (0.35) | 2.00 (0.92) | 6.40 (0.98)* | 5.74
 | RW | 0.54 (0.30) | 2.82 (0.32) | 16.14 (1.94)* | 15.60
Bold numbers in table represents statistical differences (p<0.05). (TC: Thermal Cycles, DW: distilled water, CF coffee, RW: red wine)*Indicates clinically unacceptable value (ΔE*ab<3.3)

## Slide 36: Figure 1. ΔE*ab values baseline, after thermal cycles and coloration
Chart: 
| DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | Clearfil Majestry Esthetic | Clearfil Majestry Posterior | Grandio | Grandio Flow | Filtek Silorane | Admira | Arabesk Top | Valux Plus
Baseline | 0.78 | 0.62 | 0.72 | 0.52 | 0.74 | 1.16 | 0.8 | 0.6 | 0.72 | 0.48 | 0.58 | 0.9 | 1.18 | 0.86 | 0.82 | 0.4 | 0.84 | 0.8 | 0.88 | 0.54 | 0.4 | 0.56 | 0.66 | 0.54
After TC | 0.74 | 1.12 | 0.8 | 1.24 | 0.96 | 1.36 | 1.86 | 1.34 | 1.56 | 1.3 | 1.48 | 1.34 | 2.38 | 2.4 | 2.4 | 1.3 | 1.38 | 1.56 | 1.94 | 1.56 | 1.56 | 2.22 | 2 | 2.82
After Coloration | 0.66 | 4.06 | 19.84 | 0.7 | 8.72 | 17.4 | 1.3 | 5.1 | 17.12 | 1.36 | 9.26 | 24.36 | 2.16 | 3.76 | 13.58 | 1.28 | 4.74 | 17.9 | 1.68 | 3.56 | 17.52 | 2.64 | 6.4 | 16.14

## Slide 37
The effect of thermal cycles on color and transluceny of resins was no statistically significant (P>0.05) (Tables 5 and 6, Figure 2). The null hypothesis of the present study was partially rejected due to this result.
TP values of composite resins generally decreased especially after immersion in red wine (P<0.05) (Figure 2).

## Slide 38: Table 6. Mean (Standard Deviation) and multiple comparisons of translucency parameter values baseline, after thermal cycles and coloration
Composite Materials | Solutions | Baseline | After TC | After Coloration | Mean Difference (Period 3-1)
Clearfil Majestry Esthetic | DW | 14.72 (0.28) | 14.24 (0.29) | 14.50 (0.24) | -0.22
 | CF | 14.36 (0.49) | 14.30 (0.44) | 13.70 (0.52) | -0.66
 | RW | 14.82 (0.76) | 14.62 (0.56) | 9.38 (0.90) | -5.44
Clearfil Majestry Posterior | DW | 13.54 (0.35) | 14.04 (0.59) | 13.72 (0.33) | 0.18
 | CF | 13.40 (0.48) | 13.20 (0.49) | 11.46 (0.97) | -1.94
 | RW | 13.70 (0.29) | 13.86 (0.80) | 9.48 (0.41) | -4.22
Grandio | DW | 17.60 (0.61) | 17.46 (0.72) | 16.88 (0.76) | -0.72
 | CF | 17.38 (0.25) | 17.30 (0.38) | 16.98 (0.69) | -0.40
 | RW | 17.26 (0.30) | 16.92 (0.59) | 12.12 (0.95) | -5.14
Grandio Flow | DW | 16.66 (0.22) | 16.64 (0.15) | 16.78 (0.26) | 0.12
 | CF | 16.74 (0.11) | 16.72 (0.27) | 15.82 (0.83) | -0.92
 | RW | 17.44 (0.43) | 16.90 (0.57) | 14.36 (3.90) | -3.08
Filtek Silorane | DW | 11.04 (0.59) | 11.32 (0.62) | 12.80 (0.24) | 1.76
 | CF | 11.10 (0.60) | 11.24 (0.63) | 11.54 (0.70) | 0.44
 | RW | 11.42 (0.47) | 11.74 (0.22) | 10.94 (1.42) | -0.48
Admira | DW | 14.54 (0.21) | 14.30 (0.51) | 14.40 (0.37) | -0.14
 | CF | 14.66 (0.30) | 14.00 (0.44) | 13.72 (0.56) | -0.94
 | RW | 14.58 (0.74) | 14.02 (0.35) | 10.74 (0.28) | -3.84
Arabesk Top | DW | 15.10 (0.48) | 14.84 (0.60) | 15.08 (0.52) | -0.02
 | CF | 15.14 (0.30) | 14.92 (0.33) | 14.54 (0.39) | -0.60
 | RW | 15.70 (0.48) | 14.90 (0.69) | 10.72 (0.95) | -4.98
Valux Plus | DW | 14.54 (0.30) | 14.12 (0.54) | 14.08 (0.28) | -0.46
 | CF | 15.04 (0.45) | 14.62 (0.65) | 14.26 (0.39) | -0.78
 | RW | 14.50 (0.17) | 14.38 (0.51) | 9.9 (0.73) | -4.60
Bold numbers in table represents statistical differences (p<0.05). (TC: Thermal Cycles, DW: distilled water, CF coffee, RW: red wine)

## Slide 39: Figure 2. TP values baseline, after thermal cycles and coloration
Chart: 
| DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | Clearfil Majestry Esthetic | Clearfil Majestry Posterior | Grandio | Grandio Flow | Filtek Silorane | Admira | Arabesk Top | Valux Plus
Baseline | 14.72 | 14.36 | 14.82 | 13.54 | 13.4 | 13.7 | 17.6 | 17.38 | 17.26 | 16.66 | 16.74 | 17.44 | 11.04 | 11.1 | 11.42 | 14.54 | 14.66 | 14.58 | 15.1 | 15.14 | 15.7 | 14.54 | 15.04 | 14.5
After TC | 14.24 | 14.3 | 14.62 | 14.04 | 13.2 | 13.86 | 17.46 | 17.3 | 16.92 | 16.64 | 16.72 | 16.9 | 11.32 | 11.24 | 11.74 | 14.3 | 14 | 14.02 | 14.84 | 14.92 | 14.9 | 14.12 | 14.62 | 14.38
After Coloration | 14.5 | 13.7 | 9.38 | 13.72 | 11.46 | 9.48 | 16.88 | 16.98 | 12.12 | 16.78 | 15.82 | 14.36 | 12.8 | 11.54 | 10.94 | 14.4 | 13.72 | 10.74 | 15.08 | 14.54 | 10.72 | 14.08 | 14.26 | 9.9

## Slide 40
Hardness values varied among composite resins but generally decreased after thermal cycles and immersion especially in red wine (Table 7) (Figure 3).
Filtek Silorane and Admira showed better results than methacrylate based composites in terms of the color, translucency and hardness (p<0.05) (Tables 5-7).

## Slide 41: Table 7. Mean (Standard Deviation) and multiple comparisons of hardness values baseline, after thermal cycles and coloration
Composite Materials | Solutions | Baseline | After TC | After Coloration | Mean Difference (Period 3-1)
Clearfil Majestry Esthetic | DW | 56.4 (1.34)a | 44.8 (1.10)b | 38.8 (1.10)c | -17.60
 | CF | 51.2 (1.64)a | 47.0 82.24)a | 41.2 (1.10)b | -10.00
 | RW | 47.6 (2.19)a | 50.2 (1.10)a | 37.2 (0.45)b | -10.40
Clearfil Majestry Posterior | DW | 162.4 (3.13)a | 129.0 (4.47)b | 111.8 (4.02)c | -50.60
 | CF | 134.0 (4.47)a | 147.8 (7.12)b | 105.2 (4.38)c | -28.80
 | RW | 141.8 (2.68)a | 115.4 (4.93)b | 97.8 (3.83)c | -44.00
Grandio | DW | 113.2 (4.38)a | 73.2 (1.10)b | 103.6 (3.58)a | -9.60
 | CF | 130.0 (2.74)a | 112.8 (14.79)a | 84.4 (3.29)b | -45.60
 | RW | 133.2 (9.34)a | 103.6 (3.58)b | 69.6 (2.19)c | -63.60
Grandio Flow | DW | 82.2 (4.92)ab | 74.0 (2.74)a | 80.0 (2.74)b | -2.20
 | CF | 110.0 (0.10)a | 48.2 (2.17)b | 65.6 (2.19)c | -44.40
 | RW | 110.0 (0.10)a | 97.6 (2.19)b | 57.0 (0.10)c | -53.00
Filtek Silorane | DW | 68.8 (1.10)a | 82.2 (4.09)b | 73.0 (2.34)ab | 4.20
 | CF | 83.4 80.89)a | 66.4 (2.19)b | 87.0 (5.39)a | 3.60
 | RW | 101.6 (3.13)a | 70.4 (2.19)b | 35.8 (1.10)c | -65.80
Admira | DW | 72.0 (0.10)a | 45.8 (0.45)b | 69.6 (2.19)a | -2.40
 | CF | 62.8 (1.64)a | 45.2 (1.10)b | 58.6 (2.19)a | -4.20
 | RW | 62.2 (1.64)a | 51.6 (1.34)b | 47.4 (0.55)c | -14.80
Arabesk Top | DW | 81.0 (2.24)a | 52.6 (0.89)b | 43.6 (2.19)c | -37.40
 | CF | 101.0 (3.08)a | 55.2 (1.64)b | 71.4 (3.71)c | -29.60
 | RW | 69.2 (1.10)a | 47.2 (1.64)b | 44.8 (1.10)b | -24.40
Valux Plus | DW | 134.0 (4.47)a | 89.4 (6.02)b | 113.6 (4.93)c | -20.40
 | CF | 135.0 (2.74)a | 121.0 (4.47)b | 80.0 (2.74)c | -55.00
 | RW | 139.2 (4.92)a | 125.0 (5.48) b | 87.0 (5.39)c | -52.20
Superscripts in same column represents statistical differences (p<0.05). (TC: Thermal Cycles, DW: distilled water, CF coffee, RW: red wine)

## Slide 42: Figure 3. Hardness values baseline, after thermal cycles and coloration
Chart: 
| DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | DW | CF | RW | Clearfil Majestry Esthetic | Clearfil Majestry Posterior | Grandio | Grandio Flow | Filtek Silorane | Admira | Arabesk Top | Valux Plus
Baseline | 56.4 | 51.2 | 47.6 | 162.4 | 134 | 141.8 | 113.2 | 130 | 133.2 | 82.2 | 110 | 110 | 68.8 | 83.4 | 101.6 | 72 | 62.8 | 62.2 | 81 | 101 | 69.2 | 134 | 135 | 139.2
After TC | 44.8 | 47 | 50.2 | 129 | 147.8 | 115.4 | 73.2 | 112.8 | 103.6 | 74 | 48.2 | 97.6 | 82.2 | 66.4 | 70.4 | 45.8 | 45.2 | 51.6 | 52.6 | 55.2 | 47.2 | 89.4 | 121 | 125
After Coloration | 38.8 | 41.2 | 37.2 | 111.8 | 105.2 | 97.8 | 103.6 | 84.4 | 69.6 | 80 | 65.6 | 57 | 73 | 87 | 35.8 | 69.6 | 58.6 | 47.4 | 43.6 | 71.4 | 44.8 | 113.6 | 80 | 87

## Slide 43: Conclusions
Staining beverages (coffee and especially red wine) are key factors that affect the color, translucency and hardness of composite resins.
Because of negative effects, these beverages should be carefully consumed.

## Slide 44
It is also important to note some limitations of the present study. This is an in vitro study, and it is not possible to directly mimic the oral conditions.
The oral cavity is always under dynamic stresses, such as temperature variations, wear by mastication activity, and pH variations due to the different foods and beverages.
In addition, actual staining in the oral cavity would very likely require a longer period because of the intermittent nature of stain exposure, saliva and other fluids diluting the staining media, and polishing of the restorations by brushing.

## Slide 45: THANK YOU FOR YOUR ATTENTION