## Slide 1
Photocatalytic reduction of CO2 by means of TiO2-based catalysts synthesized with high pressure fluids
Rafael Camarillo Blas
rafael.camarillo@uclm.es

## Slide 2
Average anual temperature
1880
2014
+0.8 ºC
1950
Hotter
Colder

## Slide 3
Natural factors
1880
2014
Hotter
Colder
1950

## Slide 4
Human factors
CH4
CO2
N2O
SF6
HFCs
PFCs
1880
2014
O
O
O
Hotter
Colder
1950

## Slide 5
light
electricity
Renewable energy sources
C
O
O
O
O
C
C
H
H
H
H
H
H

## Slide 6
TiO2
1- adsorption
5- desorption & diffusion
2- light absorption & excitation
4- reduction
Valence Band
Conduction Band
3- charge separation
-
+

## Slide 7
P-25
Band engineering
UV
Visible
Wavelenght (nm)
Solar radiation
2.5
2
1.5
1
0.5
0
Absorbance
200 250 300 350 400 450 500 550 600 650 700

## Slide 8
573 K
200 bar
Phase diagram of CO2
density
solvent power
viscosity
diffusivity

## Slide 9
SC-CO2
200 bar
573 K
2 h
TiO2
Synthesis of catalysts in high pressure fluids
DIPBAT
TTIP
characterization
28 mmol prec./mmol alcohol
378 K
12 h
673 K
6 h

## Slide 10
TiO2
30-40 mg
1.07 bar
3h
CH4 + CO
Xe arc lamp
450 W
+ AM 1.5 GF
Photocatalytic reaction test
CO2 + water vapour (7:2)
Photocatalytic reaction tests
GC
solubility

## Slide 11
Chart: 
| TTIP-isopr. | TTIP-ethanol | DIPBAT-isopr. | DIPBAT-ethanol
Serie 1 | 67.1 | 75.2 | 55.3 | 63.2
Yield (%)
Synthesis yields
1 mol product : 1 mol precursor
75.2 %

## Slide 12
TiO2
1- adsorption
Surface properties

## Slide 13
Chart: 
| TTIP-isopr. | TTIP-ethanol | DIPBAT-isopr. | DIPBAT-ethanol | P-25
Serie 1 | 40.28 | 152.4 | 85.02 | 100.28 | 65.52
SBET (m2/g)
BET areas
2.5x
1.6x
Anatase 145-163 m2/g
+ high porosity
Rutile 36-46 m2/g
Brookite 76-87 m2/g

## Slide 14
TTIP-isopr.
DIPBAT-isopr.
TTIP-ethanol
FTIR spectra
DIPBAT-ethanol
O-Ti-O
H2O
OH-

## Slide 15
TiO2
2- light absorption & excitation
Valence Band
Conduction Band
-
+
Band gap energy

## Slide 16
TTIP-isopr.
TTIP-ethanol
DIPBAT-isopr.
DIPBAT-ethanol
DRS spectra
2.757 eV
6x
3x
3x
3.048 eV (UV light)
P-25
3.004 eV
surface oxygen vacances
450 nm
413 nm
413 nm

## Slide 17
TiO2
Valence Band
Conduction Band
3- charge separation
-
+
crystallinity
enhanced morphology

## Slide 18
SEM images
TTIP-isopr.
TTIP-ethanol
DIPBAT-isopr.
DIPBAT-ethanol
P-25

## Slide 19
XRD diffractograms
TTIP-isopr.
TTIP-ethanol
DIPBAT-isopr.
DIPBAT-ethanol
P-25
R
R
R
22.77 nm
10.65 nm
19.97 nm
Anatase

## Slide 20
TiO2
4- reduction
Valence Band
Conduction Band
-
+

## Slide 21
Photocatalytic reduction of CO2
Chart: 
| TTIP-isopr. | TTIP-eth. | DIPBAT-isopr. | DIPBAT-eth. | P-25
CH4 | 0.039 | 0.954 | 1.125 | 0.757 | 0.075
CO | 1.154 | 6.042 | 3.753 | 2.869 | 2.014
CH4, CO (µmol/g/h)
12x
15.7x
C
O
O
O
O
C
C
H
H
H
H
H
H

## Slide 22
TiO2
5- desorption & diffusion
Valence Band
Conduction Band
-
+

## Slide 23
Conclusions
Particles with SCFs: large BET areas, good porosity, active surface compositions, narrow band gap, good visible light harvesting properties, high crystallinity and purity, appropriate morphology
Production rates are still far from industrial application
Change in geometry (TNTs) and introduction of dopants (Cu, Pd, Pt)

## Slide 24
CTM2011-26564
Acknowledgments
PEII10-0310-5840
Energy & Environment 2010/12

## Slide 25
Carlos
Jiménez
Acknowledgments
INQUIME Group
Fabiola
Martínez
Jesusa
Rincón
Jesús
García
Susana
Tostón
Isaac
Asencio

## Slide 26
Acknowledgments
Former Arms Factory (1780-1996)
> 150,000 m2
River Tagus
Sabatini Building (1780) 10,000 m2
70 km
350 km
Toledo

## Slide 27
Acknowledgments
1923
Albert Einstein
1948
Alexander Fleming

## Slide 28
Acknowledgments
1986-2016
طليطلة
טולדות

## Slide 29
Photocatalytic reduction of CO2 by means of TiO2-based catalysts synthesized with high pressure fluids
Rafael Camarillo Blas
rafael.camarillo@uclm.es