## Slide 1
Rashmi Rani*, Radheshyam Raia, Seema Sharmab,
Madan Lala, Mamta Shandilyaa, Arpana Singhb
a) School of Physics and Materials Science, Shoolini University, H.P, India.
b) Ferroelectric Research Laboratory, Department of Physics, A.N.College, Patna, India.
*Laboratoire des Solides Irradies, Ecole Polytechnique, Palaiseau, France .
Ceramic and composite materials , June 26-27, 2017 Madrid, Spain
Multiferroic and Magnetoelectric properties of BCT-ZF ceramics

## Slide 2
Introduction
Synthesis and preparation of BCT-ZF
1) Structural properties of BCT-ZF.
2) Magnetic properties of BCT-ZF.
3) Electrical properties of BCT-ZF.
4) Magnetoelectric properties of BCT-ZF.
Conclusions and perspectives
1) Mulitiferroic.
2) Idea of magnetoelectric effect.
3) Multiferroic magnetoelectric materials.
4) Barium calcium titanate (BCT) - Zinc ferrite (ZF).
Results & discussions
1) Solid state sintering method.
2) Characterizations.
3) Measurements.
Outline

## Slide 3
Multiferroic???
Ferromagnetism Ferroelectricity Ferroelasticity
spontaneous spontaneous spontaneous
magnetization polarization strain
Multiferroics are defined as materials that exhibit more than one of the primary ferroic order parameters in the same phase « formation of switchable domains:
N
S
+ -
+ -
+ -
+ -
Ferroelectric
Ferroelastic
Ferromagnetic
Ferroelastic
Piezoelectric and electrostrictive coupling
Piezomagnetic and magnetomechanical coupling
Ferromagnetic
Ferroelectric
Magnetostrictive and piezoelectric coupling

## Slide 4
Idea of magnetoelectric effect
The magnetoelectric effect (ME) is the phenomenon of inducing magnetic (electric) polarization by applying an external electric (magnetic) field. The effects can be linear or/and non-linear with respect to the external fields. In general, this effect depends on temperature. The effect can be expressed in the following form:
Pi = Ʃαij Hj + Ʃβijk Hj Hk +…..
Mi = Ʃαij Ej + Ʃβijk Ej Ek +….…..
E
H
σ
ε
M
P
N
S
Two types
1) Direct ME effect
2) Converse ME effect
Magnetoelectric effect (ME)

## Slide 5
1. Direct ME effect
2. Converse ME effect
Mechanical deformation of
the magnetostrictive phase
Mechanical deformation of
the piezoelectric phase
Magnetoelectric effects

## Slide 6
A materials which have the coexistence of long-range ferroic orders and strong coupling between pertinent order parameters such as composites based on
Magnetic materials as well as Piezoelectric materials
Ferrites Barium titanate
Maganites Lead zirconate titanate
Ferromagnetic metals Lead zinc niobate– lead niobate
Alloys Lead magnesium niobate-lead titanate
additional control to input and store data
Bismuth ferrite (BiFeO3)
In single phase, exhibits ME coupling at RT
Applications:
Sensors, multistate memories, actuators,
device applications as well as biomedical fields etc . ..
Multiferroic magnetoelectric materials:
composites

## Slide 7
“Bilayer connectivity of ferromagnetic and ferroelectric oxides was proven to
be successful to achieve giant ME coupling’’.
[C.-S. Park, A. Khachaturyan, S. Priya, Giant magnetoelectric coupling in laminate thin film structure grown on
magnetostrictive substrate, Applied Physics Letters, 100 (2012) 192904.]
Lead-free systems: (K, Na) NbO3 -ferrite, (Bi, Na) Ti O3-ferrite and BaTiO3-ferrite
BaTi O3
High dielectric & Piezoelectric properties
Ferroelectric Perovskite
Inhance electrical properties by substitution
of ‘Ca’
ZnFe2O4
Spinel structure
Paramagnet in bulk at RT
Super paramagnet in nano
scale at RT
Ba0.96Ca0.04TiO3
BaCaTiO3
ZnFe2O4
1-X
X
BCT
ZF
Magnetoelectric
Composite
BCT-ZF

## Slide 8
Synthesis and preparation of composite
((1-x)Ba0.96Ca0.04TiO3–(x)ZnFe2O4)
where x = 0.10 and 0.20
Synthesized by Solid state reaction method
Magnetoelectric composite
BaCO3
CaCO3
TiO2
ZnO
Fe2O3
Ferroelectric phase
Ferromagnetic phase
Wet ball-milling
Calcination
pressing
Raw material taken as a stoichiometric composition mixed in nylon jar with ethanol for 4-5hrs
Calcined at 900 C for 6 hrs
Pressing powders into cylindrical pellet of 10mm in diameter and 1-2 mm thickness using hydraulic press at 50MPa
Sintered at 950 C for 3 hrs for densification
Measurements…
BCT-ZF
Characterizations…
Sintering

## Slide 9
X-Ray diffraction pattern of BCT-ZF
Cubic spinel
Tetragonal
A secondary phase of ZnFe2O4 is observed which confirm that successful synthesis of
magnetoelectric multiferroic material.
The calculated average crystalline size is about ~ 32 and 22 nm for BCT and ZF respectively.
Debye-Scherrer formula

## Slide 10
Applied magnetic field 0.1T
Applied magnetic field 0.1T
Presence of uncompensated anti-ferromagnetic spins (Fe3+ ).
FC and ZFC curves consistent with the temperature dependent magnetization of anti-
ferromagnetic magnetic structure.
The magnetization increases rapidly with decreasing the temperature confirming
that there is magnetic phase transition.
Superparamagnetic
Blocking temperature shifts to lower side as the crystallite size is decreases .
x= 0.10
Variation of magnetic moment with temperature
Fig.1
Fig.2
x= 0.20

## Slide 11
Both composites demonstrate typical M-H loops at room temperature.
Existence of an ordered
magnetic structures in the
ceramics.
Highest magnetization
Enhancement of magnetization ???
Incomplete rotation of spins
along the direction of wave vector.
Increasing in spin canting due to
surface strain and oxygen defects.
Magnetic parameters
Magnetization curves of BCT-ZF ceramics

## Slide 12
Fig.3
Lossy capacitor
phenomena
Pr
Pr
Pr
Pr
Pr
Percentage dielectric phase has the significant effect in the polarization response.
As the applied field increases, the magnetoresistance effects become dominant.
Enhancement of Polarization beyond 1 keO may due to decrease of leakage current.
P-E field loop of BCT-ZF at different DC bias fields
Fig.1
Fig.2
Fig.4
Fig.5
Fig.6

## Slide 13
x= 0.10
x= 0.20
ferro to ferro
ferro to para
Two phase transitions are observed in the permittivity curve.
Dielectric constant increases gradually with the increasing temperature up to the Tc.
Value of dielectric constant is higher for (x= 0.10) than x= (0.20).
Space charge mechanism plays an important role at lower frequency.
Tc ~250C
Dielectric constant with temperature at
different frequency
Fig.1
Fig.2

## Slide 14
.
At low frequencies, the charge carriers get accumulated at the grain boundaries
resulting in a high capacitance
Dispersion can be ascribed to the phenomenon called the magnetocapacitance effect.
The overall dielectric behavior is of
Maxwell- Wanger type
δ
δ
Capacitance Vs frequency at different applied
DC magnetic fields
Fig. 1
Fig. 2

## Slide 15
Magnetoelectric coupling in BCT-ZF
Magnetoelectric coupling coefficient (MECC) increases initially due to increase in
magnetostriction of ferrite with applied DC field.
The observed MECC is quite larger than reported values, this may be due to the presence of
leakage current.
10.85
6.85
Linear dependence of AC magnetic field
A possible mechanism for magnetoelectric coupling (ME) coupling of this FE/FM
(BCT-ZF) interface is based on screening effects.
ME coupling also caused by an emergent inverse DM interaction at MF interface.
DC field dependence of MECC and ME voltage as a function of
applied AC magnetic field of BCT-ZF ceramics

## Slide 16
XRD pattern confirms the co-existence of two phase namely perovskite and spinel
corresponding to BCT and ZF respectively.
Much more gradual change of permittivity vs. temperature is observed in the composition
0.10 and 0.20.
The capacitance and the polarization of the sample are found to be magnetically tunable.
The composite have shown MECC of 10.85 and 6.85 Mv/(cm.Oe), and are highly sensitive to
AC magnetic field.
The influence of mutual orientation of polarization and magnetization on the ME effect
is addressed.
The presented results can thus offer applications in magnetoelectric devices especially in
magnetic field sensors and tunable devices.
Future engineering and employment of magnetoelectric materials for device applications especially in biomedical field will be carried out.
Perspectives
Conclusions

## Slide 17
10 mm
Thank you for your kind attention!
Email id: rashmi.rani@polytechnique.edu