## Slide 1: Department of Materials and Interfaces, Weizmann Institute, Rehovot 76100 E-mail: reshef.tenne@weizmann.ac.il

## Slide 3: The firstly observed chrysotile (asbestos) nanotubes

## Slide 4: Why do inorganic nanotubes and fullerene-like structure form: The different bonding state of bulk and rim atoms in graphite and MoS2

## Slide 7: Endoscope/catheters insertion/extraction from human body simulating constrictions

## Slide 9: Portland-concrete reinforcement by nanotubes

## Slide 10: Microwave synthesis of IF-MoS2

## Slide 12: Core-shell nanotubes

## Slide 13: Stable IF-Cs2O nanostructures

## Slide 14: Vapor-liquid-solid (VLS) growth of SnS2 nanotubes with Bi catalyst

## Slide 15: GaSe/Gas nanotubes and fullerene-like by laser ablation and heat treamtnet

## Slide 16: “Misfit” compounds

## Slide 17: Nanotubes from the LnS-TaS2 (NbS2) family of compounds

## Slide 18: Families of “misfit” MS-TS2 nanotubes reported, so far and future work

## Slide 20: Calcium Cobalt oxide: the First Member of a New Family of Oxide-Based Misfit Nanotubes

## Slide 21: Euler Rule for Archimedeans

## Slide 22: IF-MoS2 produced by solar ablation at >2000 ºC (transition from laser ablation to furnace synthesis of IF nanoparticles)

## Slide 27: Pull-out of individual WS2 nanotubes from water (liquids) surfaces

## Slide 28: SnS-SnS2 (O-T-T) ordered superstructure nanotubes

## Slide 29: Nanotubes from misfit compounds

## Slide 31: Field-Effect Transistors from WS2 Nanotubes with High Current-Carrying Capacity and Electromechanical Torsion Device

## Slide 32: Films of self-repelling Re:IF-MoS2 NP: Significantly reduced encrustation of urological catheters

## Slide 33: Tensile test of WS2 nanotube -computation by MD-DFT

## Slide 34: Biocompatibility of the IF/INT nanoparticles

## Slide 35: GaN nanotubes grown on ZnO nanowire template

## Slide 37: Plasma assisted synthesis of 1-to 3-wall WS2 nanotubes

## Slide 39: Measuring the mechanics of individual IF nanoparticles in the SEM

## Slide 40: Effect of charge transfer on conductivity (PANI/INT-INT-WS2)

## Slide 41: Polyurethane glue reinforced by WS2 nanotubes

## Slide 44: IF-nanoparticles of PbS-SnS2 obtained by solar ablation (>2000 K)

## Slide 45: The Burstein-Moss Shift in Re-doped IF-MoS2

## Slide 47: SEM view of a buckling of an individual WS2 nanotube

## Slide 49: Re atoms in IF-MoS2 nanoparticles

## Slide 50: Doping PANI with INT-WS2

## Slide 51: SEM of SbS-TaS2 nanotubes

## Slide 53: Mie surface plasmon scattering of WS2 nanotubes in solution

## Slide 54: Advanced Mg alloy nanocomposites reinforced by WS2 nanotubes

## Slide 55: Reinforcing Cement by MWCNT or INT-WS2

## Slide 56: HRTEM analysis of CeS-CrS2 nanotube

## Slide 57: On the mechanism of lubrication of IF nanoparticles

## Slide 58: Lanthanide-sulfide (misfit) nanotubes with CrS2 and VS2

## Slide 59: Electrospun PMMA fibers

## Slide 60: Summary of the mechanical properties of IF NP

## Slide 61: V2O5 IF-like nanoparticles produced by pusled laser ablation

## Slide 63: Cobalt coated self-lubricating films

## Slide 65: The role of rolling friction? in nanomaterials

## Slide 66: Isotactic polypropylene/IF-WS2 nanocomposites

## Slide 70: Torsion of a gold pedal suspended on WS2 nanotube

## Slide 75: IF nanocomposites with polyetheretherketone (PEEK) IF-WS2/PEEK nanocomposite coatings have been produced using aerosol-assisted deposition process With 1 wt%IF nanoparticles, the thermal stability of the nanocomposite coatings increases by 20–30 °C

## Slide 76: IF nanocomposites with polyphenylenesulfide

## Slide 77: Pressing individual IF-WS2 nanoparticle

## Slide 79: Tribological measurements of IF-MoS2 nanoparticles

## Slide 81: Mass production of multiwall WS2 nanotube (type 2)

## Slide 82: Stress-strain curve of a WS2 nanotube from SEM tensile stress experiment

## Slide 84: Synthesis of IF-MoS2 by the gas phase reaction between MoO3 vapor and H2S

## Slide 85: Comparison between the calculated and STM determined bandgaps of WS2 nanotubes

## Slide 86: Shock wave synthesis of inorganic nanotubes

## Slide 87: Resonance Raman excitation spectroscopy of WS2 nanotubes

## Slide 88: Band structure of MoS2 nanotubes

## Slide 89: Nanomechanics of WS2 nanotubes (type I and II)

## Slide 90: Reinforcement of epoxy resin by WS2 nanotubes

## Slide 92: Re (Nb) doped IF-MoS2

## Slide 95: Stability range for the PbI2@MoS2 core-shell nanotubes

## Slide 97: Raman spectra of SnS2 and SnS/SnS2 ordered superstructure nanotubes

## Slide 98: SKF Launched New “NanoLub inside” Line of Products based on UTA Graphite Cage Technology (and the IF-WS2 nanoparticles)

## Slide 104: Synthesis of MX2 nanotubes by solar ablation

## Slide 105: Orthodontic and medical devices

## Slide 106: Possible new medical applications of IF/INT

## Slide 107: The scaling-up of IF and INT-WS2 at “NanoMaterials”

## Slide 108: Tribology of Epoxy/WS2 Composites