## Slide 1: Cementation of Aesthetic Resin Composite Indirect Restorations
Resin Cements
Dr. Rui Franco
27 July 2015

## Slide 2: Introduction
Evolution in the adhesion of dental materials
Direct Restorations vs Indirect Restorations
Cement Importance in the Adhesion
Aesthetics importance from Society Point of View

## Slide 3: Objectives
Resin Cements – State of the Art;
Cementing Technique in Indirect Composite Restoration:
  Polymerization type;
  Adhesive System.

## Slide 4: Ideal Material
Ideal Material
Biocompatible
Mechanically stable
Minimally conductive thermally and electrically
Esthetic – identical to natural tooth
Easy to manipulate
Adherent
Tasteless and odorless
Cleanable and repairable
Cost-effective

## Slide 5: Factors Influencing the Success of a Restoration
Patient Factors
Dentist Factors
Material Factors
Longevity Dental Restoration

## Slide 6: Indirect Restorations
Recent developments in resin‐based composite resins have made it possible to fabricate esthetic indirect adhesive restorations
    No polymerization shrinkage;
    No inadequate degree of conversion.
Indirect restoration requires more dentin exposure than direct restoration and thus increases dentin sensitivity.
Zorba et al, 2009

## Slide 7
With indirect restorations, all technical processing of the restoration, including polymerization, are performed externally.
However, it is still possible for polymerization stress to occur during the curing phase of the resin cement:
    marginal leakage
Zorba et al, 2009

## Slide 8
An adequate polymerization of resin cement is crucial to acquire optimal physical and biological properties and clinical performance
Marginal adaptation influences the longevity of indirect restorations.
Medina et al, 2012

## Slide 9: Case Review Study

## Slide 10: First Appointment
“I have a cavity” SIC

## Slide 11: Rehabilitation Options
Direct Restoration;
Indirect Restoration:
Porcelain
Resin Composite
Metal
Metal-Porcelain
Zorba et al, 2009
Sakrana, 2013
De demand of esthetically pleasing dental restorations has made the all-ceramic crown a popular option.

## Slide 12: Indirect resin composite restoration – Preparing
Laboratory-processed indirect composite resin systems are an attractive esthetic alternative for intracoronal posterior restorations.
Cetin et al, 2009

## Slide 13: Study models, Diagnostic wax up and silicone key

## Slide 14: Cavity Evaluation

## Slide 15: Temporary direct composite restoration
Filtek Z250® (3M ESPE – Minnesota, USA)
Extensively destroyed teeth are commonly restored with composite resin before cavity preparation for indirect restorations.
Dos Santos et al, 2014

## Slide 16: Tooth Preparation
Characteristics:
  Enamel margins
  Rounded Internal angles;
  Occlusal divergence.
Cetin et al, 2009

## Slide 17: Temporary Acrylic Resin Restoration
Protemp® (3M ESPE – Seefeld, Germany)

## Slide 18: Cementing Temporary restoration
TempBond NE® (Kerr – California, USA)

## Slide 19: Laboratory execution
Microhybrid resin composite (Enamel Plus HFO® - Micerium-Avegno, Italy)

## Slide 20: Resin Characterization
brown and white pigments from Enamel Plus HFO® (Micerium-Avegno, Italy)

## Slide 21: Polishing
Sof-Lex discs® (3M ESPE Dental Division - Minnesota, USA).

## Slide 22: Cementing the indirect resin composite restoration
The clinical and biological longevity of adhesive restorations is dependent on the performance of the adhesive systems
Cetin et al, 2009

## Slide 23: Temporary filling removal and Prophylaxis with Pumice
There is no negative influence if:
  Prophylaxis with pumice after two weeks, if there is eugenol presence;
  Adhesive System Application.
  Gomes AJ et al., 2006
  Wazzam KA et al., 2000

## Slide 24: Surface Treatment
If no surface treatment is done, the outcome can be:
  Microinfiltration;
  Margin discoloration.
With Aluminum Oxide jet as surface treatment it is believed to obtain the best adhesive properties.
D’Arcangelo C e Vanini L, 2007
Dos Santos et al, 2014

## Slide 25: Self-Etch and Self-Adhesive System vs. Etch and rinse Adhesive System
Krämer et al., 2006
Rosentritt et al., 2004
There are no differences in Adhesion Potential.
Perdigão J et al., 2009
Self-etch
Strong adhesion to dentine
Low adhesion to enamel.

## Slide 26
Cantoro A et al., 2008
Chieffi N et al., 2007
Frankenberger et al., 2007
Frankenberger et al., 2008
Zorba et al, 2009
Etch and Rinse Adhesive Systems promote better results. For example:
  Less interface crack formation;
  Good marginal adaptation;
  Better adhesive resistance;
  Correct enamel adhesion.

## Slide 27: Adhesive System Application
All-Bond 2® (Bisco – Illinois, USA) Adhesive System.

## Slide 28
Dry enamel and wet dentine after etching technique.

## Slide 29: Ideal Dental Cement
Requirements during Placement
Requirements after Cementation
Patient Comfort
Easy to use
Most important
Resin cements produce high levels of stress during polymerization.
The incorporation of air bubbles during the manipulation of the cement weakens it and makes it more susceptible to fractures.
Medina et al, 2012

## Slide 30: Cement Types
Light-Cure
Increased working-time excess removal is easier;
Self-curing
Increased curing time;
Weak adhesion during the first hour.
Dual-Cure
Reduced working time;
Incomplete Polymerization.
Correct and definitive monomer conversion.
Color instability;
Size of the cavity (light reach)
Jivraj SA et al., 2006
Ferrari M et al., 2007
Fonseca RG et al., 2005
Habekost et al., 2007
Schneider R et al., 2007
Jivraj SA et al., 2006
Ferrari M et al., 2007

## Slide 31: Resin Cement Application
Resin Cement Multilink Automix® - Ivoclar Vivadent – Schaan, Liechtenstein) transparent.
“The quality of indirect restorations depends on the properties of the luting cements used”
Rosentritt M et al., 2004.

## Slide 32: Applied Pressure Influence
Chieffi N et al., 2007
Sakrana, 2013
Extending the application of pressure
Improved interface integrity
Increased bond strength
Adhesive Permeability Reduction
Reduce intracoranal stress

## Slide 33: Excess Removal

## Slide 34: Final Result

## Slide 35: Before and After
Begin
End
“Adequate cement/adhesive combination is essential to avoid postoperative hypersensitivity”,
Ferrari M et al., 2007

## Slide 36: Discussion

## Slide 37: Discussion
The extra-oral polymerization of composite resins increases the degree of conversion.
  Improved mechanical properties. Dejak B et al., 2008
  (in vitro)
The ceramic has low fracture resistance because it is harder than enamel and a low deformation limit.
  Lower cost in indirect composite resin restorations;
  Cannot withstand elastic deformation while resinous materials can;
  High levels of abrasion on antagonizing teeth with ceramics.
  Dejak B et al., 2008
  Sakrana, 2013
On the other hand, the ceramic gets a superior stability on maintaining color and marginal discoloration.
Fabianelli A et al., 2006
(in vivo)

## Slide 38
Surface conditioning has a significant effect on the shear bond strength.
    Zorba et al, 2009
Surface treatment can be carried out by chemical treatment silanization.
Soares JC et al., 2004
(in vitro)
If there is no prior mechanical treatment of the surface of the restoration, the silanization does not influence in any way the bonding.
  The hydrofluoric acid followed by silane application is plausible.
  The oxide aluminum jet gets the best adhesive properties.
D’Arcangelo C e Vanini L, 2007
(in vitro)

## Slide 39
The self-etch adhesives are not as effective in enamel as etch and rinse are, but are relatively effective in dentin and post-operative sensitivity.
Yoneda S et al., 2005
There is no difference between the postoperative sensitivity depending on the choice of adhesive system and is rather related to a good or bad technical execution.
Perdigão et al., 2003
In cementing indirect restorations is advocated an etch and rinse adhesive system and resin cement application that is not only light-curing.
Ritter AV et al., 2009

## Slide 40: Conclusions
Indirect restorations in composite resin are a current and rapidly developing technique.
With this work it is concluded that the growing clinical success of resin cements.
  Influence the aesthetics and longevity of this type of restorations.
  For this is necessary an effective adhesion to the remaining tooth .

## Slide 41
Yet to assess in the long-term:
  Secondary caries;
  Postoperative sensitivity;
  Color stability;
  Integrity of the restoration;
  Cement wear at marginal level.

## Slide 42
Muito Obrigado!
Hartelijke Dank!
Thank you very much!