## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Phrama scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3: Photo-excited hot electrons from conductive films forming heterojunctions
Satoshi Ishii,1,2,3 Thang Duy Dao1,2 Akira Otomo3 and Tadaaki Nagao 1,2
1 International Center for Materials Nanoarchitectonics (MANA), National Institute for Materials Science (NIMS), Japan
2 Core Research for Evolutional Science and Technology (CREST), Japan Science and Technology Agency (JST), Japan
3 Advanced ICT Research Institute, National Institute of Information and Communications Technology (NICT), Japan

## Slide 4: Contents
Introduction
  Hot electron excitation from metals
Photodetectors for optical waveguides
Transparent photodetectors with oxides
Summary
References
Japanese patent: Application number (2014) 39325
S. Ishii, et al, under review (2014)

## Slide 5: Optical properties of metals
Metals
  Reflect light
    No transmission
Gold
Metallic surface
Surface plasmon polaritons (SPPs)
Propagation length : ~mm
Hot electrons
Heat
  Thermo-plasmonics
G. Baffou, et al, ACS Nano (2010)
losses
  Complex permittivities
e ‘ < 0

## Slide 6: Metallic photodetectors
Schottky contacts
  Metal-semiconductor contacts
    e.g. Au-Si
  Internal photoemission from metal
    (photon energy) < (bandgap)
I. Goykhman, Nano Lett. (2011)
Absorption in metals = generation of hot electrons
K.H. Gundlach, et al, JAP (1975)
MIM structures
  Metal-insulator-metal (MIM) with thin films
  Photocurrent by the hot carriers crossing the insulator barrier
    (photon energy) < (bandgap)

## Slide 7: Recent studies using MIM structures
H.Chalabi, et al, Nano Lett. (2014)
F. Wang and N.A. Melosh, Nano Lett. (2011)
Kovacs, et al, PRB (2007)
D. Diesing, et al, J Solid State Electrochem. (2003)
Electrochemical surface science
Excitation by photons & particles
Excitation by surface plasmons (SPs)
Plasmonic resonances

## Slide 8: Contents
Introduction
  Hot electron excitation from metals
Photodetectors for optical waveguides
Transparent photodetectors with oxides
Summary
References
Japanese patent: Application number (2014) 39325
S. Ishii, et al, under review (2014)

## Slide 9: MIM photodetector for optical waveguides
Copyright: IBM
Metals are everywhere on opto-electronic chips
Ishii and Inoue, patent application (2014)
Hot electrons excited in metal films by the evanescent field of guided light

## Slide 10: Device fabrication
SU-8 waveguide:
  Height: 1.53 m
  Ave. width: 6.5 m
  Film thicknesses:
  Top (Ti): 25 nm
  Middle (SiO2): 10 nm
  Bottom (Au): 20 nm
  Film widths: 5 m

## Slide 11: Photodetection
A
I > 0
Au
Ti
SiO2
Photocurrent generation by the guided light
Positive bias↑ => photocurrent ↑
Open circuit voltage (Voc) = -0.05 V
Voc
Input wavelength:  = 680 nm
Notes: MIM121821, 12/25/13, for a single contact 680 nm

## Slide 12: Wavelength dependence
Input power: 0.1 mW
Wavelength: 680, 760 & 1064 nm
Photodetection up to  = 1064 nm
Higher photocurrent at shorter input wavelength
Open circuit voltage (Voc) ~ 0

## Slide 13: Mode analysis
Mode index:
n = 1.5579
 = 680 nm
absorption
Mode index:
n = 1.5570+i9.310-5
Small portion of guided light is absorbed by the metals

## Slide 14: Electronic structures of MIMs
Au-SiO2-Ti
  Barrier height ~ 4 eV
  Tunneling for visible and NIR
    Open circuit voltage (Voc) ~ 0
Au
Ti
SiO2
EF
4.2 eV
E
→
Au
Ti
TiO2
Au-TiO2-Ti
  Barrier height ~ 0.9 eV
  Open circuit voltage (Voc) for  < ~1.4 μm
  Tunneling for  > ~1.4 μm
0.9 eV
E
→

## Slide 15: MIM with Au-TiO2-Ti
1310 nm
Input power: 1.0 mW
Photodetection up to  = 1550 nm
   < ~1400 nm: Open circuit voltage (Voc) < 0
   > ~1400 nm: Voc = ~0 (tunneling)
Input power: 1.75 mW
Notes: (IV_1310nm_fulldark2_1.75mW.csv、041714-MIM021214B)、(IV_1550nmp3_fulldark2_1.75mW.csv、041814-MIM021214B)

## Slide 16: Where can we use MIM?
Silicon photonics
  Si-Ge photodiodes
  Schottky contacts
Ⅲ-Ⅴ photonics (e.g. InP)
  Ⅲ-Ⅴ photodiodes
Polymer/dielectric photonics
  Semiconductor photodiodes
  <= replace with our detectors
Shiraishi, et al, OFC/NFOEC (2011)
© Optical Interlinks

## Slide 17: Contents
Introduction
  Hot electron excitation from metals
Photodetectors for optical waveguides
Transparent photodetectors with oxides
Summary

## Slide 18: Properties of TCOs
Transparent conductive oxides (TCOs)
  High carrier concentrations ( < ~10-21 cm-3 )
  Transparent (if thin)
  Small light absorption
    Im[e] > 0
Al:ZnO 50 nm
A. Klein, et al, Materials (2010)
=> Transparent photodetectors with TCO–insulator(I)–TCO structures
EF
TCO
TCO
I
e
Notes: ZnO 50 nm, 072514 on glass

## Slide 19: Photodetection with TCOs
AZO
TiO2
AZO
fused silica
A
AM 1.5
filter
AZO-TiO2-AZO
AZO
Photodetection in VIS & NIR
  Eg(TiO2) = 3.2 eV (l = 387 nm)
  No pn junctions
S. Ishii, et al (2014) unpublished
Notes: Sample info on the photo
Sputtered date: 8/7/14
Films: AZO 30nm/TiO2 20 nm/ AZO 30nm
Tri-layer area: ~1.5 x 2.0 mm (?)
Substrate: fused silica
FIG AZO 30nm/TiO2 20 nm/ AZO 30nm on 8/20/14, on fused silica 2, No anneal, IV on 10/2/14

## Slide 20: Summary
MIM photodetectors for optical waveguides
  Photodetection in visible and NIR including telecom wavelengths
  Simple & compact geometry
  Applicable for insulator waveguides (e.g. polymers)
Transparent photodetecors with TCOs
Acknowledgements
Strategic Information and Communications R&D Promotion Programme (SCOPE)
The Japan Prize Foundation

## Slide 21
0 1 0 1 0
0 1 0 1 0
light
current

## Slide 22: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: http://materialsscience.conferenceseries.com/
Contact us at
materialsscience.conference@omicsgroup.us
materialsscience@omicsgroup.com