## Slide 1: Chemical Characterization of Coke Fouling
From Pipeline, Refinery and Upgrader Process Units.
Roxanne Shank, P.Chem. M.Sc.
shank.roxanne@cleanharbors.com

## Slide 2: Introduction
One of the biggest fouling problems in refineries, upgraders and pipelines is coke fouling
Little Research
Mechanical Methods
Better Way?

## Slide 3: Coke Fouling
Largely misunderstood, often misinterpreted
Most of the fouling in the energy sector is attributed to coke
  Usually a mixture, iron sulfides likely
Sample research may be difficult
Feedstock changes
  Impurities
  Sulfur Content
  Asphaltene/Maltene content

## Slide 4: Fouling Process
A number of models exist for the formation of coke fouling in the process stream.
Thermal Conversion Model
  Asphaltenes converted to ashaltene cores.
  Concentration < solubility, cores precipitate out as coke.
Thermal Cracking Model
  Hot Spots = thermal cracking = coke particles in fluid
Mechanisms of Coke Fouling
Free flowing particulates in the fluid, plugging off pipes and tubes
Coke precipitates and is deposited on the metal surface
Layer of coke forms at the metal surface and grows.

## Slide 5: Temperature and Pressure
Temperature is a key factor in the process
  As temperature increase, coke formation increases rapidly
As the pressure increases, the temperature increases, but the fluid is not uniform
  Hot Spots arise in the fluid, resulting in spontaneous thermal cracking, and an increase in the formation of coke.

## Slide 6: Samples
Over 60 samples have been collected over the past 20 years from various pipeline, refinery and upgraded process units worldwide, each deemed to be ‘coke’

## Slide 7: Experimental Methods
Multi-part Chemical Analysis
  Organic extraction
  Inorganic Digestion
Instrumental Analysis of Inorganic Components
  X-Ray Fluorescence (XRF)
  Powder X-Ray Diffraction (XRD)
  Fourier Transform – InfraRed (FT-IR)

## Slide 8: Chemical Analysis
A multi-stage approach is used distinguish the different fractions in the sample.
  Organic extractions
    Distinguish between light hydrocarbons, asphaltenes and heavy fractions, paraffin and water.
  Inorganic Digestion
    Digestion of the inorganic portion in various acids to determine composition.

## Slide 9: X-Ray Fluorescence
The inorganic portion of the sample is analyzed by qualitative XRF (detects S to Se)
Chart: X-Ray Fluorescence Spectrum for RD13-17
Fe
Background
Signal
Ca
S
Cu Zn

## Slide 10: X-Ray Diffraction (Powder)
Inorganic Portion is crushed and assessed by XRD to determine composition.
RD23-17
RD13-13
Iron Sulfide - 9.3%
Iron Sulphate – 70.8%
Iron Oxide) - 5.7%
Iron Sulphate – 52.7%
Crystalline Coke – 19.5%
Iron Oxide – 8.5%

## Slide 11: FT-IR
Samples are assessed by diamond ATR
FT-IR analysis before and after organic extraction
Chart: FT-IR Spectrum For RD01-13
Notes: Label this a little bit more

## Slide 12: Results
A total of 62 samples were tested
  Varying levels of amorphous and crystalline carbon (coke or graphitic carbon)
  Nearly 70% of the samples contained sulfur in some form (elemental, iron sulfide, sulfates)
  Silicates (Sand) is a major contaminate in many samples
  Asphaltenes remain as a major carbon source in many of the samples.

## Slide 13: Coke Foulant Spectrum
The samples assessed could be broken up into 5 major categories
Primarily Amorphous Carbon
Primarily Asphaltic
Primarily Sulfurous
Silicate-based Scale
Mixture
Corrosion Products were also observed
Salts and Carbonates may also be present

## Slide 14: Category 1 – Primarily Amorphous Carbon
Fraction | %wt
Lt. Hydrocarbon | 0.44%
Paraffin | 0.10%
Asphaltenes | 0.78%
HCl Acid Soluble | 2.40%
Sulfurous | 2.19%
Silicates | 2.31%
Unreacted Residue | 91.78%
RD03-13
Chart: X-Ray Fluorescence Spectrum for RD03-17
S
Ti
V
Cr
Fe
Background
Signal
Iron – 0.4%
Mereiterite – 14.6%
CrS – 6.6%
Quartz – 12.1%
Graphite – 18.5%
Sulfur – 24.2%
25/62 ~ 40% of samples

## Slide 15: Category 2 – Primarily Asphaltic
Chart: X-Ray Fluorescence Spectrum for RD26-17
Fraction | %wt
Lt. Hydrocarbon | 19.48%
Paraffin | 0.26%
Asphaltenes | 76.30%
HCl Acid Soluble | 2.75%
Sulfurous | 19.53%
Silicates | 0.00%
Unreacted Residue | 0.67%
RD26-17
V Cr
Fe
Background
Signal
Ca
Sc Ti
S
Iron Oxide – 27.2%
Iron Sulfide – 16.8%
Silicate – 34.8%
Salt – 7.9%
9/62 ~ 15% of samples

## Slide 16: Category 3 – Primarily Sulfurous
Chart: X-Ray Fluorescence Spectrum for RD11-13
Fraction | %wt
Lt. Hydrocarbon | 2.19%
Paraffin | 0.51%
Asphaltenes | 8.57%
HCl Acid Soluble | 4.30%
Sulfurous | 71.87%
Silicates | 1.16%
Unreacted Residue | 11.40%
RD11-13
Cr
Fe
Background
Signal
Ca
Iron Oxide/ Metal Oxide – 15.7%
Iron Phosphate – 11.7%
Sulfur/
Sulphur – 18.0%
10/62 ~ 16% of samples

## Slide 17: Category 4 – Silicate Based Scale
Chart: X-Ray Fluorescence Spectrum for RD49-17
Fraction | %wt
Lt. Hydrocarbon | 7.56%
Paraffin | 0.42%
Asphaltenes | 5.54%
HCl Acid Soluble | 14.76%
Sulfurous | 10.78%
Silicates | 55.04%
Unreacted Residue | 5.90%
RD49-17
Cl
Cr
Fe
Background
Signal
Silicate – 63.3%
Silicate – 25.4%
Ni Cu Zn
3/62 ~ 5% of samples

## Slide 18: Category 5 – Mixture
Chart: X-Ray Fluorescence Spectrum for RD22-17
Fraction | %wt
Lt. Hydrocarbon | 18.77%
Paraffin | 0.45%
Asphaltenes | 5.34%
HCl Acid Soluble | 13.95%
Sulfurous | 21.74%
Silicates | 7.82%
Unreacted Residue | 31.93%
RD22-13
S
Ca
Cr
Fe
Background
Signal
Iron Oxide – 3.6%
Iron Sulfide/ Metal Sulfide – 25.2%
Iron Sulphate – 49.7%
7/62 ~ 10% of samples

## Slide 19: Conclusions
Fouling in refineries is often attributed to Coke
  Coke Fouling is more complex
  Spectrum of coke fouling can be derived
  It may be possible to map the fouling based on process to some degree
  Coke Fouling may be dealt with chemically, reducing cost/downtime of maintaining process units.
Hydrocarbon
Sulfurous Compounds
Silicates
Amorphous Carbon
Crystalline Carbon
Metal Oxides
Asphaltenes
Hydrocarbon
Sulfurous Compounds
Silicates
Amorphous Carbon
Crystalline Carbon
Metal Oxides
Asphaltenes
Hydrocarbon
Sulfurous Compounds
Silicates
Amorphous Carbon
Crystalline Carbon
Metal Oxides
Asphaltenes

## Slide 20: Future Studies
CHNS, LOI, Ash Analysis
Elemental Analysis by AES-MP
DRIFTS FT-IR
Map the Foulant Spectrum
Chemical Cleaning Laboratory Studies
In-field Case Studies

## Slide 21: Acknowledgements
I would like to thank my colleagues
  Thomas R. McCartney, P. Chem.
  Samar Gharaibeh, P. Chem. Ph.D.
  Darcy Granburg, R. Chem.
  Charlie Clune
Thank you to all companies who have provided samples over the years.

## Slide 23
Chart: Light Hydrocarbon and Paraffin

## Slide 24
Chart: 

## Slide 25
Chart: Oxides, Salts, Carbonates and Sulfates

## Slide 26
Chart: Sulfurous Content

## Slide 27
Chart: 

## Slide 28
Chart: Amorphous Carbon ‘Coke’