## Slide 1
Genetic Engineering of D. radiodurans for uranium bioremediation from high radiation environment
Shree Kumar Apte
Molecular Biology Division
Bhabha Atomic Research Centre, Mumbai-400085, India
8th European Biotechnology Congress, Frankfurt, Germany
August 18, 2015

## Slide 2
Uranium resources
Primary
High grade ore: 2% U (20,000 ppm)
Low grade ore: 0.1% U (1000 ppm)
[India : 0.03-0.06% U (300-600 ppm)]
Uranium in sea water
3ppb / 13 nM, pH 7.5-7.8
Di-/Tetravalent uranyl carbonate complex,
[UO2(CO3 )3] 2-/ [UO2(CO3)3] 4-
Total U in sea water: 4.5 billion tonnes
(1000 X of terrestial ores)
Secondary
Rock phosphate: 100-200 ppm
Monazite: 50-200 ppm
Carbonaceous matter: 300 ppm
Uranium in spent fuel
Acidic waste
< 1mM uranyl nitrate, pH 3-7
Alkaline waste
< 1mM uranyl carbonate, pH 7-10
Dilute solutions with 1- 4 mM uranium at pH 5-10 need to be addressed

## Slide 3
Mechanism of metal precipitation by PhoN
Localised high concentration of Pi
Outer membrane
Inner membrane
Periplasm
Cytoplasm
PhoN
-Phosphoglycerate
Pi
UO22+ (soluble)
HUO2PO4 (insoluble and membrane bound)

## Slide 4
Over expression of PhoN
S.typhi E. coli Controls E.coli 5µg 50µg 5µg PhoN
5µg
Engineering E. coli for PhoN Overexpression
Samonella phoN gene with its native promoter works well in E. coli
(Seetharam, Soundarajan, Udas, Rao and Apte, Proc. Biochem. 44: 246-250, 2009)
Multicopy plasmid (pUC19) based PhoN overexpression

## Slide 5
VIABLE CELLS ARE NOT NEEDED
E.
>95% URANIUM (1mM) IS PRECIPITATED
FROM AQUEOUS SOLUTIONS BY GM
coli
URANIUM BIO-PRECIPITATION with BACTERIA
0
1
2
3
4
0
20
40
60
80
100
% Uranium precipitated
Time (hrs)
citrate buffer
unbuffered
acetate buffer

## Slide 6
Post-lyophilisation Performance of E. coli bearing phoN
Cells retained their integrity and activities, but lost viability
Metal
(Seetharam, Soundarajan, Udas, Rao and Apte, Proc. Biochem. 44: 246-250, 2009)

## Slide 7
Column based uranium precipitation by E. coli-phoN clones
E. coli-pRAD1
E. coli-pPN1
Total Loading on the column
7.6 g of U/g dry wt. of cells
INPUT SOLUTION
5 mM Uranyl Nitrate with10 mM β-glycerophosphate in 1.5 litres of 2 mM Acetate Buffer
COLUMN
200 mg of lyophilized cells immobilized in 15% polyacrylamide gel.
GEL VOLUME : 100 ml
Run time : 56 h

## Slide 8
The Extreme Radioresistance of Deinococcus radiodurans
Provides opportunities for novel basic research and applications

## Slide 9
Engineering phoN in Deinococcus radiodurans
Restriction digested with XbaI and NdeI
Restriction digested with NdeI and BamHI
(Appukuttan , Rao & Apte, Appl. Env. Microbiol. 72: 7873-7878, 2006)

## Slide 10
1 - E. coli - pRAD1
2 - E. coli - groESL+phoN (GN)
3 - E. coli - full phoN (CL#50)
4 - D. rad - pRAD1
5 - D. rad - full phoN (CL#29)
6 - D. rad - groESL+phoN (DN)
Deinococcus radiodurans
Wild type Engineered
Genetic engineering of phoN gene into D. radiodurans
(Appukuttan , Rao & Apte, Appl. Env. Microbiol. 72: 7873-7878, 2006)

## Slide 11
E. coli (c)
D. radiodurans (c)
D. radiodurans (i)
E. coli (i)
0
2
4
6
8
10
0
20
40
60
80
100
% Uranium precipitated
Time (h)
Uranium precipitation by E. coli and Deinococcus clones under 6kGy dose of irradiation
(Appukuttan, Rao & Apte, Appl. Env. Microbiol. 72: 7873-7878, 2006)

## Slide 12
Cell-surface bound uranyl phosphate precipitate (SEM)

## Slide 13
Seeing is believing …………….
Cell-surface bound uranyl phosphate precipitate (TEM)

## Slide 14
γ-ray
7 kGy
Mito-C
20 µg ml-1
H2O2
50 mM
C S C S C S C S
UV
5 kJ m-2
pSN4
pSN3
60Co, γ-ray (7 kGy)
pSN2
C T C T C T
rpsF 6 ssb
phoN
pRN1
pSN2
-102bp
pSN3
-132bp
pSN4
-351bp
RDRM2 RDRM 1
rpsF 18
C
S
60Co, γ-ray (7 kGy)
pSN4
pSN3
pSN2
pRN1
A Radiation responsive Deinococcal Promoter (Pssb)
(Ujaoney, Potnis, Dani, Mukhopadhyay & Apte, J.Bacteriol., 2011)

## Slide 15
(a)
Control Irradiated
56.8 Gy/min
4 Gy/min
(c)
(b)
(d)
Use of radiation-induced Pssb promoter for U bioprecipitation

## Slide 16
0
1
2
3
4
5
6
7
8
9
10
11
12
0
2
4
6
8
10
nmoles p-NP/min
pH
5
pH optima for acid and alkaline phosphatase
of Novosphingobium sp. BSAR-1
Zymogram for alkaline
phosphatase analysis
175kDa
An Alkaline Phosphatase Over-producer Bacterial Isolate
Genetic Basis of this Enzyme Activity was investigated and cloned
9
(Nilgiriwala, Alahari, Rao and Apte, Appl. Env. Microbiol. 74: 5516-5523, 2008)

## Slide 17
BSAR-1
KN20
EK4 - IPTG
EK4 + IPTG
Phenotype of various native and recombinant PhoK expressing strains
(Nilgiriwala, Alahari, Rao and Apte, Appl. Env. Microbiol. 74: 5516-5523, 2008)

## Slide 18
Uranium bioprecipitation at pH 9.0 using PhoK
(Nilgiriwala, Alahari, Rao and Apte, Appl. Env. Microbiol. 74: 5516-5523, 2008)

## Slide 19
Precipitate identified as H2(UO2)2(PO4)2.8H2O, metaautunite or chernikovite by Powder-XRD analysis
(Nilgiriwala, Alahari, Rao and Apte, Appl. Env. Microbiol. 74: 5516-5523, 2008)

## Slide 20
BSAR-1
KN20
pET29b
EK4
- cells
- GP
White light
UV light
Uranium precipitation at pH 9.0 using PhoK alkaline phosphatase

## Slide 21
Deino-PhoK without uranium treatment
Deino-PhoK with uranium treatment
TEM images of Deino-PhoK cells
500 nm
Needle shaped crystals of uranyl phosphate seen in uranium treated samples
500 nm
Seeing is believing …….

## Slide 22
A
B
C
Empty beads Deino-PhoK (-U) Deino-PhoK (+U)
D
E
Easy recovery of precipitated uranyl phosphate through beads

## Slide 23
Clones | Specific Activity (nmoles of p-NP liberated/min/mg of total cellular protein)
Deino- pRAD1 | 18 + 5
Deino-PhoK | 7000 + 1000
Deino-PhoN | 200 + 10
1 Deino-pRAD1
2 Deino-PhoK
3 Deino-PhoN
Phosphatase activity of recombinant strains
Recombinant Deinococcus strains on PDP-MG plate
Comparison of Deino-PhoN and Deino-PhoK strains

## Slide 24
Maximum loading possible with Deino-PhoN

## Slide 25
Maximum loading possible with Deino-PhoK

## Slide 26
SUMMARY
Metal precipitation using phosphatases is an old story.
Novelty of the present work :
  Use of heavy metal tolerant enzymes
  Cloning/characterization of a very active alkaline phosphatase (PhoK)
  Extension of metal bioremediation to alkaline solutions
  Recombinant radioresistant microbes to biorecover uranium from
  acidic/alkaline solutions in high radiation environments.
  Lyophilization to extend shelf-life while retaining precipitation ability
  Volume reduction, high U loading, easy recovery

## Slide 27
Related Publications
Appukuttan, D, Rao, A. S. and Apte, S. K. (2006) Appl. Env. Microbiol. 72 : 7873-7878.
Nilgiriwala, K., Alahari, A., Rao, A. S. and Apte, S. K. (2008) Appl. Env. Microbiol. 1784 : 1256-1264.
Seetharam, C., Soundarajan, S., Udas, A. C., Rao, A. S. and Apte, S. K. (2009) Proc. Biochem. 44 : 246- 250.
Nilgiriwala, K., Bihani, S C., Das, A., Prashar, V., Kumar, M., Ferrer, J-L, Apte, S. K. and Hosur, M. V. (2009) Acta Cryst. F65 : 917-919.
Ujaoney, A. K., Potnis, A., Mukhopadhyay, R. and Apte, S. K. (2010) J. Bacteriol. 192 : 5637-5644.
Bihani, S., Das, A., Nilgiriwala, K., Prashar, V., Pirocchi, M., Apte, S. K., Ferrer, J. and Hosur, M. V. (2011) PLoS ONE 6 : e22767.
Appukuttan, D., Seetharam, C., Padma, N., Rao, A. S. and Apte, S. K. (2011) J. Biotechnol. 154 : 285- 290.
Seetharam-Misra C., Appukuttan D., Kantamreddi V. S. S., Rao A. S. and Apte S. K. (2012) Bioengineered Bugs 3 : 44-48.
Kulkarni, S., Ballal, A. and Apte, S. K. (2013) J. Hazard. Metals 262 : 853-861.
Misra, C.S., Mukhopadhyaya, R. and Apte, S. K. (2014) J. Biotechnol. 189 : 88–93.

## Slide 28
ACKNOWLEDGEMENTS
Deinococcus radiodurans strain R1 M. Daly & K. Minton Useful Vectors Mary Lidstrom
PhoN for U/Cd bioprecipitation Deepti Appukuttan, Chitra Seetharam & A.S. Rao
PhoK for U bioprecipitatio Kayzad Nilgiriwala, Anuradha Alahari & A. S. Rao,
Sayali Kulkarni,
SEM-EDX Shovit Bhattacharya & N. Padma (TPPED, BARC)
TEM Anand Ballal, Alka Gupta
ICP-MS Sanjukta A. Kumar (ACD, BARC)
AAS A.C. Udas & Suvarna Soundarajan (ACD, BARC)
XRD Analysis N. Raghumani & Rakesh Shukla (CD, BARC)
Funding : Department of Atomic Energy and Department of Science & technology, India

## Slide 29
Addition of PhoK does not compromise or alter radioresistance
Irradiation (6 kGy, 60Co -rays) does not influence bioprecipitation
B
A
Recombinant strain functions well in high radiation environment