## Slide 1: Supercritical CO2 for Green Polymer Chemistry
by
Silvio Curia
International Conference on Biopolymers and Bioplastics
10 August 2015, San Francisco

## Slide 2: REFINE project: REnewable FunctIoNal matErials for a sustainable polymer industry
Plastic industry is heavily reliant on petrochemicals.
REFINE aims to combine:
green raw materials
green synthesis
green processing and modification
Notes: My PhD is part of the refine project. Refine stands for… and it aims to …. in order to achieve a greener polymer industry

## Slide 3: Plastics: the facts (2014)
Plastics – the Facts 2014, PlasticsEurope and European Plastics Converters, 2014
57 Mtonnes in EU
300 Mtonnes globally
Notes: Now you’re maybe wondering why it is important to obtain a greener poly science/industry.
Well: this slide is to show u some facts about plastics. The plastic industry is heaviliy reliant on non-biodegr and non renewable polymers. More in detail 58Mtonnes… and most of the used polymer were derived from petrochemicals… etc

## Slide 4: Plastics: the facts (2014)
Plastics – the Facts 2014, PlasticsEurope and European Plastics Converters, 2014
<10% derived from biodegradable polymers1
[1] C. Rolando, Biodegradation – Life of Science, 2013
Notes: Now you’re maybe wondering why it is important to obtain a greener poly science/industry.
Well: this slide is to show u some facts about plastics. The plastic industry is heaviliy reliant on non-biodegr and non renewable polymers. More in detail 58Mtonnes… and most of the used polymer were derived from petrochemicals… etc

## Slide 5
CO2 for polymer chemistry
Reduce the
viscosity
Energy saving
New green routes
Notes: Now you’re maybe wondering why it is important to obtain a greener poly science/industry.
Well: this slide is to show u some facts about plastics. The plastic industry is heaviliy reliant on non-biodegr and non renewable polymers. More in detail 58Mtonnes… and most of the used polymer were derived from petrochemicals… etc

## Slide 6: Polymer processing & synthesis: high viscosity problem
Major obstacle
High Viscosity!
Notes: Since the common poin of plymer processing is the use of polymer melts, high viscosity is a big issue. it can make the processing hard and expensive.
So We have several solutions. The use of… but they can be toxic and bad for the environment, the use of.. But its very easy to have the degrad of the polymers and any bioactive addtitives sush as drugs etc when using HT… and finally we can use the scCO2 as plasticiser that is non toxic, inexpensive and can be very useful to make easier the processing of polymers.

## Slide 7
Major obstacle
High Viscosity!
Solutions
Solvents
✗
Toxic
Polymer processing & synthesis: high viscosity problem
Notes: Since the common poin of plymer processing is the use of polymer melts, high viscosity is a big issue. it can make the processing hard and expensive.
So We have several solutions. The use of… but they can be toxic and bad for the environment, the use of.. But its very easy to have the degrad of the polymers and any bioactive addtitives sush as drugs etc when using HT… and finally we can use the scCO2 as plasticiser that is non toxic, inexpensive and can be very useful to make easier the processing of polymers.

## Slide 8
Major obstacle
High Viscosity!
Solutions
Solvents
High T
✗
✗
Toxic
Thermal degradation + expensive
Polymer processing & synthesis: high viscosity problem
Notes: Since the common poin of plymer processing is the use of polymer melts, high viscosity is a big issue. it can make the processing hard and expensive.
So We have several solutions. The use of… but they can be toxic and bad for the environment, the use of.. But its very easy to have the degrad of the polymers and any bioactive addtitives sush as drugs etc when using HT… and finally we can use the scCO2 as plasticiser that is non toxic, inexpensive and can be very useful to make easier the processing of polymers.

## Slide 9
Major obstacle
High Viscosity!
scCO2
✓
Temporary plasticiser
Non-toxic
Inexpensive
Accessible Tc & pc
Solutions
Polymer processing & synthesis: high viscosity problem
Notes: Since the common poin of plymer processing is the use of polymer melts, high viscosity in a big issue. it can make the processing hard and expensive.
So We have several solutions. The use of… but they can be toxic and bad for the environment, the use of.. But its very easy to have the degrad of the polymers and any bioactive addtitives sush as drugs etc when using HT… and finally we can use the scCO2 as plasticiser that is non toxic, inexpensive and can be very useful to make easier the processing of polymers.

## Slide 10: CO2-induced polymer plasticisation - how does it work?
Polymer chains
Notes: The reason behind the plasticisation is the fact that CO2 molecules can increase the free volume of polymers decreasing their viscosity...in this way we can process the materials as we want… Without using HT and solvents And we can obtain a very clean and pure material by simply depressurizing the autoclave! This can clearly be really important for food pakcaging and medical applications

## Slide 11
scCO2
Polymer chains
CO2 molecule
Lower viscosity
Lower melting point
CO2-induced polymer plasticisation - how does it work?
Notes: The reason behind the plasticisation is the fact that CO2 molecules can increase the free volume of polymers decreasing their viscosity...in this way we can process the materials as we want… Without using HT and solvents And we can obtain a very clean and pure material by simply depressurizing the autoclave! This can clearly be really important for food packaging and medical applications

## Slide 12
CO2-induced polymer plasticisation - how does it work?
Poly(lactic acid) at 35 oC
Notes: The reason behind the plasticisation is the fact that CO2 molecules can increase the free volume of polymers decreasing their viscosity...in this way we can process the materials as we want… Without using HT and solvents And we can obtain a very clean and pure material by simply depressurizing the autoclave! This can clearly be really important for food packaging and medical applications

## Slide 13: High Pressure Rheometer
Max Pressure: 300 bar
Notes: In oreder to understand and quantify the effects of CO2 on polyesters, I used an high pressure rheometer that allows to measure rheological properties of polymers at several shear rates and up to 300°C and 15 Mpa. It can work both in a rotating mode and in an oscillating mode. I chose PCL as a model because PLA has been widely studied while data on PCL are currently lacking.

## Slide 14: Oscillatory vs rotational experiments
Oscillation
Full rotation
Stiffness
Melting point
Shear-Viscosity
Flow properties
Polymer

## Slide 15: Elastic modulus of PCL – ambient pressure
Pamb
S. Curia et al., Polymer, 2015
Semi-crystalline
Biodegradable
Used for packaging
Suitable for medical applications
Notes: Adding more CO2 and waiting again 50mins it was possible to shift even more the G’ drop. As you can see from this slide…

## Slide 16: Elastic modulus of PCL – in CO2
Pamb
Soaking time
50 mins
50 bar
S. Curia et al., Polymer, 2015
Notes: Adding more CO2 and waiting again 50mins it was possible to shift even more the G’ drop. As you can see from this slide…

## Slide 17: Elastic modulus of PCL – in CO2
100 bar
120 bar
70 bar
50 bar
Pamb
Soaking time
50 mins
∼23 oC
S. Curia et al., Polymer, 2015
Notes: Adding more CO2 and waiting again 50mins it was possible to shift even more the G’ drop. As you can see from this slide…

## Slide 18: Viscosity of PCL 10 kDa: ambient pressure
80 oC
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 19: Viscosity reduction under CO2: PCL 10 kDa
PRESSURE
80 oC
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 20: Viscosity reduction under CO2: PCL 10 kDa
PRESSURE
80 oC
96%
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 21: Q: can CO2 plasticise higher MW PCL?
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 22: Viscosity: PCL 80 kDa vs 10 kDa
10 kDa
(ambient pressure)
80 oC
Shear Rate (s-1)
Viscosity (Pa.s)
Longer chains = higher viscosity
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 23: Polymers: non-Newtonian fluids
log Shear Rate
log Viscosity
Zero Shear Viscosity
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 24: Viscosity of PCL 80 kDa: ambient pressure
80 °C
Shear Rate (s-1)
Viscosity (Pa.s)
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 25: Viscosity reduction under CO2: PCL 80 kDa
PRESSURE
Shear Rate (s-1)
Viscosity (Pa.s)
S. Curia et al., Polymer, 2015, in press
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 26: Viscosity reduction under CO2: PCL 80 kDa
PRESSURE
80 oC
95%
Shear Rate (s-1)
Viscosity (Pa.s)
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 27: Viscosity vs pressure
80 oC
Pressure (bar)
Zero Shear Viscosity (Pa.s)
PCL80
CO2
Q: can we use another gas?
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 28
80 oC
Pressure (bar)
Zero Shear Viscosity (Pa.s)
PCL80
CO2 vs N2
N2
CO2
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 29: CO2 vs N2
80 oC
Pressure (bar)
Zero Shear Viscosity (Pa.s)
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 30: Viscosity of PCL vs T
80 oC
1/Temperature (1/K)
180 oC
Without CO2
S. Curia et al., Polymer, 2015
Zero Shear Viscosity (Pa.s)
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 31: Viscosity of PCL vs T
180 oC
80 kDa
80 oC
CO2 300 bar
10 kDa
80 oC
CO2 300 bar
80 oC
1/Temperature (1/K)
Zero Shear Viscosity (Pa.s)
300 bar at 80 oC in CO2 = 250 oC without CO2!
S. Curia et al., Polymer, 2015
Notes: so taking the viscosity at a given shear rate you can see on the left the data taken at fixed T (20 °C) while increasing pressure and the data taken at fixed p (ambient p) while increasing T…

## Slide 32
Fossil-based resources
Green resources
Monomers
High T
Organic solvents
Toxic catalysts
Polyesters
Low T
No solvents
Enzyme catalysed

## Slide 33
Oleic acid
Barley, rye, wheat
Azelaic acid
Extraction
Ozonolysis
Bio-derived ✓
Non-harmful ✓

## Slide 34: Polymerisation of azelaic acid
T>200 oC
Metal catalysts

## Slide 35
Oleic acid
Barley, rye, wheat
Azelaic acid
Extraction
Ozonolysis
Tm≈110 oC ✗
Insoluble in apolar solvents ✗

## Slide 36: Polymerisation of azelaic acid
Can a green lower T approach be achieved in CO2?

## Slide 37: HP reaction vessel
\
CO2 in
CO2 out
Mechanical stirrer
(60 mL or 20 mL base)

## Slide 38: Green Route to Green Functional Materials
Naturally derived  100% bio-content
Low T:
Save €€€/£££
Preserve enzyme
Preserve functionalities
S. Curia et al., Phil Trans A, 2015, accepted
Lipase
Molecular sieves

## Slide 39: Sorbic alcohol end-capping: NMR
End-capped ✓
MW ✓
No side reactions ✓
3
S. Curia et al., Phil Trans A, 2015, accepted

## Slide 40: Sorbic alcohol end-capping: MALDI-ToF
m/z
Intensity (a.u. x 104)
270.4 g/mol
S. Curia et al., Phil Trans A, 2015, accepted

## Slide 41: Sorbic alcohol end-capping: MALDI-ToF
m/z
Intensity (a.u. x 104)
A=
B=
A3
A4
A5
A6
A7
A8
B4
S. Curia et al., Phil Trans A, 2015, accepted

## Slide 42: Further reaction: Diels Alder chain extension
+
Chain extended interpenetrated network
DA
RT, 24 h
2n
n
DA
Swollen in
CHCl3

## Slide 43: Thermal analysis
40 °C
25 °C
Before curing
After curing
Heat Flow (endo down)
Decreased
crystallinity

## Slide 44: Enzyme recycling: propyl oleate synthesis
Fresh enzyme
Enzyme used at 35 oC/275 bar (CO2)
Enzyme used at 110 oC (melt synthesis)

## Slide 45: Enzyme recycling: propyl oleate synthesis
Chart: Time (h)
| 0 | 1 | 3 | 5 | 24
OLD | 0 | 94.2678 | 96.6666 | 97.0093 | 97.4312
Fresh
S. Curia et al., Phil Trans A, 2015, accepted

## Slide 46: Enzyme recycling: propyl oleate synthesis
Chart: Time (h)
| 0 | 1 | 3 | 5 | 24
OLD | 0 | 94.2678 | 96.6666 | 97.0093 | 97.4312
NEW | 0 | 96.7864 | 98.5542 | 97.9753 | 97.1351
Fresh
CO2 (35 oC, 275 bar)
S. Curia et al., Phil Trans A, 2015, accepted

## Slide 47: Enzyme recycling: propyl oleate synthesis
Chart: Time (h)
| 0 | 1 | 3 | 5 | 24
OLD | 0 | 94.2678 | 96.6666 | 97.0093 | 97.4312
NEW | 0 | 96.7864 | 98.5542 | 97.9753 | 97.1351
 | 0 | 44.7514 | 45.6522 | 48.9796 | 53.271
Fresh
CO2 (35 oC, 275 bar)
Melt process (110 oC)
S. Curia et al., Phil Trans A, 2015, accepted

## Slide 48: Conclusions
CO2 is able to plasticise PCL with varied MW
Used CO2 as a reaction medium to achieve a green low T route to functional materials
Recycling tests showed that the high-pressure reactions are commercially sustainable

## Slide 49: Next Steps
Test cross-linking of the green functional polymers (DSC, DMA) + efficiency test (real time FTIR etc.) (collaboration with KTH)
S. Torron et al., Macromol Phys and Chem, 2014

## Slide 50: Next Steps & future outlook
Radical chain extension of telechelic
A-B-A block copolymer synthesis + analysis
Hydrophilic
Hydrophilic
Hydrophobic
Micelle?
Hydrogel?
Drug delivery?

## Slide 51
Acknowledgments:
Prof Steven M Howdle and Dr Derek J Irvine
KTH people: Prof Karl Hult, Prof Mats Johansson, Prof Mats Martinelle, Susana Timhagen, Stefan Semlitsch
Mark Guyler, Pete Fields and Richard Wilson
Helen Carson
EU, 7th FP and MC actions for funding

## Slide 52: Thank you! … any questions?