## Slide 1
Synthesis and characterization of green nanoparticles and their effect on seed germination.
Sudipta Panja, Kalyani Khanra, Indranil Choudhuri, and Nandan Bhattacharyya
Department of Biotechnology, Panskura Banamali College; Panskura RS; PIN 721152; Purba Medinipur; West Bengal; INDIA

## Slide 2: Introduction
What is nanoparticle?
Nanoparticle is defined as a cluster of atom between 1 to 100 nanometer in size that behaves like a whole unit with respect to its all properties. Nanoparticle is one of the most important gifts of science in modern era.
Nanoparticle have superior properties than the bulk substances
  Mechanical strength
  Thermal stability
  Catalytic activity
  Electrical conductivity
  Magnetic properties
  High driving force for diffusion due to its high surface area to volume ratio
  surface plasmon resonance
  Application of nanoparticles
Microworld
0.1 nm
1 nanometer (nm)
0.01 m
10 nm
0.1 m
100 nm
1 micrometer (m)
0.01 mm
10 m
0.1 mm
100 m
1 millimeter (mm)
1 cm
10 mm
10-2 m
10-3 m
10-4 m
10-5 m
10-6 m
10-7 m
10-8 m
10-9 m
10-10 m
Nanoworld

## Slide 3: Why did we use plant as a starting materials for synthesis of nanoparticles?
Involves the use of less toxic chemicals.
The biologically synthesized nanoparticles may be less toxic.
Eco-friendliness
There are no maintenance as microbial culture.
Cost effective
The plants is a good source of various phytochemicals which have good medicinal value.

## Slide 4: Aim of the study
Synthesis of plant mediated silver nanoparticle which is cost effective.
Characterization of the silver nanoparticle by UV/VIS, TEM, XRD and FTIR.
Study of the antibacterial, antifungal, larvicidal activity of the nanoparticle
Study of cytotoxicity of the silver nanoparticle in cancer cell by MTT assay.
Study the effects of the nanoparticles on the seed germination.

## Slide 5: Synthesis of plant mediated silver nanoparticles
synthesis of silver nanoparticles from plant extract by using 1mM silver nitrate solution
Hydrothermal process.
The plant biomass acts as both reducing agent and stabilizing agent and the solvent is aqueous solution.
Washing of nanoparticle.
Color change of the solution is the indication of synthesis of silver nanoparticles
A
B
C
Leaves of
Cryptolepis buchanani
A
B
C
Stem of
Cryptolepis buchanani
A
B
C
Leaves of
Ehretia laevis Roxb
A
B
C
Leaves of
Rauvolfia serpentina

## Slide 6
Antibacterial and antifungal activity were studied by well diffusion method.
The larvicidal activity of the synthesized silver nanoparticle was tested against mosquito larvae of Aedes aegypti.
Study of cytotoxicity by MTT assay against MCF7 and HeLa cell line.
Study the effect on seed germination by using Lens culinaris.

## Slide 7
Fig A. Nanoparticle from
leaf extract of
Cryptolepis buchanani
Fig B. Nanoparticle from
stem extract of
Cryptolepis buchanani
Fig C. Nanoparticle from
leaf extract of
Ehretia laevis Roxb
Fig D. Nanoparticle from
leaf extract of
Rauvolfia serpentina
A
B
C
D
Characterization of the synthesized nanoparticles by UV -VIS

## Slide 8: Characterization of the synthesized nanoparticles by TEM
A
Fig A. Nanoparticle from leaf extract of
Cryptolepis buchanani
Fig B. Nanoparticle from stem extract of
Cryptolepis buchanani
Fig C. Nanoparticle from leaf extract of
Ehretia laevis Roxb
Fig D. Nanoparticle from leaf extract of
Rauvolfia serpentina
B
C
D

## Slide 9: Characterization of the synthesized nanoparticles by FTIR
A
B
C
D
Fig A. Nanoparticle from leaf extract of
Cryptolepis buchanani
Fig B. Nanoparticle from stem extract of
Cryptolepis buchanani
Fig C. Nanoparticle from leaf extract of
Ehretia laevis Roxb
Fig D. Nanoparticle from leaf extract of
Rauvolfia serpentina

## Slide 10
Bacillus subtilis
Enterococcus faecalis
Antibacterial activity of the AgNP against gram positive bacteria
Chart: Concentration of AgNP in µg/ml
| 25 µg/ml | 50 µg/ml | 75 µg/ml | 150 µg/ml
AgNP from leaf of Cryptolepis buchanani | 6 | 10 | 12 | 13
AgNP from stem of Cryptolepis buchanani | 9 | 12 | 13 | 14
AgNP from leaf of Ehretia laevis Roxb | 8 | 10 | 11 | 13
AgNP from leaf of Rauvolfia serpentina | 11 | 13 | 14 | 16
Ciprofloxacin | 18 | 20 | 22 | 25
Chart: Concentration of AgNP in µg/ml
| 25 µg/ml | 50 µg/ml | 75 µg/ml | 150 µg/ml
AgNP from leaf of Cryptolepis buchanani | 11 | 12 | 13 | 15
AgNP from stem of Cryptolepis buchanani | 11 | 12 | 14 | 15
AgNP from leaf of Ehretia laevis Roxb | 10 | 11 | 13 | 14
AgNP from leaf of Rauvolfia serpentina | 12 | 14 | 15 | 17
Ciprofloxacin | 23 | 27 | 28 | 31

## Slide 11
Antibacterial activity of the AgNP against gram negative bacteria
Pseudomonas aeruginosa
E.coli
Chart: Concentration of AgNP in µg/ml
| 25 µg/ml | 50 µg/ml | 75 µg/ml | 150 µg/ml
AgNP from leaf of Cryptolepis buchanani | 11 | 12 | 13 | 15
AgNP from stem of Cryptolepis buchanani | 10 | 12 | 14 | 16
AgNP from leaf of Ehretia laevis Roxb | 8 | 10 | 12 | 13
AgNP from leaf of Rauvolfia serpentina | 12 | 14 | 15 | 17
Ciprofloxacin | 24 | 27 | 28 | 31
Chart: Concentration of AgNP in µg/ml
| 25 µg/ml | 50 µg/ml | 75 µg/ml | 150 µg/ml
AgNP from leaf of Cryptolepis buchanani | 12 | 14 | 15 | 17
AgNP from stem of Cryptolepis buchanani | 12 | 14 | 15 | 17
AgNP from leave of Ehretia laevis Roxb | 10 | 12 | 13 | 14
AgNP from leave of Rauvolfia serpentina | 13 | 15 | 16 | 18
Ciprofloxacin | 20 | 24 | 26 | 30

## Slide 12
Antifungal activity of the AgNP
Aspergillus niger
Candida albicans
Chart: Concentration of AgNP in µg/ml
| 25 µg/ml | 50 µg/ml | 75 µg/ml | 150 µg/ml
AgNP from leaf of Cryptolepis buchanani | 10 | 12 | 13 | 14
AgNP from stem of Cryptolepis buchanani | 10 | 11 | 13 | 14
AgNP from leaf of Ehretia laevis Roxb | 8 | 9 | 11 | 12
AgNP from leaf of Rauvolfia serpentina | 9 | 11 | 12 | 13
Chart: Concentration of AgNP in µg/ml
| 25 µg/ml | 50 µg/ml | 75 µg/ml | 150 µg/ml
AgNP from leaf of Cryptolepis buchanani | 10 | 11 | 12 | 14
AgNP from stem of Cryptolepis buchanani | 11 | 13 | 14 | 16
AgNp from leaf of Ehretia laevis Roxb | 9 | 11 | 13 | 14
AgNP from leaf of Rauvolfia serpentina | 14 | 16 | 17 | 19

## Slide 13
Larvicidal activity of the AgNP against Aedes aegypti
% Mortality = [(% test mortality- % control mortality)/100-% control mortality]x 100
Chart: Concentration of AgNP in ug/ml
| 2.5 ug/ml | 5 ug/ml | 10 ug/ml | 25 ug/ml
AgNP from leaf of Cryptolepis buchanani | 0 | 0 | 10 | 13 | 23
AgNp from stem of Cryptolepis buchanani | 0 | 16 | 49 | 57 | 77
AgNP from leaf of Ehretia laevis Roxb | 0 | 0 | 17 | 27 | 40
AgNP from leaf of Rauvolfia serpentina | 0 | 75 | 86 | 89 | 91

## Slide 14: Cytotoxicity study of the AgNP against HeLa and MCF7 cell line
HeLa cell line
MCF 7 cell line
Chart: Concentration of nano µg/ml
| 1 ug/ml | 2.5 ug/ml | 5 ug/ml | 10 ug/ml | 25 ug/ml
AgNP from leaf of Cryptolepis buchanani | 89.78 | 92.91 | 95.31 | 85.39 | 81.01
AgNP from stem of Cryptolepis buchanani | 87.53 | 80.42 | 75.31 | 70.63 | 61.7
AgNP from leaf of Ehretia laevis Roxb | 83.72 | 81.39 | 79.65 | 56.97 | 32.55
AgNP from leaf of Rauvolfia serpentina | 82.4 | 65.28 | 63.73 | 57.51 | 29.01
Chart: Concentration of the AgNP in ug/ml
| 1 ug/ml | 2.5 ug/ml | 5 ug/ml | 10 ug/ml | 25 ug/ml
AgNP from leaf of Cryptolepis buchanani | 73.44 | 67.23 | 48.02 | 17.51 | 9.04
AgNp from stem of Cryptolepis buchanani | 78.06 | 70.91 | 54.08 | 16.32 | 8.67
AgNP from leaf of Ehretia laevis Roxb | 90.21 | 94.66 | 80.64 | 52.15 | 45.16
AgNP from leaf of Rauvolfia serpentina | 88.37 | 77.67 | 34.88 | 30.23 | 28.37

## Slide 15
Fig A. Nanoparticle from
leaf extract of
Cryptolepis buchanani
Fig B. Nanoparticle from
stem extract of
Cryptolepis buchanani
Fig C. Nanoparticle from
leaf extract of
Ehretia laevis Roxb
Fig D. Nanoparticle from
leaf extract of
Rauvolfia serpentina
Effects of AgNP on seed germination
A
B
C
D

## Slide 16: Effects of AgNP on the germination of Lens culinaris Seed
Chart: Concentration of AgNP in µg/ml
| 0 µg/ml | 250µg/ml | 500µg/ml | 1000µg/ml
AgNP from leaf of Cryptolepis buchanani | 56 | 76 | 84
AgNP from stem of Cryptolepis buchanani | 60 | 80 | 84
AgNP from leaf of Ehretia laevis Roxb | 68 | 84 | 92
AgNP from leaf of Rauvolfia serpentina | 64 | 72 | 88
Control | 60

## Slide 17: Effects of AgNP on the Vigour Index (VI) of germinated Lens culinaris Seed
Chart: Concentration of AgNP in µg/ml
| 0 µg/ml | 250µg/ml | 500µg/ml | 1000µg/ml
AgNP from leaf of Cryptolepis buchanani | 275.52 | 390.64 | 460.32
AgNP from stem of Cryptolepis buchanani | 346.8 | 490.4 | 559.44
AgNP from leaf of Ehretia laevis Roxb | 425 | 580.44 | 691.84
AgNP from leaf of Rauvolfia serpentina | 414.72 | 491.04 | 633.6
Control | 226.8

## Slide 18: Effects of AgNP on the root length of Germinated Lens culinaris Seed
Chart: Concentration of AgNP in µg/ml
| 0 µg/ml | 250µg/ml | 500µg/ml | 1000µg/ml
AgNP from leaf of Cryptolepis buchanani | 2.69 | 2.85 | 3.04
AgNP from stem of Cryptolepis buchanani | 3.37 | 3.54 | 3.78
AgNP from leaf of Ehretia laevis Roxb | 4.07 | 4.67 | 5.18
AgNP from leaf of Rauvolfia serpentina | 4.29 | 4.54 | 4.72
Control | 2.1

## Slide 19: Effects of AgNP on the shoot length of Germinated Lens culinaris Seed
Chart: Concentration of AgNP in µg/ml
| 0 µg/ml | 250µg/ml | 500µg/ml | 1000µg/ml
AgNP from leaf of Cryptolepis buchanani | 2.23 | 2.29 | 2.44
AgNP from stem of Cryptolepis buchanani | 2.41 | 2.59 | 2.88
AgNP from leaf of Ehretia laevis Roxb | 2.18 | 2.24 | 2.34
AgNP from leaf of Rauvolfia serpentina | 2.19 | 2.28 | 2.48
Control | 1.68

## Slide 20: Conclusion
The synthesized Ag NPs were characterized by different techniques for calculation of crystalline size, particles size, morphology,antimicrobial , larvicidal activity etc.
The different concentrations of AgNPs effect on Lens culinaris seed germination . All the AgNP shows positive effects on seed germination. AgNP from Ehretia laevis shows positive activity on seed germination and AgNP prepared from Ehretia laevis also breaks seed dormancy.

## Slide 21: Future study
The cytotoxicity study on selective cancer cells may lead to therapeutic use as anticancer agent.
It may also effect on breaking of seed dormancy. Further studies are needed to confirm and to determine the mechanisms of breaking seed dormancy.

## Slide 22
Thank You for Your Attention