## Slide 1: A study on the MSWI fly ash modifying for inorganic gel of cement admixtures
2nd World Congress and Expo on
Recycling
Berlin, Germany, July 25-27, 2016.
Sue-Huai Gaua, Chang-Jung Sunb, Ming-Guo Lia and Yen-Hsun Leea
Tamkang University
Taoyuan Innovation Institute of Technology
Taiwan, ROC.

## Slide 2: Outline
Background
1
Methods
2
Results and Discussion
3
Conclusions
4

## Slide 3
Background

## Slide 4: Background
Municipal solid waste incinerator (MSWI) fly ashes contain high concentrations of heavy metals and dioxins, which are defined as hazardous wastes usually.
Solidification followed by designated landfilling has been popular used in the world, but the long term stability still be worried about.
Zero-Waste or Zero-Landfill policy has been ask in many countries, therefor, there were many studies discussed with the recycling of the MSWI fly ash, while seldom of then were commercialized.

## Slide 5: Background
Eco-cement and melting technologies have been developed in Japan for three decades already, but still been questioned a lot today.
Dioxin could be destroyed in the high temperature of cement kiln, but most of the heavy metals will evaporated in the form of chloride compounds, increased the hazard of fly ash in the APCD.
MSWI fly ashes have the characteristics of pozzolanic property, but applied as the substitute of cement directly is not feasibly due to the impurities in it.

## Slide 6: Background
Washing followed by wet ball milling had been proved to have the ability to elevate the pozzolanic property and destroy Dioxin effectively, due to the mechno-chemical reaction.
The pozzolanic material could be activated by alkali hydroxide accompanied with sodium silicate, which could produce an inorganic gel material to elevate the strength during cementing.

## Slide 7: Background
In this study, the silicate component comes from metakaolin, calcium comes from washed MSWI fly ash, and the activation were executed by wet ball milling under the sodium hydroxide solution, after drying, the product was used as the cement admixture.

## Slide 8
Methods

## Slide 9: Methods
Fly ash was collected from the reaction product of a 1,350 ton/d MSW mechanical grate incinerator operated around 950 oC, with semi-dry and bag-filter system.
Ash washing was carried out twice with distill water in a liquid to solid ratio 5 for 5 min.

## Slide 10: Methods
Metakaolin was adopted the industrial grade of kaolin from Yun-nan China. After drying, calcining at 550 oC for 1.5 hr, then 700 oC 3hr.
Conventional ball-milling machine were used, the liquid to solid ratio was 9 during the milling of the mixed ash, the ball miller were operated below the critical speed.

## Slide 11
Results and Discussion

## Slide 12
Table 1 The properties of MSWI fly ash and metakaolin |  |  |  | 
 | pH | Moisture content (%) | Ignition loss (%) | D50 (μm)
Raw fly ash | 11.28 | 1.03 | 3.38 | 7.38
Washed fly ash | 12.15 | 2.8 | - | 7.07
Metakaolin | 4.37 | 0.5 | - | 8.92

## Slide 13
Table 2 Elements |  |  | 
Elements | Washed fly ash |  | metakaolin
Ca | 32.4 |  | 0.09
Si | 2.03 |  | 19.3
Al | 0.61 |  | 16.7
Mg | 1.06 |  | 0.07
Fe | 0.72 |  | 0.71
Na | 0.62 |  | 0.54
K | 0.46 |  | 1.22
 |  |  | Unit：wt.%
Table 3 Heavy metals content |  |  |  | 
Elements |  | Washed fly ash |  | metakaolin
Zn |  | 18,400 |  | 124
Pb |  | 3,170 |  | 352
Cd |  | 207 |  | N.D. a
Cr |  | 281 |  | 90
Cu |  | 3,450 |  | 438
aN.D.：Not detectable |  |  |  | Unit：mg/kg

## Slide 14
Table 4 TCLP leaching concentration |  |  |  |  |  | 
Elements |  | Washed fly ash |  | metakaolin |  | Hazardous waste standard
Zn |  | 1.84 |  | 0.14 |  | -
Pb |  | 7.69 |  | 0.3 |  | 5
Cd |  | N.D.a |  | N.D. |  | 1
Cr |  | 0.06 |  | N.D. |  | 5
Cu |  | 0.11 |  | N.D. |  | 15
aN.D.： No detectable (Pb=5 ppb, Zn=0.3 ppb, Cu=0.6 ppb, Cd=0.35 ppb, Cr=0.5 ppb) |  |  |  |  |  | Unit：mg/L

## Slide 15: Fig. 1 XRD pattern

## Slide 16: Fig. 2 XRD pattern of active powder ( 1M NaOH, 24h)

## Slide 17: Fig. 5 XRD crystalline of milling activation
and so on
XRD crystalline phase
* Activation： 1M NaOH 24h

## Slide 18: Fig. 3 FTIR pattern (1M NaOH, 24h)

## Slide 20: Table 6 TCLP leaching the activation powder ( 1M NaOH 24h)
Not detectible
Powder ratios
Regulation

## Slide 21
Fig. 4-8 The XRD pattern of milled active powder treated by NaOH active solution (50% CKAO + 50%WFA, 24h)

## Slide 22: Table 7 XRD crystalline of milling activation powder in NaOH solution
Activation: 50% CKAO + 50%WFA, 24h of milling
XRD crystalline phase

## Slide 23
Fig. 4-9 FTIR pattern of the milling activation (50% CKAO + 50%WFA, 24h)

## Slide 24
Table 8 The TCLP leaching of the milling activation powder
Not detectible
Active parameter： 50% CKAO + 50%WFA, 24h of active time
NaOH active solutions
Limitation

## Slide 25: 活化液濃度對活化粉取代水泥之影響(1/1)
NaOH活化液濃度對研磨活化粉取代水泥10%之28天水泥漿體與28天水泥漿體經SAM前處理之FTIR分析
活化粉條件：
1.50%CKAO+50%WFA
2.活化24 hr
Pure cement ：養護28天純水泥漿體
SAM：水楊酸-甲醇萃取前處理

## Slide 26
Fig. 4-12 XRD pattern of milled active powder in different active time (50% CKAO + 50%WFA, 24h)

## Slide 27: Table 9 XRD crystalline of milling activation powder
XRD crystalline phase
metakaolin and extracted fly ash before active process
Milling activation： 50% CKAO + 50%WFA, 1M of NaOH

## Slide 28
Fig. 4-12 FTIR pattern of milling activation powder (Active parameter： 50% CKAO + 50%WFA, 1M of NaOH)

## Slide 29
Table 10 The TCLP of the milling activation powder at different activation time
active time
Regulation
Not detectible
Activation： 50% CKAO + 50%WFA, 1M of NaOH

## Slide 30: Relative compressive strength
Activation:
1 M NaOH, milling 24 hr
10%
5%
Relative compress strength (%)
Relative compress strength (%)
Curing time (day)
Curing time (day)

## Slide 31: Relative compressive strength
Cement additive 5%
Activation 24 hr
50%CKAO+50%WFA
Cement additive 5%
Activation:1M NaOH
50%CKAO+50%WFA
7 28
Curing time (day)
7 28
Curing time (day)
Relative compress strength (%)
Relative compress strength (%)

## Slide 32
Fig. 4-22 FTIR pattern of active powder with stirring and milling activation(50% CKAO + 50%WFA, 1M of NaOH 24h)
stirring active
milling active

## Slide 33
Cement additive 5%
Relative compressive strength (%)
7 28
Curing time (day)
stirring activation
milling activation

## Slide 34
Conclusions

## Slide 35: Conclusions(1/3)
The reaction of 50% metakaolin, 50% washed fly ash (5C5W) with 1M NaOH solution after 24 hr milling produces multiple crystal species of inorganic gel.
TCLP test showed that, the activated powder were far below the hazard waste limitations of heavy metals.

## Slide 36: Conclusions(2/3)
The milling activation powder were replaces 10% of cement, low workability caused lower relative compressive strength.
Replacing 5% cement grouting to cure 7 days and 28 days, could form inorganic gels in the cured cement evidently, which raised the relative compressive strength up to 100% compared to the pure cement sample.

## Slide 37: Conclusions(3/3)
For the activated powder process, milling activation has more contribution than stirring activation in the formation of inorganic gel and helps the growth of inorganic gel in cement curing.

## Slide 38
Taiwan, ROC
Sunset of Tamsui River

## Slide 39
Thank you for your Attention
E-mail: shgau@mail.tku.edu.tw