## Slide 1
Nanostructured Composites of Graphene/Metal Oxides for Effective Natural Gas Sweetening
-Dr. Sunil Lonkar
Department of Chemical Engineering
The Petroleum Institute
Abu Dhabi, UAE

## Slide 2: PI at Glance
PI was established in 2001 in Abu Dhabi, UAE
A premier engineering education institute in Middle East, 2000 undergraduate and graduate students, over 200 faculty
The PI’s sponsors and affiliates include the Abu Dhabi National Oil Company (ADNOC) and four major international oil companies that include BP, Japan Oil Development Company, Shell and Total.
Nanotek 2014

## Slide 3: Outline
  Introduction
  Synthesis and Characterization
  - Graphene Oxide
  -Graphene/Metal Oxide nanohybrids
  Adsorption Mechanism
  Sorption studies
  Remarks
2
Nanotek 2014
Notes: 2
2

## Slide 4: Introduction
Natural Gas (NG)
Purification
Raw gas
Purified gas
The geology of NG recourses
Source: US geological survey
Cleanest fossil fuel
I
II
3
Nanotek 2014
Notes: Most natural gas extracted from the Earth contains, to varying degrees, low molecular weight hydrocarbon compounds; examples include methane (CH4), ethane (C2H6), propane (C3H8) and butane (C4H10).

## Slide 5: Natural Gas Sweetening
S
H
H
Sour Gas
- The gas containing more than 4 ppm of hydrogen sulfide (H2S) under STP
Offensive odor
High toxicity
Serious corrosion problems
Reduce efficiency of gas treatments
Natural Gas sweetening processes
Chemical absorption using aqueous amines (Amine Sweetening process)
  Challenges
  -Intensive energy requirement for regeneration
  -Amine foaming in the absorber
  -Corrosion
  -Oxidative and thermal degradation of amine in the regenerator
Amine column
4
Nanotek 2014
Notes: 100 ppm for longer time is enough to cause death
H2S is also known to be a major contributor to acid rain when oxidized in the atmosphere to SO2.
Amine treatment/scrubbing: Alkylamines, Monoethanolamine (MEA), Methyldiethanolamine (MDEA)

## Slide 6: Solid Adsorbents
Physical process: van der Waals and electrostatic forces
High surface area, thermal stability, defined pore size and reactivity (polarity)
Zeolites (natural and synthetic), Metal oxides, and Carbonaceous adsorbents for gas separations
Adsorption
H2S
Metal Oxide
5
Nanotek 2014

## Slide 7: Hybrid Adsorbent Materials
“Multidimensional hierarchical composites can take full advantages of each kind of components, which is an effective way for the preparation of multifunctional materials with exceptional properties”
Metal Oxides:
-Zinc, Iron and Copper Oxides posses high thermal stability and proven reactivity towards H2S
Carbon materials
- Activated carbon, Graphene, CNTs etc. posses very high surface area, ability tailor surface properties
Chemosphere 58 (2005) 467–474., Chem. Engg. J. 166 (2011) 1032–1038.,.
Graphite Oxide with Copper (Hydr) oxychlorides
Bandosz et al., ACS Appl. Mater. Interfaces 2012, 4, 3316−3324
ZnO–silica composites with 3D macropores structures as sorbents for H2S removal at RT, Wang et al. ACS Appl. Mater. Interfaces, Article ASAP
6
Nanotek 2014
Notes: If we combine the porosity and high surface area of carbon materials and reactivity of metal oxide a new adsorbent system with high efficiency can be developed.
The combination of multidimensional nanomaterials can take full advantages of each kind of components

## Slide 8: Graphene/Metal Oxide Nanohybrids
Single layer of carbon atoms arranged in a honeycomb lattice
Surface area = 2630 m2/g ,
Mechanical Properties (1200 GPa),
Electrical Conductivity (3000 S/cm),
Thermal conductivity (5000 W/(m.K)
Hybridization of selected nanosized metal oxides (NMOs) supported on carbonaceous graphene. This combination allows for efficient adsorption due to the very high surface area of graphene and high reactivity of NMOs.
Nanoparticle aggregation is major issue in gas-solid adsorption
Loss in active surface area and subsequently lower efficiency as adsorbent.
Aggregation
7
Nanotek 2014
Notes: Graphene (2 dimensional, mono-atomic thick sp2-carbon structure) has recently received increasing attention as a material of interest due to its high electronic conductivity, large surface area and high mechanical strength
For gas-solid adsorption, one of the major issues is to avoid aggregation of nano-sized particles Which eventually losses in active surface area, with consequences of lower utilization efficiency of the adsorbent.

## Slide 9: Adsorption mechanism
I.
ZnO (s) + H2S (g)
ZnS (s) + H2O (g)
Hot air /O2
II.
CuO (s) + H2S (g)
CuS (s) + H2O (g)
III.
F2O3 (s) + 3H2S (g)
Fe2S3 (s) + 4H2O (g)
8
Nanotek 2014
Notes: Higher conductivity of the graphene phase than that of graphite oxide helps in electron transfer in redox reactions

## Slide 10: Experimental
GO synthesis (Improvised Tours Method)
Graphite Oxidation
30 min
90 min
72 hr
96 hr
Graphite
+
H2SO4
H3PO4
+
KMNO4
H2O2
+
H2O
  High surface area GO can be obtained
  May have high pore volume
  Greater amount of hydrophilic oxidized graphene
  More regular carbon framework and large GO sheets
9
Nanotek 2014
Notes: 9
9

## Slide 11: GO Characterization
GO
XPS
0.34
Graphite
0..81
Graphite Oxide
Oxidation
XRD
TEM
AFM
10
Nanotek 2014

## Slide 12: Synthesis of Graphene/Metal Oxide Hybrids
In-situ thermo-annealed synthesis
Similar protocol was used to synthesize Graphene/CuO and Graphene/Fe2O3 composites
11
Nanotek 2014
Notes: Electonegatice sites such as epoxy, carboxyl and hydoxyl easily interacts with metal hydroxides which is the seeds for metal oxide nanopaticles

## Slide 13: Characterization of Nanohybrids
Graphene/ZnO
XRD
TEM
XRD reveals formation of highly crystalline ZnO nanoparticles in conjunction with reduction GO to TRG
TEM confirms the uniform dispersion of ZnO NPs into resulting hybrids.
Particle size appear to be below 10 nm (ZnO QDs)
12
Nanotek 2014

## Slide 14: Graphene/CuO
CuO
TRG
XRD
TEM
TEM confirms the uniform dispersion of CuO NPs into resulting hybrids having particle size below 20 nm
XRD reveals formation of highly crystalline CuO nanoparticles in conjunction with reduction GO to TRG
13
Nanotek 2014

## Slide 15: Graphene/Fe2O3
XRD
XRD reveals formation of highly crystalline Fe2O3 nanoparticles in conjunction with reduction GO to TRG
Phase change from alpha to gamma for Fe2O3 was observed in presence of graphene.
Uniform dispersion of Fe2O3 NPs into resulting hybrids having particle size below 50 nm
Fe2O3
TRG/ Fe2O3
TEM
14
Nanotek 2014

## Slide 16: H2S sorption capacity
Adsorption Parameters:
Pressure = Ambient Pressure
Temperature = 23-25°C
H2S Flow Rate = 48 mL/min
N2 (Purge) Flow Rate = 50 mL/min
N2 (Balance) Flow Rate = 20 mL/min
(N2)
(N2)
(2,000 ppm H2S/N2)
(N2)
15
Nanotek 2014

## Slide 17: Graphene/ZnO H2S Sorption capacity @ 25 oC
Sorbent = TRG/ZnO ( 5 wt%)
Mass Increase = 18% (Maximum sorption capacity was NOT reached)
Mass of H2S Adsorbed (per 1.00 g sorbent) = 0.18 g H2S
Moles of H2S Adsorbed (per 1.00 g sorbent) = 5.28 mmol H2S
Sorption Capacity of Sorbent = 5.28 mmol H2S/g TRG-ZnO
(Sorption capacity of Methyldiethanolamine [MDEA] is about 4.2 mmol H2S/g amine)
16
Nanotek 2014

## Slide 18: Remarks
Successfully synthesized nanohybrids of graphene with selected metal oxide (ZnO, CuO and Fe2O3).
In-situ thermo annealing process is effective for NPs synthesis with simultaneous GO reduction.
Characterization confirms that hybridization result in uniform dispersion of NPs on graphene surface.
Initial H2S adsorption studies confirms that these hybrid posses great potential to be used in natural gas sweetening process
Further studies are required to understand the regeneration process and efficiency of other metal oxides.
17
Nanotek 2014

## Slide 19: Acknowledgements
Chair, Chemical Engineering Department
Dr.Ahmed Abdala & Dr.Vikas Mittal
Mr.Vishnu Pillai
18
Nanotek 2014

## Slide 20: Thank you!!
19
Nanotek 2014