## Slide 1
Hydrodeoxygenation of bio-oil model compounds over supported Nickel Catalysts
T.M. Sankaranarayanan1, A. Berenguer1,P. Jana1, I.Moreno1,2,J.M.Coronado1,P.Pizarro1,2,
D.P. Serrano1,2
1IMDEA Energy Institute, Avda. Ramón de la Sagra 3, Móstoles, Madrid, Spain
2Department of Energy and Chemical Technology, ESCET, Universidad Rey Juan Carlos, Móstoles, Madrid, Spain

## Slide 2
How long will Fossil
Hydrocarbon fuels last ?
FUEL Reserve/Production
Oil 13978 days (~38 years)
Gas 59404 days
Coal 150,573 days
The use of fossil fuels at the present rate is not sustainable due to:
1. Rapid depletion of resources
2. Carbon emission – global warming due to greenhouse gases (GHG)

## Slide 3
Biomass Sources For Biofuels
Lignocellulose (cellulose, Hemicellulose, Lignin)
Starch
Sugars
Lipid glycerides ( Vegetable Oils & Animal Fats)
USE RENEWABLE
AND
CARBON NEUTRAL BIO-MASS BASED FUELS

## Slide 4
B.Kamm and M.Kamm, Appl Microbiol Biotechnol 64 (2004) 137-145

## Slide 5
Ligno-cellulosic
Biomass
Bio-oil
~ 50 wt.% oxygen
~28-35 wt.% water
Pyrolysis
500 ºC
Inert atmosphere
Bio-Oil yield: 60-70 wt.%
Energy yield:~ 60-70 %
Wt, % | Composition
20-30 | Water
15-30 | Lignin compounds
10-20 | Aldehydes
10-15 | Carboxylic acids
5-10 | Carbohydrates
2-5 | Phenols
1-4 | Furfurals
2-5 | Alcohols
1-5 | Ketones
1 Ton
~0.6-0.7 Ton
Ref: http://www.btgworld.com/en/news

## Slide 6
Objective
The HDO of bio-oil model compounds.
Experimental
Results and discussion
Conclusion

## Slide 7
Guaiacol [GUA]
Propionic acid [PA]
Catalysts:
5% of Ni on
H-ZSM-5 Comm
hierarchical-ZSM-5 [Seed Silanization]
Mesostructured Al-SBA-15
Mesostructured SBA-15
Feed:
Ref: Catalysis Today, Volume 243, 163-172, 2015
Feed 1: GUA (3%) in decalin
Feed 2: GUA(2%)+PA(1%) decalin

## Slide 8
Experimental and Catalytic activity
h-ZSM-5
SBA-15
Al-SBA-15
Incipient Wetness impregnation method
5% of Ni loaded on the supports
Calcined at 550 ᵒC/5h (static air)
Reduced at 500 ᵒC/3h (∼80 ml of H2)
Reactant : | 3% of Feed in decalin
Catalysts : | 0.15 g
Reactor volume and speed: | 100 ml, 1000 rpm
Temperature : | 260 ᵒC
H2Pressure(Initial): | 40 bar
Reaction Time : | 2 h
Product Analysis : | GC, GC-MS

## Slide 9
Physicochemical characteristics of the catalyst

## Slide 10
Sample Name | Actual Metal Content [%] [ICP]a | SBET [m2/g]b (Sext)* | Vpore [cc/g]c | D[%]d | Metallic surface area, S [m2/g-M] d | Metal Crystallite size, dp [nm] d | Acidity [mmol/g]e
H-ZSM-5 Comm | 30 (Si/Al) | 437(93)* | 0.42 | - | - | - | 0.331
Ni/H-ZSM-5 Comm | 4.53 | 381(45)* | 0.27 | 4.4 | 28 | 24 | --
h-ZSM-5 | 47(Si/Al) | 563(302)* | 0.601 | - | - | - | 0.353
Ni/h-ZSM-5 | 4.41 | 469(210)* | 0.545 | 12 | 80 | 8.5 | --
Al-SBA-15 | 70(Si/Al) | 922 | 1.25 | - | - | - | 0.123
Ni/Al-SBA-15 | 4.55 | 697 | 0.82 | 7.6 | 50 | 13.3 | --
SBA-15 | - | 772 | 1.38 | - | - | - | 0.049
Ni/SBA-15 | 4.37 | 544 | 1.10 | 2 | 14 | 48 | --
Surface area, Surface acidity and H2-Chemisorption
aSi/Al ratio and actual metal content from ICP; bSurface area determined by BET method; cTotal pore volume measured at P/Po- 0.98; dMetal dispersion, Metallic surface area and Metal crystallite size from H2-chemisorption method; eAcidity data measured by TPD analysis using Ammonia as a probe molecule [mmols of NH3 desorbed /g of sample in the range, 100-600 ˚C
micro
hierarchical
Mesostructure

## Slide 11
X-Ray Diffraction
h-ZSM-5
The low angle diffraction reveals the presence of orderded Meso structure before and after metal impregnation.
The well-defined peaks corresponding to (1 0 0), (1 1 0) and (2 0 0) reflections, which are characteristics of a 2D hexagonal mesostructure p6mm, are clearly observed for SBA-15.
Additional phases were not observed in the case of MFI based samples, where as Ni-phases were observed in mesoporous supported samples
Al-SBA-15
SBA-15

## Slide 12
Temperature Programmed Reduction (TPR)
Transmission electron microscopy (TEM)
metal-support interaction and Dispersion:
h-ZSM-5 > Al-SBA-15 >H-ZSM-5 comm> SBA-15

## Slide 13
RESULTS AND DISCUSSIONS
The Conversion of Guaiacol was in the order :
Ni/h-ZSM-5~Ni/Al-SBA-15>Ni/SBA-15>Ni/H-ZSM-5 Comm
3% of Guaiacol; Temp,260˚C; Pres, 40 bar; Time, 2h
Ni/H-ZSM-5 Ni/h-ZSM-5 Ni/Al-SBA-15 Ni/SBA-15
Comm

## Slide 14
Product distributions

## Slide 15
The Conversion of Guaiacol was in the order :
Ni/h-ZSM-5>Ni/Al-SBA-15>Ni/SBA-15>Ni/H-ZSM-5 Comm
The Conversion of Propionic acid was in the order :
Ni/Al-SBA-15>Ni/h-ZSM-5>Ni/SBA-15>Ni/H-ZSM-5 Comm
75%
78%
2% of GUA +1% of PA; Temp,260˚C; Pres, 40 bar; Time, 2h
Ni/H-ZSM-5 Ni/h-ZSM-5 Ni/Al-SBA-15 Ni/SBA-15
Ni/H-ZSM-5 Ni/h-ZSM-5 Ni/Al-SBA-15 Ni/SBA-15
Conversion of GUA
Conversion of GUA+PA
Comm
Comm

## Slide 16
Product distributions with respect to Guaiacol

## Slide 17
Product distributions with respect to Propionic acid

## Slide 18
CH3OH
CH3—O—CH3
+
Reaction pathway
DMO
HYD
HYD
DH
DH
DMO
HYD
DDO
ISO
CRK
CRK
ISO
Ni/h-ZSM-5
Ni/Al-SBA-15
Feed 1
DMO - Demethoxylation
DDO - direct deoxygenation
HYD - Hydrogenation
DH - dehydration
ISO - isomerization
CRK - craking

## Slide 19
CH3OH
CH3—O—CH3
+
Reaction pathway
DMO
HYD
HYD
DH
DH
DMO
HYD
DDO
ISO
CRK
CRK
ISO
Ni/h-ZSM-5
Ni/Al-SBA-15
Feed 2
HYD
DH
HYD

## Slide 20
CH3OH
CH3—O—CH3
+
Reaction pathway
DMO
HYD
HYD
DH
DH
DMO
HYD
DDO
ISO
CRK
CRK
ISO
Ni/h-ZSM-5
Ni/Al-SBA-15
Feed 2
CH3OH
+
PA

## Slide 21
HYD
DM
HYD
Ni/SBA-15
Reaction pathway
Feed 1

## Slide 22
CH3OH
HYD
DM
HYD
DMO
Ni/SBA-15
Reaction pathway
Feed 2

## Slide 23
CH3OH
C6H11OH
HYD
DM
HYD
DMO
Ni/SBA-15
Reaction pathway
Feed 2

## Slide 24
Best Activity
Ni/h-ZSM-5 > Ni/Al-SBA-15 > Ni/SBA-15 > Ni/H-ZSM-5 Comm

## Slide 25
Conclusions
Ni/h-ZSM-5 supported catalysts show the highest guaiacol conversion compared to supports.
  The acidity of the supports associated with the metals strongly favors the HDO conversion of Guaiacol. DMO favours the propionic acid esterification.
Hydrodeoxygenation, hydrodearomatization and isomerization reactions take place in high extension over the Ni/h-ZSM-5 sample, revealing it is a suitable catalyst for bio-oil processing in order to attain high quality fuels

## Slide 26
Sincere Thanks to all my group members, Technicians, Administrative Staffs!!
Thank you all for your kind attention !!!