## Slide 1: Title
Institute of Fluid Science
Large Scale Molecular Simulations for Transport Phenomena in Polymer Electrolyte Fuel Cell
Quantum Nanoscale Flow Systems Laboratory, Nanoscale Flow Division
Novel Battery Nanoscale Flow Laboratory, Innovative Eenrgy Research Center
Institute of Fluid Science, TOHOKU UNIVERSITY
Takashi Tokumasu
12/08/2015
Nanotechnology-2015

## Slide 2: Background
1kW 10kW 100kW 1MW 10MW 100MW
Mobile
Home
Car
Factory
Office
PAFC
SOFC
PEFC
MCFC
Power
How to
use
Kind
Fuel Cell : Next Generation Power Supply System
High efficiency of energy exchange
Low environment damage (without generating NOx, SOx, .etc)
Low vibration, low noise (without explosion and combustion)
Low driving temperature
No scatter of electrolyte
High power density
Polymer Electrolyte Fuel Cell (PEFC)
Firstly commercialize among all fuel cells

## Slide 3: Importance of material transport
Transport phenomena of materials in PEFC
・Gas Diffusion Layer: GDL
・Micro Porous Layer: MPL
・Catalyst Layer: CL
・Polymer Electrolyte Membrane: PEM
construct the flow fields whose characteristic length is from micro to nano meter.
GDL
MPL
GDL
MPL
CL
CL
PEM
The analyses of transport phenomena of materials in nanoscale to mezoscale greatly contribute to the development of next generation of fuel cell
The characteristics cannot be analyzed by continuum theory
Currency
Voltage
Ohmic
Loss
Transfer
Loss
Catalytic
Loss
POWER
POWER
Ideal(1.23V)
Trasfer loss : reactant materials (proton, oxygen) and
product material (water) cannot move faster in PEFC
enough to generate such high currency
It is very important to analyze the transport phenomena of materials (proton, water and oxygen) in PEFC.
Decrease of transfer loss is important to improve the efficiency of a PEFC

## Slide 4: Research Theme about Fuel Cells
Oxygen permeability of ionomer
in Catalyst Layer
Phase diagram of water in a nano pore of MPL
(with the University of Tokyo)
Transport properties of nanoscale water droplet in MPL
Initial Translational Energy
: Pt-Fix
: T=0 K
: T=300 K
Dissociation Probability [-]
Dissociation phenomena of H2 on Pt catalyst
Proton diffusivity in PEM

## Slide 5: 1st Topic
Analysis of transport phenomena of proton and water in polymer electrolyte membrane
Oxygen permeability of ionomer
in Catalyst Layer
Phase diagram of water in a nano pore of MPL
(with the University of Tokyo)
Transport properties of nanoscale water droplet in MPL
Initial Translational Energy
Dissociation phenomena of H2 on Pt catalyst
Proton diffusivity in PEM

## Slide 6: Mechanism of Proton Transfer
Mechanism of Proton Transfer
・Vehicle Mechanism (slow)
(H3O+ ion moves directly)
-
PerFluoroSulfonic Acid Membrane (PFSA)
Main Chain
Side Chain
Main Chain
Side Chain
Water Cluster
Structure of water in PEM
Network of hydrogen bonding is formed in the membrane
Information of the relation between transport phenomena and structure of water is needed.
Transport
Structure
Strong relation
Proton (H+): has high chemical reactivity.
exists as an Oxonium ion (H3O+) by connecting with a water molecule (H2O).
・Grotthus Mechanism (fast)
(H3O+ is seen to move by hopping
in network of hydrogen bonding)

## Slide 7: Objectives of This Research
To obtain knowledge about the relation between proton and water transport and water structure by using Molecular Dynamics (MD) simulation.
Institute of Fluid Science
Vehicle Mechanism
Grotthus Mechanism
What is the characteristics to determine the proton conductivity of membrane?
Water culster

## Slide 8: EVB Model
R=2.2～2.8Å
q
Zundel cation（H5O2+）
 | DH3O+ [10-5 cm2/s] | DH2O [10-5 cm2/s]
w/o hopping | 0.75 | 2.37
w/ hopping | 5.23 | 2.38
Experiment | 9.4 | 2.3
255 H2O & 1 H3O+
T = 298.15 [K]
P = 1 [atm]
*Park, K. J. Phys. Chem. 2012, 116, 343.
Diffusivity of H3O+ and H2O in water

## Slide 9: Simulation Method
Structural analysis
RDF & Cluster analysis
Dynamical analysis
MRT & MSD
Nafion chain
・(N7P)13
・25 chains
Samping with NVE (300 K)
Annealing
t (ns)
0
1.2
N
P
Solvent molecules (liq=H3O++H2O)
・ NH3O+=NSO3-=325
・Water contents λ=(NH3O++NH2O)/NSO3-
=1, 3, 6, 9, 12, 15, 18
Annealing
Chemical structural formula of Nafion
The agreement with experiment is within 1.3 %.
1. Morris, D. R. J. Appl. Polym. Sci. 1993, 50, 1445.
Notes: 9

## Slide 10: Cluster Analysis
Abrupt decrease
= Network formation
Small clusters
Large clusters
Wide range of
cluster size
The number of water cluster and their size is analyzed.
The transport channels for oxonium ions are widely formed at λ = 6.
SO3-
H2O
H3O+
Polymer

## Slide 11: Diffusion Coefficient of H3O+ and H2O
Water content : low (λ=3)
Network of hydrogen bond is short
Grotthus contribution is small
Proton diffusivity is small
λ=3
Water content : high (λ>6)
Water cluster becomes continuous
Grotthus contribution is large
Proton diffusivity is large
λ=6
The results are qualitatively consistent with the experimental results.
From this research we can obtain the relation between proton conductivity and nanoscale structure of water cluster in PEM
The information is useful to develop a membrane which has high proton conductivity

## Slide 12: 2nd Topic
Analysis of Oxygen Permeation of Ionomer in Catalyst Layer
Oxygen permeability of ionomer
in Catalyst Layer
Phase diagram of water in a nano pore of MPL
(with the University of Tokyo)
Transport properties of nanoscale water droplet in MPL
Initial Translational Energy
Dissociation phenomena of H2 on Pt catalyst
Proton diffusivity in PEM

## Slide 13: Cathode Catalyst Layer in PEFC
Ionomer = polymer + water molecule
e-
O2
H+
1nm
Structure of cathode catalyst layer
Polymer electrolyte
membrane
Supported carbon
PEM
CL
GDL
O2
H+
H2O
Catalyst (Platinum)
Ionomer
(Ionized thin film : 3nm)
Proton transport in ionomer (proton conductivity)
larger as the ionomer is thicker
Oxygen permeate through ionomer (oxygen permeability)
larger as the ionomer is thinner
4H++4e-+O2 → 2H2O
Transport phenomena of materials(H+, O2) in/through ionomer is very important!
A good ionomer makes proton and oxygen reach to Pt surface in the proper ratio (H+:O2=4:1)
Now we focus on the oxygen permeability of ionomer.

## Slide 14: Objective of This Research
Real
System
：Polymer
：
：
：Pt
To make an ionomer which consists of fluorocarbon and water
To characterize the structure of ionomer on Pt surface
To investigate the oxygen permeability of the ionomers against water content
To analyze the oxygen permeability of ionomer on Pt surface by molecular dynamics method.
Parameters : water content
Details of this research
Simulation
Model

## Slide 15: Simulation Method
- Periodic boundary condition (x,y)
- Mirror boundary condition (z)
- Time Integration: velocity verlet + rRESPA
- Water content (λ=(Noxo+Nwat)/Nso3-) : 3,5,7,9,11
- Temperature：350K (operation temperature of PEFC)
- Simulation domain：66.5×57.6×100.0 Å
- Temperature control：velocity scaling
10 MPa
0MPa
Simulation process
PFSA : 15 chains (5205 atoms)
H3O+ : 75 molecules(300 atoms), Pt : 5layers (2880 atoms)
H2O : changes according to water content
150, 300, 450, 600, 750 molecules
(450, 900, 1350, 1800, 2250 atoms)
0ns
0.8ns
21.6ns
1.6ns
Annealing Process
Sampling Process
1.5ns
To make
an ionomer
To put the ionomer
on a Pt surface
To sample the properties
Oxygen is added

## Slide 16: Material Distribution
Density [kg/m3]
PFSA
Ionomer swells according to water content
A higher peak is observed near Pt surface (z=15Å)
↓
Polymer adsorbs on a Pt surface
A higher peak is observed in the peak of PFSA
↓
More water distributes in the peak of PFSA
z
11Å
z [Å]
Ionomer
Water
Characteristics of Ionomer of PFSA

## Slide 17: Oxygen Permeability
Oxygen permeability decreases against water content
Water content λ | 3 | 5 | 7 | 9 | 11
No. of permeated O2 | 67 | 21 | 19 | 13 | 11
O2 is more difficult to permeate through both ionomer-gas interface and bulk region with the increase in water content
The number of O2 permeation path is large in ionomer-Pt interface at λ=3
The number of path decrease at λ=11
→ Water molecules put in the O2 permeation path at ionomer-Pt interface with the increase in the water content
z [Å]
x [Å]
λ=11
λ=3
λ=7
Density distribution of O2
Ionomer
Water
z [Å]
Density [kg/m3]
Bulk region
Pt
ionomer-Pt
interface
ionomer-gas
interface
From this research we can obtain the relation between oxygen permeability and nanoscale structure of ionomer in CL
The information is useful to develop a CL which perform efficient chemical reaction

## Slide 18: Summary
Transport phenomena in Fuel Cell
(1) Transport phenomena in polymer electrolyte membrane
(2) Transport phenomena in catalyst layer
The nano/mezo scale mechanism of transport phenomena in MEA is analyzed by large scale quantum/molecular dynamics simulation.
From the results, design concept of MEA (GDL, CL, PEM) which have the most efficient transport characteristics is obtained.
(Accuracy of numerical estimation of efficiency of fuel cell is dramatically increased.)
The period and cost of development by experiment is largely cut.
Contribution of Green Innovation is very large!
Various flow fields which size is from nanometer to micrometer is formed
Flow (transport) phenomena is different from that obtained by
conventional macroscopic theory

## Slide 19: Acknowledgment
Institute of Fluid Science
Thank you for
the kind attention!
A part of this study was financially supported by Research and Development of Polymer Electrolyte Fuel Cells from New Energy and Industrial Technology Development Organization (NEDO) of Japan.
Almost all simulations were performed by a supercomputer system of Advanced Fluid Information in Institute of Fluid Science, Tohoku University.
Special Thanks:
Hironori Sakai Shengfong Huang Takuya Mabuchi Kiyoto Kawai Yuya Kurihara Masataka Nakauchi Joji Aochi Chiemi Kokubun Kayoko Konda