## Slide 1
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA
Development of highly sensitive micro magnetic sensor for biomagnetic field measurement using magneto-impedance element
Tsuyoshi Uchiyama
1Graduate school of Engineering, Nagoya University, Nagoya, Japan , tutiyama@nuee.nagoya-u.ac.jp

## Slide 2: Domain Structure of Amorphous Wire and Current Magnetization Utilizing the Skin Effect
Hex
ω ： Angular frequency of a current
μ ： Maximum differential permeability along
the circumferential direction
ρ ： Electric resistivity （１３０μΩ‐ｃｍ）
Hex： Applied dc magnetic field
a
I(w)
outer shell
intermediate
μ
domain wall
Ks
Ki
V
inner core
Kc
Skin effect
k = (1-j) /δ
Skin depth
Magnetoimpedance (MI ) effect
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA
Notes: まず、磁気インピーダンス効果について説明します。
アモルファスワイヤに高周波電流を通電させ表皮効果を生じさせたとき、
ワイヤ円周方向最大微分透磁率μが外部磁界で変化するため、表皮深さδも変化します。
アモルファスワイヤのインピーダンスZは、ベッセル関数を用いてこのように表されます。そして表皮効果が起こっていないときは、このように表され、一定となります。
表皮効果が顕著な場合には、このようになり、最大微分透磁率μが磁界で変化するため、インピーダンスZもルートμに比例して変化します。
これをMI効果といいます。

## Slide 3
Chart: 
| -225.99999999999997 | -188 | -150 | -113 | -95 | -75 | -56.000000000000007 | -37 | 0 | 37 | 56.000000000000007 | 75 | 95 | 113 | 150 | 188 | 225.99999999999997
20MHz | 93.1533 | 97.9995 | 103.335 | 109.163 | 111.701 | 113.685 | 113.003 | 105.978 | 85.8887 | 113.526 | 116.468 | 114.565 | 111.322 | 108.419 | 102.142 | 96.8672 | 92.0064
40MHz | 124.172 | 128.224 | 131.365 | 131.422 | 129.974 | 126.598 | 118.425 | 104.525 | 85.9998 | 126.839 | 135.602 | 138.678 | 139.303 | 138.865 | 135.124 | 130.208 | 124.965
60MHz | 145.618 | 148.427 | 148.07 | 142.152 | 136.03 | 125.136 | 109.63 | 89.5738 | 75.1914 | 120.056 | 139.903 | 150.341 | 155.912 | 157.879 | 157.387 | 153.82 | 149.317
80MHz | 162.799 | 165.782 | 166.118 | 161.416 | 155.53 | 144.386 | 127.566 | 105.312 | 87.5436 | 136.68 | 156.834 | 167.122 | 172.708 | 174.443 | 173.733 | 170.285 | 165.863
Magnetoimpedance Characteristics
of Amorphous Wire
CoFeSiB (L=10mm,30 mm diameter)
Z (Ω）
m0Hex (mT)
ΔZ/Z0
Z0
is more
than100%
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 4
Off diagonal impedance
Impedance
Magnetic Field Response of MI Element
Off diagonal component
a: radius of the wire
n: number of turns per unit length
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 5
PREVIOUS WORK
( Micro Magnetic wire ＆ OFF diagonal MI sensor)
・ S. Gudoshnikov, N. Usov, A. Nozdrin, M. Ipatov, A. Zhukov and V Zhukova, “Highly sensitive magnetometer based on the off-diagonal GMI effect in Co-rich glass-coated microwire,” Phys. Status Solidi A, DOI 10.1002/pssa.201300717 , 2014.
・B.Dufay, S. Saez, C. P. Dolabdjian, A. Yelon, and D.Menard,” Characterization of an Optimized Off-Diagonal GMI-Based Magnetometer,” IEEE Sensors Journal, vol. 13, No. 1, pp. 379- 388, 2013.
・T. Uchiyama, S. Nakayama, K. Mohri, and K. Bushida, “Biomagnetic field detection using very high sensitivity magneto-impedance sensors for medical applications, ”Phys. Status Solidi A 206, No.4, pp.639-643, 2009.
・ V. Zhukova, M. Ipatov and A Zhukov, “Thin Magnetically Soft Wires for Magnetic Microsensors,” Sensors 9, 2009.
・S. Sandacci, D. Makhnovskiy, L. Panina, K. Mohri, and Y. Honkura, “Off-diagonal impedance in amorphous wires and its application to linear magnetic sensors,” IEEE Trans. Magn., vol. 40, no. 6, pp. 18–23, 2008.
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 6
CMOS Circuit for MI Sensor
Pulse generation circuit
(CMOS multi-vibrator)
Signal processing circuit
MI element with pick-up coil
（Amorphous wire）
Vdd
Vdd
E-out (Hex)
ＡＳ
Hex
K. Mohri, Y. Honkura, Amorphous Wire and CMOS IC Based Magneto-Impedance Sensors – Origin, Topics, and Future, SENSOR LETTERS, Vol.5, pp.267-270, 2007.
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 7
Eout
Magnetic Field Detection Characteristics
of CMOS MI Sensor
Almost no hysteresis : It seems that single like domain structure is realized
due to dc component (total amount ) of pulse current passing through the a- wire.
Sensitivity
70kV/T
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 8
Ultra Low Intrinsic Noise
It has been pointed out that magnetic field noise spectral density of the MI element within a simplified model for single domain structure is expressed as
L .G. C. Melo, D. Menard, A. Yelon, L. Ding, S. Saez, and C. Dolabdjian, “Optimization of the magnetic noise and sensitivity of giant magnetoimpedance sensors”, J. Appl. Phys. vol. 103, pp. 033903-1-03303-6, 2008.
T : the temperature
a : the magnetic damping constant
kB : is Boltzman constant
g : gyro magnetic ratio
M0 : saturation magnetization
a : diameter
l : length of a wire element
Intrinsic magnetic noise is approximately 10 fT for 1cm Co- rich amorphous wire at room temperature.
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 9: Magnetic Field and Magnetic Sensors
10-8
10-4
1
104
10-10
10-6
10-2
102
106
pT
nT
μT
mT
T
Bio magnetic
field
Nature magnetic
field
Industrial magnetic field
μG
mG
G
nG
kG
SC-magnet
Hall sensor
ＭＲ、ＧＭＲ sensor
Commercial Fluxgate sensor
Amorphous wire MI sensor (in developing)
SQUID
Proton magnetometer
（0 ~ 0.01Ｈｚ）
kT
(0 ~ 1 MHz)
(0 ~ 10 MHz)
(0 ~ 10 kHz)
(0 ~ 10 kHz)
MG
Geo-magnetisms
Storage and magnet
Intrinsic noise level
at room temperature.
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 10
Magnetic noise
around 1nT
(1Hz - 30Hz)
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 11
Sensing
Reference
PG
d/dt
AS
AS
V1
V2
+
-
PG : Pulse generator
AS : Analogue switch
Vout
Sensing
Reference
Prototype Biomagnetic Field Measurement System
MI sensor head
(First order gradiometer)
This sensor element was supplied by Aichi Steel Corp..
ΔB
∝ΔB
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA
Notes: センサヘッドは二つのMI素子が含まれる。素子間の距離は3センチです。前のは計測用、脳波と環境ノイズを検出します。後ろのは参照用、環境ノイズだけ検出します。この二つの素子の電圧差を出力します。
センサヘッドのアモルファスワイヤは高周波数パルス電流の状態で動作するので、計測回路は主にパルス電流を作ります。
フィルタ回路は電源ノイズと高周波数ノイズを除去します。

## Slide 12
修士期間の研究内容
Environmental Magnetic Field in Our Lab
Chart: 
B( T/Hz1/2)
f (Hz)
Bn
⊿B
40
Bn: Environmental field
⊿B: Gradiometer output
Measurement frequency range
Influence of environmental
magnetic field noise as small
as 10 pT in the measurement
frequency range.
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 13
electrode
MI sensor
Stomach musculature
(5mm square）
Cell tissue
( isolated from guinea pig)
MI sensor (magnetic measurement)
Ag-AgCl electrode
Outer solution
(circulating)
Temperature control 32～34℃
Measurement of Biomagnetic Field
from Living Tissue
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 14
0
0.04
0.10
0.14
Frequency (Hz)
0
1.0
Ex
MI
Power spectrum
10s
500pT
100μV
Voltage
Magnetic
Ex Interval (s)
11
12
13
14
11
12
13
14
MI Interval (s)
Interval of spike
It is known that regular electrical wave is observed
in stomach musculature (after isolated)
Measurement results； Biomagnteic
field from living tissue sample
Fundamental frequency corresponds with each other.
The time interval of the spike has correlation y=x (R=0.93).
Analysis
Intensity ratio (-)
by Shinsuke Nakayama
Graduate school of medicine
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 15
5s
500μV
500pT
Voltage
Magnetic
Simultaneously measurement electrical and magnetic activity
after Tetraethylammonium (TEA) application.
Biomagnteic measurement from different kinds of living tissue
Taenia caeci
Mouse heart
by Shinsuke Nakayama
Graduate school of medicine
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 16
MI sensor
Pair head
~ 8 mm
Wooden bed
Body surface
Table
MCG Measurement
Pit of the stomach
Right
Left
Ten times averaged data
Left
Right
40 mm
(Magnetic cardiography)
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 17
Body
Coil
Top of Head
< 5mm
Sensor is installed
in the shield case
to avoid influence
of magnetic noise
Shield case
Open hole
ＭＩ
ECG
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 18
Event-Related Potential
An event-related potential (ERP) is the measured brain response that is the direct result of a specific sensory, cognitive, or motor event. More formally, it is any stereotyped electrophysiological response to a stimulus.
We challenged to measure event-related magnetic field
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 19
N100 (N1) Experiment ： Method
Audio stimuli ： f = 1000 Hz
Duration 200 ms
Interval 800ms-1400ms
(random)
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 20
修士期間の研究内容
100 times averaged data (Three times repeat experiment)
Time[msec]
Time[msec]
Sensor-output[pT]
Sensor-output[pT]
N100 Experiment ： Result
Opposite side of audio source
(right side)
Same side of audio source
(left side)
N100
N100
Noise level
≒１ｐＴ
Because
of 100 times
averaging.
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 21
Discussions
MI
~ 1.5cm
~ 1.0 cm
Magnetoencephalography : MEG
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 22
~100 fT for Z = 60 mm
~10 pT for Z = 15mm
Q = 50nA・m
Dipole Current Model with Return Current
(SQUID)
(MI)
Parameter : D = 20mm
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 23
We carried out biomagnetic field measurement from living cell tissue using developed precise gradiometer. We have detected magnetic field synchronized with electric potentials at the surface of stomach tissue isolated from guinea pig.
In addition, magnetic field from mouse heart with rhythmical activity can be detected using developed gradiometer system.
We have also tried to measure biomagnetic field from the heart and brain of the human. Cardiac magnetic field which corresponds to MCG was identified (ten times averaging data). The signal strength of N100 evoked magnetic field measured by MI sensor is compared with the strength measured by SQUID.
Summary
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA

## Slide 24
Thank you for your attentions !
Material Science &
Engineering,
September 14-15,
2015, Orlando, USA