## Slide 1: DEVELOPMENT OF NANOCOMPOSITES FOR BIOMEDICAL APPLICATIONS
V. RAJENDRAN
R. Suriyaprabha, S. Sutha, K. Kavitha and M. Prabhu
PROFESSOR AND DIRECTOR
R & D and
CENTRE FOR NANO SCIENCE AND TECHNOLOGY
K. S. Rangasamy College of Technology
K S R Group of Institutions Tiruchengode - 639 209, Namakkal (Dt.) Tamil Nadu, India
Phone Fax Email
: 91- 4288 – 274880 (Direct) 274741- 44
: 91- 4288 – 274870 (Direct) 274860
: veerajendran@gmail.com

## Slide 2
K.S.R Group of Institutions
K.S.R. Kalvi Nagar, Tiruchengode-637215 Tamil Nadu
Birds Eye view - KSR Group of Institutions
Site Map
•
•
•
•
•
•
•
•
K.S. Rangasamy College of Technology (Autonomous) •
K.S.R. Institute of Dental Science and Research •
K.S.R. College of Engineering (Autonomous) •
K.S.R. Institute for Engineering and Technology •
K.S. Rangasamy College of Arts & Science (Autonomous) •
K.S. Rangasamy institute of Technology •
K.S.R. Polytechnic College •
K.S.R. College of Arts & Science for Women •
K.S.R. College of Education
K.S.R. Matriculation Higher Secondary School
K.S.R. Industrial Training School Rajammal Rangasamy I.T.I
Rajammal Rangasamy Teacher Training Institute Rajammal Rangasamy Higher Secondary School Avvai K.S.R. Matriculation School
K.S.R. Akshara Academy
Dr. K. S. Rangasamy, Chairman Mr. R. Srinivasan, Secretary

## Slide 3: APPLICATIONS

## Slide 4: CENTRE FOR NANOSCIENCE AND TECHNOLOGY
TiO2 Nanoparticles
Ilmenite Ore Quartz Sand
SiO2 Nanoparticles
Rice Husk
Bauxite
Al2O3 Nanoparticles
SiO2 Nanoparticles
Spray Pyrolyser Indigenous Furnace
Centre expertise - Mass production of metal oxide nanoparticles
SiO2, TiO2, Al2O3, ZrO2, MgO
Nano Si

## Slide 5: NANOCOMPISTES FOR BIOMEDICAL APPLICATIONS
Nanometal oxide composite
TiO2-Chitosan
Optimisation –with in 5 different concentrations
Nanobioactive Glass (NBG)
NBG with MgO
NBG with Ag2O
Nano Hydroxyapatite
HAp with Si –Coating with chitosan

## Slide 6: NANOBIOMATERIALS APPLICATIONS
NANO BIOMATERIALS
METALS
CERAMICS
POLYMERS
Tissue engineering
Drug Delivery Devices
Orthopedic screws/fixation
Dental Implants
Bone replacements
Dental Implants
Biosensor and Cosmetic

## Slide 7: BONE REGENERATION & RECONSTRUCTION
Emerging areas
Bone tissue engineering and orthopedics
Objectives
Mimic the natural process to repair
Improve the osseointegration
•
•
Maintain the function of the bone

## Slide 8: METAL OXIDE & POLYMER - NANOCOMPOSITE
METAL IMPLANT
  Bone replacement
Defects-Overcome
  In sufficient biocompatibility
  Less Infection prevention
  Less interactions with tissue
  In sufficient anti-corrosion properties

## Slide 9: in situ PREPARATION OF NANOCOMPOSITES
Isopropyl alcohol
Titanium Isopropoxide
Formation of Gel
Drying at 120 oc - 2h
Nanocomposite powder
Drop by drop addition- Chitosan polymer solution
Vigorous Stirring
Add -Acetyl acetone
Vigorous Stirring for 1h
Under Vigorous Stirring in Controlled Conditions

## Slide 10: CHARACTERISATIONS
XRD
SEM
TEM
XRD- amorphous nature
TEM- particle size
TiA =10.5 nm TiAC=5.23 nm
SEM- TiAC-irregular morphology due to the addition of chitosan
Sample code | Sample Description
TiA | Pure-TiO2
TiAC | TiO2-chitosan
C | Control
TiA
TiAC

## Slide 11: BIOLOGICAL STUDIES
pH - SBF
Bioactivity study - SBF
Anti microbial acitivity in S.aureus
XRD- TiAC- well formed crystalline HAp
• pH – confirms good ion
exchanges – TiAc shows continuous
exchanges of ions
• Zone of inhibition =TiAc 10 mm

## Slide 12: IN VITRO TOXICITY STUDIES
C
TiA TiAC
Cytotoxicity study- in AGS cell line
TiAC- composite
Cell Morphology is good
than the pure TiO2
Cell viability is higher than attachment
K. Kavitha, M. Prabhu, V. Rajendran, P.
Manivasankan, P. Prabu, T. Jayakumar, Optimization of nano-titania and titania-chitosan nanocomposite to enhance biocompatibility, Current Nanoscience, 2013

## Slide 13: OPTIMISATION - in situ SYNTHESIZED TITANIA-
Sample | Concentration of chitosan (g/L) | Crystallite size (nm) | Particle size (nm) | Surface area (m2/gm)
T-C0 | 0 | 3.60 | 10.58 | 208.41
T-C0.12 | 0.125 | 3.58 | 5.98 | 114.24
T-C0.25 | 0.25 | 3.22 | 5.87 | 214.73
T-C0.5 | 0.5 | 3.00 | 5.73 | 244.47
T-C1 | 1 | 2.13 | 5.23 | 265.33
T-C2 | 2 | 2.13 | 4.50 | 237.71
CHITOSAN NANOCOMPOSITE
• TiO2–chitosan nanocomposites with five chitosan ratios
• Synthesised by above in situ method

## Slide 14: OPTIMISATION – in situ SYNTHESIZED TITANIA- CHITOSAN NANOCOMPOSITE
TEM
chitosan
decreases
Particle size
spherical morphology chitosan -increases
T-C0
T-C0.12
T-C0.25
T-C0.5
T-C1
T-C2
TEM
T-C0
T-C0.12
T-C0.25
T-C0.5
T-C1
T-C2
SEM

## Slide 15: OPTIMISATION - in situ SYNTHESIZED TITANIA- CHITOSAN NANOCOMPOSITE
In situ synthesized novel biocompatible titania-chitosan
nanocomposite
HAp formation- well observed in composites
T-C0.5 and T-C10- well crystalline HAp
XRD – Before SBF study
XRD – After SBF study

## Slide 16: OPTIMISATION OF in-situ SYNTHESIZED TITANIA- CHITOSAN NANOCOMPOSITE
In situ synthesized novel biocompatible titania-chitosan
nanocomposite
1415 cm1 corresponds to CO3 - formation of HAp layer
2
chitosan addtion - facilitate well formed HAp
FTIR– Before SBF study
FTIR– After SBF study

## Slide 17: OPTIMISATION OF IN SITU SYNTHESIZED TITANIA- CHITOSAN NANOCOMPOSITE
pH – confirms good ion exchange - progressively from T-C0.25 to T-C2
Cytotoxicity -T-C1 is the optimal concentration for the biomedical application
Ion Exchange –during SBF study
K. Kavitha, S. Sutha, M. Prabhu, V. Rajendran and T. Jayakumar, In situ synthesized novel biocompatible titania–chitosan nanocomposites with high surface area and antibacterial activity
Carbohydrate Polymers 93 (2013) 731– 739
Cytotoxicity– AGS cell line

## Slide 18: IN VIVO STUDIES IN ZEBRAFISH EMBRYOS
Zebrafish - Alternative to animal studies
Rapid screening in a feasible way
for nanotoxicity
and transparent
Econimical
imaging
Easy handling

## Slide 19: in vivo TOXICITY STUDIES
In vivo studies in zebrafish (Danio rerio)
Hatching rate was increasesd50:50
Inactive: 20%
Dead rate: 1 out of 10
48 h
72 h
In vivo Toxicity analysis

## Slide 20: NANO BIOACTIVE GLASS (NBG)
Nanobioactive glass (NBG)
  Non-resorbable biomaterial (<100 nm)
  Interact with biological systems
Ability to bond with bone and soft tissues
Composed of SiO2-CaO-P2O5 with additives (Na2O, TiO2 & ZrO2) and antimicrobial agents (Ag2O, ZnO, MgO)
Additives
Increase bioactivity and biocompatibility
Increase mechanical strength
•
Antimicrobial agents
- Prevent microbial contaminations

## Slide 21: NANOBIOACTIVE GLASS (NBG)
Synthesis methods
Hydrothermal and
Sol-gel
Sonochemical
•
•
Spray pyroliser
Salient features of Nanobioactive glass (NBG)
Biodegradability
Good bioactivity and biocompatibility
Osteoconductivity
•
•
Bone bonding ability and load bearing applications

## Slide 22: NANOBIOACTIVE GLASS (NBG) - SYNTHESIS

## Slide 23: OPTIMISATION OF NANOBIOACTIVE GLASSES
Synthesis of magnesium substituted nanobioactive glass powders with various compositions (58SiO2-(33-x)CaO-9P2O5-xMgO) x= 0, 10 and 20 mol %
various
Synthesis of silver doped nanobioactive glass powders with compositions (58SiO2-(33-x)CaO-9P2O5-xMgO)
x= 0, 0.5, 1, 2 and 3 mol %

## Slide 24: XRD AND FTIR PATTERN OF MgO SUBSTITUTED NBG PARTICLES BEFORE AND AFTER in vitro STUDIES
NANO SILICA
No diffraction peaks
Amorphous nature
Before in vitro
10 % MgO - good formation of HAp
Better bioactivity-10% MgO
After in vitro

## Slide 25: TEM IMAGES OF MgO SUBSTITUTED NBG PARTICLES
0% MgO
10% MgO
Spherical morphology < 50 nm
SAED - amorphous
10% MgO - good spherical morphology - uniform size
20% MgO

## Slide 26: SEM IMAGES OF MgO SUBSTITUTED NBG PARTICLES BEFORE AND AFTER in vitro STUDIES
0% MgO
10% MgO
0% MgO
10% MgO
SEM- Before in vitro
SEM- After in vitro
After in vitro
10% MgO doped glass-higher hydroxyapatite formation
Before in vitro
10% MgO glasses- good spherical
morphology
EDX pattern exhibits 99% purity

## Slide 27: in vitro CYTOTOXICITY OF MgO SUBSTITUTED NBG PARTICLES
In vitro cytotoxicity assay
Human gastric adenocarcinoma cell line
10% MgO glass show better biocompatibility at a concentration of 100 µg ml-1
Antibacterial activity
Staphylococcus aureus and
Escherichia coli
No zone of inhibition for MgO doped glass particles
Publication
M. Prabhu, K. Kavitha, P. Manivasakan, V. Rajendran* and P. Kulandaivelu Ceramics International, 39, 1683-1694 (2013 )

## Slide 28: in vivo TOXICITY STUDIES - ZEBRAFISH EMBRYO (DANIO RERIO)
Control
NBG particles - 100µg/mL
Mg- NBG particles - 100µg/mL
The mortality rate is reduced by 20% in the NBG-treated samples

## Slide 29: XRD PATTERN OF Ag2O DOPED NBG PARTICLES BEFORE AND AFTER in vitro STUDIES
Before in vitro
Ag2O – Well formation of HAp
Better bioactivity - 2 and 3 mol % Ag2O
After in vitro
No diffraction peaks
Amorphous nature

## Slide 30: TEM IMAGES OF Ag2O SUBSTITUTED NBG PARTICLES
0% Ag2O
2% Ag2O
3% Ag2O
Spherical morphology < 50 nm
SAED – Amorphous
2 & 3 mol % Ag2O -good spherical morphology - uniform size

## Slide 31: SEM IMAGES OF Ag2O DOPED NBG PARTICLES BEFORE AND AFTER in vitro STUDIES
2% Ag2O
3% Ag2O
2% Ag2O
3% Ag2O
SEM- Before in vitro
SEM- After in vitro
After in vitro
2 & 3 mol% Ag2O - higher HAp layer formation
Before in vitro
2 & 3 mol% Ag2O glasses- good spherical morphology
EDX - 98% purity

## Slide 32: in vitro CYTOTOXICITY OF Ag2O DOPED NBG PARTICLES
In vitro cytotoxicity assay
Human gastric adenocarcinoma cell line
2 & 3 mol % Ag2O glass show better biocompatibility at a concentration of 100 µg ml-1 with slight toxic
Antibacterial activity
Staphylococcus aureus and
Escherichia coli
Zone of inhibition for Ag2O doped glass particles is around 1.5 mm
Publication
M. Prabhu, K. Kavitha, R. Suriyaprabha P. Manivasakan, V. Rajendran* and P.
Kulandaivelu, Journal of Nanoscience and Nanotechnology, 2013, 13(8), 5327-39.

## Slide 33: HYDROXYAPATITE (HAp)
Salient Features of HAp
Composite of natural bone in nano form
Excellent biocompatibility
Direct chemical bond with hard tissues
Metal Doped Hydroxyapatite
Formation of strong mechanical bond
Improved bioactivity, Enhance osteoblast interaction
Improved bone in-growth
Antimicrobial resistance

## Slide 34: COATING ON IMPLANT
METALLIC IMPLANTS
Metallic implants – Stainless steel, Titanium and its alloys and Cobalt Chromium alloys
STAINLESS STEEL (SS)
High corrosion resistance and wear resistance
Disadvantages - Release of Fe, Cr & Ni shows
Allergic and adverse reaction
Advantages - low cost, high tensile strength
•
•
•
•
Bioactive coating on stainless steel – inhibit the release of Fe, Cr
& Ni ions. Enhance bone in growth

## Slide 35: SEM IMAGE OF Si DOPED HAp/CH COMPOSITE COATING ON 316L SS
0SiHAp/CTS
0.8SiHAp/CTS
0.4SiHAp/CTS
1SiHAp/CTS
1.6SiHAp/CTS
Si -HAp well coated on SS with Chitosan
Increase in Si content -good
adherent coating

## Slide 36: HAp FORMATION - NANOCOMPOSITE COATED 316L SS IN SBF
0SiHAp/CTS
0.8SiHAp/CTS
0.4SiHAp/CTS
1SiHAp/CTS
1.6SiHAp/CTS
White precipitate -HAp
1 wt% Si- HAp on the implant surface

## Slide 37: BIOCORROSION STUDY - 316L SS IN SBF
Corrosion stability -HAp composite increased -Si concentration
1.6 wt% Si concentration - maximum corrosion stability
PUBLICATION
S. Sutha, K. Kavitha, G.Karunakaran, V. Rajendran and T. Jayakumar, In-vitro bioactivity, biocorrosion and antibacterial activity of silicon integrated hydroxyapatite/chitosan composite coating on 316L stainless steel implants. Materials Science and Engineering C.2013.

## Slide 38: OBSERVATIONS
Optimisation - NBG
Compositions of MgO and Ag2O
Bioactivity
Enhanced biocompatibility
Optimisation of TiO2-chitosan nanocomposite
Concentration of Chitosan
Improved specific surface area
Enhanced cytocompatibility
Si doped HAp/chitosan composite coating on 316 L SS
Increased apatite formation
Biocorrosion stability

## Slide 39: NEEM DOPED NBG (58SiO2–33CaO–9P2O5)
Neem
Powder
Klebsiella sp. Gram (-ve)
Bacillus sp. Gram (+ve)
N - Neem doped NBG
C - Base glass
Materials | : | Azadirachtha indica - Nano powder
Composition | : | Nanobioactive glass (Neem-58SiO2–33CaO–9P2O5)
Process method | : | Ball Milling / In situ preparation
C
N
14 mm
C
N
18 mm
Neem (Azadirachtha indica ) Leaves
Neem Doped NBG (58SiO2–33CaO–9P2O5)
Base glass (58SiO2–33CaO–9P2O5)

## Slide 40: Al2O3-ZrO2-NBG (58SiO2–33CAO–9P2O5)- HAp
Nano Zirconia
Composition | : | Al2O3-ZrO2-NBG (58SiO2–33CaO–9P2O5)-HAp
Process method | : | In situ preparation
Nano Alumina
(Al2O3-ZrO2-NBG
(58SiO2–33CaO–9P2O5)-HAp)
Base glass
(58SiO2–33CaO–9P2O5)
Nano Hydroxyapatite
Dental Filling
Technology Transfer

## Slide 41
TOXICOLOGICAL EVALUATION OF BIOMEDICAL
IMPORTANT METAL OXIDE NANOPARTICLES
To study the beneficial and adverse effects of the nano- and micro- metal oxide particles on different biological systems such as bacteria, algae for enhanced applications
The interaction of nanoparticles with the ecosystem and biological system should be studied to avoid the ill-effects on human health
Industrially important metal oxide particles which should be evaluated for their toxicity are: SiO2, Al2O3, ZrO2 and TiO2

## Slide 42
Particles | Nature | Purity | Zeta potential (mV) | Contact angle (°A) | Particle size distribution (mean size) |  | BET Surface area (m2 /g)
 |  |  |  |  | Water | Saline | 
Nano- SiO2 | Amorphous | ≥ 99 % | -25.8 | 54.65 | 50 nm | 70 nm | 361
Bulk- SiO2 | - | ≥ 99 % | -25.6 | 50.31 | - | - | -
Nano- Al2O3 | Cubic | ≥ 99 % | +49 | 35.67 | 58 nm | 68 nm | 190
Bulk- Al2O3 | - | ≥ 99 % | -21.8 | 17.37 | - |  | -
CHARACTERISATION - NANO AND BULK SiO2 AND Al2O3
PARTICLES

## Slide 43: SOIL BACTERIAL POPULATION TREATED WITH NANO AND BULK SiO2 AND Al2O3 PARTICLES
Nano alumina shows significant toxicity towards soil bacteria than bulk
Rather, nano and bulk silica have a higher population than any other groups

## Slide 44: IMPACT OF NANO AND BULK SiO2 AND Al2O3 PARTICLES ON SOIL BACTERIA
Publication
G. Karunakaran, R. Suriyaprabha, P. Manivasakan, R. Yuvakkumar, V. Rajendran, N. Kannan , Current Nanoscience, 9 (6) 2013.

## Slide 45
Particles | Crystalline phase | Purity | Zeta potential | Contact angle | Particle Size Distribution (mean size) |  | BET
 |  | (%) | (mV) | (Å) | Water (nm) | Saline (nm) | (m -1)
Nano ZrO2 | Cubic | ≥ 99 | +11.8 | 73.37 | 39 | 50 | 227
Bulk ZrO2 | - | ≥ 99 | -13.4 | 33.20 | - | - | -
Nano TiO2 | Tetragonal | ≥ 99 | -22.0 | 47.82 | 50 | 65 | 112
Bulk TiO2 | - | ≥ 99 | -22.0 | 23.12 | - | - | -
CHARACTERISATION - NANO AND BULK ZrO2 AND TiO2
PARTICLES

## Slide 46: SOIL BACTERIAL POPULATION TREATED WITH NANO AND BULK ZrO2 AND TiO2 PARTICLES
Nano TiO2 shows decrease in population with an increase in concentration
Both nano and Bulk ZrO2 are not significantly affect the bacterial groups

## Slide 47: IMPACT OF NANO AND BULK ZrO2 AND TiO2 PARTICLES ON SOIL BACTERIA
Publication
G. Karunakaran, R. Suriyaprabha, P. Manivasakan, R. Yuvakkumar, V. Rajendran, N. Kannan, Influence of nano and bulk SiO2 and Al2O3 particles on plant growth promoting rhizobacteria and soil nutrient contents, Current nanoscience 2015.

## Slide 48: IMPACT OF NANO AND BULK SiO2 AND Al2O3 PARTICLES ON GREEN ALGAE
Al2O3 particles reduce algal growth in contrast to SiO2 particles.
Algal cells treated with Al2O3 particles settled down at the bottom of the flask and no growth is observed further.
The intensity of the medium reflects more toxic nature of Al2O3 nanoparticles than their micro counterparts.

## Slide 49: IMPACT OF NANO AND BULK TiO2 AND ZrO2 PARTICLES ON GREEN ALGAE
The OD of the medium increases for ZrO2 particles whereas it decreases for TiO2 particles, compared to that of control.
ZrO2 particles enhance algal growth whereas TiO2 particles suppress the growth.

## Slide 50: BIOMEDICAL IMPORTANT HERBAL NANOPARTICLES

## Slide 51
AZADIRACHTA INDICA LEAVES FOR TEXTIL APPLICATIONS
Medicinal Plant
Azadirachta indica or Neem
Antibiotic agent - bacterial pathogens
Constituents : nimbidin, nimbolide, mahmoodin, margolone, margolonone, isomargolonon

## Slide 52: AZADIRACHTA INDICA – NANOPARTICLE SIZE DISTRIBUTIONS
Trial | 1 : | 30 nm
Trial | 2 : | 32 nm
Trial | 3 : | 34 nm

## Slide 53: UV-VISIBLE SPECTRUM OF AZADIRACHTA INDICA LEAF NANOPARTICLES

## Slide 54: SEM-EDAX IMAGE – NANOPARTILCES COATED FABRICS
Coated Fabric
Un-coated Fabric
After 5th wash
After 10th wash

## Slide 55: ANTIMICROBIAL ASSESSMENT OF THE AZADIRACHTA
Test Organisms | 25 mg/ml | 50 mg/ml | 100 mg/ml
E .coli | 18.61 ± 0.61 | 21.78 ± 1.05 | 23.27 ± 1.66
S.aureus | 20.87 ± 0.66 | 21.91 ± 1.38 | 26.54 ± 1.14
INDICA NANOPARTICLES
Zone of inhibition (mm)
A :25 mg/ml
B : 50 mg/ml
C :100 mg/ml

## Slide 56: ANTIMICROBIAL ASSESSMENT OF THE AZADIRACHTA INDICA
Test Organisms | Chitosan coated fabric | Azadirachta caoted fabric | Control - Uncoated fabric
E .coli | 25.45 ± 0.34 | 31.58 ± 0.36 | -
S.aureus | 26.81 ± 0.97 | 34.00 ± 0.88 | -
NANOPARTICLES COATED FABRICS
Zone of inhibition (mm)
A : uncoated
B : Chitosan
C :nanoparticles

## Slide 57: INFLUENCE NANOPARTICLE SIZE ON ANTIMICROBIAL PROPERTIES OF TRIDAX PROCUMBENS LEAF NANOPARTICLES
Medicinal Plant
Diseases like respiratory and intestinal tract diseases anticoagulant, anticancer, antifungal,
insect repellent applications
Constituents: dexamethasone luteolin, glucoluteolin, β-sitosterol quercetin, procumbenetin β-sitosterol-3-O-β-D-xylopyranoside,

## Slide 58: HERBAL NANOPARTICLES – DIFFERENT SIZES
Trial 1 : 6
Trial 2 : 9 h
Trial
Trial
3 :12 h
4 : 15 h

## Slide 59: ANTIBACTERIAL STUDIES
A :6 h
B : 9 h
C :12 h
D: 15 h

## Slide 60: PI AND TEAM @ CNST, KSRCT
Completed Projects
Total No. of Projects Completed
: 20
Total Cost of the Completed Projects
DST (4), DRDO (7), IGCAR (2), BRNS (2), INMAS (1), DESIDOC (1),
UGC (1), UGC-DAE CSR (1), CSIR (1)
: 325.37 (in lakhs)
PI: 17; CI: 3
Human Recourses
Total No. of Ph. D., Produced : 23 Total No. of Technical Staff Trained : 08 Total No. of Patents : 14
: 204
Total No. of Papers Published in Peer reviewed International Journals
On Going Projects
Total No. of Projects on Going : 2 (PI: 2)
DST -1 (2015-2018), BRNS -1 (2014-2017)
Total Cost of the on going Projects
: 48.94 (in lakhs)
Conferences Organised
NANO-15, NANO-10, NANO-5, MAM-12
Nobel laureate Association
Six Nobel laureates Visited CNST, KSRCT

## Slide 61: FACULTY
Dr. K. Saminathan
Fuel cell nanotecnology
Alternative nano energy storage
Nano sensors
Dr. P. Prabu
Nanoscale biostructures
Nano medicine
Dr. P. Manivasakan
Nanostructured surface protective coating
Solid State Chemistry of Nanomaterials
00
Mr. P. Paramasivam
Ultrasonics characterisation of nanomaterials
Dr. V. RAJENDRAN
DIRECTOR, R&D
CENTRE FOR NANOSCIENCE AND TECHNOLOGY
Nanoscale metal oxides
Ultrasonics characterisation of nanomaterials
Nanocomposite refractories
Nano biomaterials
Nano magnetic materials
Dr. R Suriyaprabha
UGC- Post-Doctoral Fellow Nanobiotechnology – Agriculture Environmental Toxicology

## Slide 62: RESEARCH SCHOLARS
Mr. S. Karthik Herbal Nanoparticles |  | Mr. Prem Ranjan Rauta Nano Metal Oxides Refractory Applications
Mr. M. Sridharpanday Metals Metal Oxides Ceramics and Solar cell |  | Mrs. V.S. Sangeetha Graphene Nanocomposites
Mr. P. Siva Supercapacitors Nano Metal Oxides |  | Mr. M. Vinoth Nano Photonics Solar Cell

## Slide 63: INTERNATIONAL SCIENTISTS / RESEARCH SCHOLARS / STUDENTS VISITS / EXCHANGE @ CNST
 | Category | Name & Affiliation
 | Adjunct Professor | Prof. Suresh Valiyaveettil National University of Singapore, Singapore
 | Visiting Professor | Prof. Dr. Karan V.I.S. Kaler University of Calgary, Canada
 | Category | Name & Affiliation
 | Student Internship | Mr. Clement BESSON University of Auvergne, France
 | Visiting Doctoral Researcher | Mr. Victor Ochigbo National Research Institute of Chemical Technology, Nigeria
 | NAM-S & T Research Training Fellowship for Developing Countries (RTF-DCS) | Mr. Zongo Sidiki University of South Africa, Pretoria
 | NAM-S & T Research Training Fellowship for Developing Countries (RTF-DCS) | Dr. M. Abdoulaye Diallo University of South Africa, South Africa

## Slide 64
 | Category | Name & Affiliation
 | Student Internship | Ms. Emeline Moulin University of Auvergne, France
 | NAM-S & T Research Training Fellowship for Developing Countries (RTF-DCS) | Dr. Ntevhe Thovhogi, Post Doctoral Researcher, National Research Foundation/ iThemba LABS, South Africa
INTERNATIONAL SCIENTISTS / RESEARCH SCHOLARS / STUDENTS
VISITS / EXCHANGE @ CNST

## Slide 65: RESEARCH HIGHLIGHTS OF CNST
Highest downloaded articles in Science Direct journals
S.No. | Articles | Downloads
1. | G. Karunakaran et al., Ecotoxicology and Environmental Safety, 93, 191-197. | 554
2. | S. Sutha et al., Mater Sci Eng C Mater Biol Appl., 33, 4046-4054. | 696
3. | K. Jothi Ramalingam et al., Synthetic metals. 191, 113-119. | 574
Most reviewed Manuscript by 19 Reviewers
D. Shanmugapriya, R. Suriyaprabha, R. Yuvakkumar & V. Rajendran. (2014) Chitosan Nanoparticle- incorporated Composite HPMC Films For Food Preservation. J Nanopart Res., 16, 2248.
Highlight of our Research in Magazines

## Slide 66: MEMORANDUM OF UNDERSTANDING
•
University of Aveiro, Portugal
•
Edith Cowan University, Perth, Australia
•
Mintek Inc, Johannesburg, South Africa
•
Chonbuk National University, Jeonju, South Korea
•
University of Missouri, Columbia, USA
•
Kaiserslautern University, Kaiserslautern, Germany
•
Gwangju Institute of Science and Technology (GIST), Korea
•
National Institute for Nanotechnology (NINT) Innovation Centre, Canada
•
York University, Toronto, Canada
•
University of Calgary, Canada
•
Jomo Kenyatta University of Agriculture, Nairobi, Kenya

## Slide 67: MEMORANDUM OF UNDERSTANDING
Mahidol University, Bangkok, Thailand
University of Saskatchewan, Saskatoon, Canada
Centre of Molecular and Macromolecular Studies, (Polish Academy of Sciences) Warsaw, Poland
University of Witwatersrand Johannesburg, South Africa
University of Mauritius (UM), Mauritius
Institut Català de Nanociència i Nanotecnologia, Spain
Université d'Auvergne France

## Slide 68: THANK YOU