## Slide 1
Fabrication and characterization of Magnesium/Hydroxyapatite (HA) nanocomposites for biomedical applications
Yan Huang
Institute of Materials and Manufacturing
Brunel University London, UK
Thanks to:
EPSRC and The Royal Society for financial support
Dr Mehdi Razavi, Mr Junyi Li, Dr Li Zhou and Dr Mingxu Xia for collecting experimental results

## Slide 2
  Biocompatible
  Bioresorbable
  Mechanically compatible
  Promising candidate for degradable orthopaedic and cardiovascular implants
  – less complications and no revisit surgeries.
Mg for implantation
Mg2++ 2H2O = Mg(OH)2 + H2↑

MgCl2  dissolve
Mg = Mg2+ + 2e (Anodic reaction)
2H2O + 2e2- = H2 + 2OH- (Cathodic reaction)
(Total reaction)
In body fluid:

## Slide 3
    In vivo corrosion too fast:
      Loss of integrity before healing completion
      Harmful hydrogen accumulation
    Over dosage of potentially toxic alloying elements
    Inadequate toughness in pure state.
Problems

## Slide 4
Degradation control - why HA?
  Hydroxyapatite (HA) Ca10(PO4)6(OH)2 is a natural bone constituent.
  In physiological environment, excessive OH− due to Mg(OH)2 dissolution can result in reaction:
  10Ca2++ 6PO43− + 2OH−= Ca10(PO4)6(OH)2
    HA becomes more stable with increasing pH value (>>7.4)
  HA- non-resorbable
  forming a protection barrier on Mg surface

## Slide 5
    Natural HA flakes are coarse and porous; yet pH ~7.4 should be maintained in surgeries and HA formation is practically limited – insufficient and ineffective in degradation control
    Adding nano-HA has several benefits:
      Promote uniform HA nucleation and the formation of an evenly distributed HA layer in the Mg surface
      Intensify the protection layer by the gradual deposition of the HA particles upon corrosion
      Strengthening the material
    Alloying and coating are not sufficient.
Degradation control - why HA?

## Slide 6
A key problem for particulate MMC fabrication is particle agglomeration, resulting in poor bonding, heterogeneous microstructures and inadequate properties.
Powder metallurgy cannot overcome the problem.
Technical challenge

## Slide 7
Fabrication - a novel approach for fabricating biodegradable Mg/HA nanocomposites:
  High shear solidification + ECAE/extrusion
Characterization – microstructure, mechanical and electrochemical properties, in vitro performance.
Present work

## Slide 8
Matrix alloy:
  Commercial pure Mg-3Zn-0.5Zr
  High purity Mg-2Zn-0.1Mn-0.5Ca
  High purity Mg-2Zn-0.2Mn-0.5Ca
  High purity Mg-4Zn-0.2Mn-0.5Ca
  High purity Mg-0.5Ca
Reinforcing HA particles:
  Spherical, 20-50nm in diameter
  Needle, 20×100nm
Experiments -material

## Slide 9
Experiments -fabrication
Rotor-stator mechanism
Rotor
Stator
Steel
crucible
Melt
Fabrication tech 1: high shear melt treatment
Conditions:
~10k rpm, 660-680oC, 5-10min

## Slide 10
Experiments -fabrication
Conditions:
350oC, 60mm/min
60 ingot  15×15mm bar
60 ingot  3×30mm sheet
Fabrication tech 2: extrusion

## Slide 11
Experiments -fabrication
ECAE-equal channel angular extrusion
Fabrication tech 3: ECAE
ED
P
Billet
True strain per pass: 0.67
ECAE conditions:
Route A, 350oC, 50mm/min graphite lubricated, ~6 passes

## Slide 12
Experiments -fabrication
Heat treatment
Isochronic annealing: 1h @ 300, 350 and 400C
Fabrication routes 1: HSS + Extrusion
Fabrication routes 2: HSS + ECAE
Fabrication routes 3: HSS + Extrusion + ECAE

## Slide 13
Spherical HA
Needle HA
XRD results
Experiments -characterization

## Slide 14
b)
Effect of HA particles and high shear
Matrix alloy –no shear
Mg/5HA
Mechanically mixed but No shear
Mg/5HA
With shear
Experiments -characterization

## Slide 15
Experiments -characterization
Matrix alloy
Mg/1HA
As-cast microstructures
Mg/3HA
Mg/2HA

## Slide 16
Experiments -characterization
Matrix alloy
Mg/1HA
As-cast microstructures
Mg/3HA
Mg/2HA

## Slide 17
100µm
500µm
Experiments -characterization
As-cast microstructures
Mg/10HA
Mg/5HA

## Slide 18
Experiments -characterization
200µm
100µm
50µm
25µm
As-cast HA particles
Mg/5HA

## Slide 19
Experiments -characterization
As-cast HA particles
Mg/5HA
5µm
5µm
1µm
100nm

## Slide 20
6 pass ECAE microstructures
Mg/10HA
Mg/3HA
Mg/1HA
Experiments -characterization

## Slide 21
1µm
100µm
HA particles after 4 pass ECAE
Mg/5HA
Experiments -characterization

## Slide 22
Experiments -characterization
As extrusion microstructures for bars
Matrix alloy
Mg/1HA
Mg/2HA
Mg/3HA

## Slide 23
Experiments -characterization
Bar, 1h@300C
Bar, 1h@350C
Bar, 1h@400C
Microstructures after heat treatment for bars (Mg/3HA)
sheet, as-deformed
Sheet, 1h@350C
Sheet, 1h@400C

## Slide 24
Mg/0HA
Extruded
Modulus = 44GPa
0.2 = 179MPa
Elongation = ~11.5%
Mg/0HA
Extrusion+annealing
1h@350°C
Modulus = 42GPa
0.2 = 88MPa
Elongation = ~27%
Experiments -characterization
Compression tests(STAM standard

## Slide 25
Mg/3HA
Extruded
Modulus = 47GPa
0.2 = 234MPa
Elongation = ~12%
Mg/3HA
Extrusion+annealing
1h@350°C
Modulus = 46GPa
0.2 = 160MPa
Elongation = ~16%
Experiments -characterization
Compression tests(ASTM E9)

## Slide 26
Experiments -characterization
Chart: Log current density (Log A/cm2))
1wt% HA (spherical)
Extruded bar
Chart: Log current density (Log A/cm2))
1wt% HA (spherical)
Bar -annealed at 400C
Polarization tests: SBF (Hank’s solution) @37C, constant pH 7.4

## Slide 27
Processing state | HA content, wt% | Ecorr (V) | Icorr (nA/cm2)
As-cast | 0 | -1.70 ± 0.05 | 17560 ± 7560
Extruded | 0 | -1.54 ± 0.01 | 13900 ± 2600
Annealed 1h@350 °C | 0 | -1.43 ± 0.03 | 7540 ± 1640
As-cast | 1 | -1.51 ± 0.05 | 17852 ± 4844
Extruded | 1 | -1.45 ± 0.01 | 11726 ± 1150
Annealed 1h@400 °C | 1 | -1.45 ± 0.02 | 5101 ± 806
As-cast | 2 | -1.48 ± 0.04 | 15344 ± 1626
Extruded | 2 | -1.45 ± 0.01 | 13000 ± 3188
Annealed 1h@350 °C | 2 | -1.41 ± 0.02 | 29330 ± 1528
As-cast | 3 | -1.48 ± 0.02 | 30741 ± 3748
Extruded | 3 | -1.40 ± 0.02 | 23297 ± 1213
Annealed 1h@350 °C | 3 | -1.39 ± 0.02 | 31274 ± 5924
Polarization tests: SBF (Hank’s solution) @37C, constant pH 7.4
Experiments -characterization

## Slide 28
Chart: Time (h)
| 4 | 24 | 72 | 168 | 264 | 504 | 720
 | 0 | 0 | 0.333 | 1.05 | 2.19 | 8.68 | 13.29
4h
1d
3d
7d
21d
30d
11d
Immersion tests: SBF (Hank’s solution) @37C, constant pH 7.4
Experiments -characterization
Mg/2HA Annealed 1h@350 °C

## Slide 29
Chart: Time (h)
| 4 | 24 | 72 | 168 | 264 | 504 | 720
 | 0 | 0 | 0.18768 | 0.26232 | 0.33432 | 0.702 | 0.78984
Immersion tests: SBF (Hank’s solution) @37C, constant pH 7.4
Experiments -characterization
Mg/2HA Annealed 1h@350 °C

## Slide 30
7d
Immersion tests: 7 days in SBF (Hank’s solution) @37C constant pH 7.4
Experiments -characterization
Processing state | HA content, wt% | Corrosion rate (mg/cm2/day)
Extruded | 0 | 0.43 ± 0.04
Extruded | 1 | 0.28 ± 0.02
Annealed 1h@400 °C | 1 | 0.26 ± 0.05
Extruded | 2 | 0.18 ± 0.07
Annealed 1h@350 °C | 2 | 0.15 ± 0.05
Extruded | 3 | 0.23 ± 0.07
Annealed 1h@350 °C | 3 | 0.21 ± 0.04

## Slide 31
The combined HSS and ECAE is feasible for fabricating Mg-HA nanocomposites with a range of HA weight percentage of up to 10.
HSS results in grain refinement and uniform distribution of HA particles. ECAE further refines microstructure, breaks down HA aggregates and generates an HA dispersion in the Mg matrix.
The fabricated Mg/HA nanocomposites displayed excellent and adjustable mechanical properties.
The nanocomposites displayed also enhanced corrosion resistance.
Conclusions

## Slide 32
Thanks for your attention!