## Slide 1
ON SAMPLE STRUCTURE
FOR FABRICATING MICRO-MATERIAL
BY ELECTROMIGRATION
Yasuhiro KIMURA
6th International Conference and Exhibition on
Materials Science and Engineering
September 12, 17:05-17:20
Young Research Forum
TEL +81-22-795-6898 FAX +81-22-795-6893
kimura@ism.mech.tohoku.ac.jp
Tohoku University
Department of Nanomechanics,
Aoba 6-6-01, Aramaki, Aoba-ku, Sendai 980-8579, Japan
Graduate student
|
Masumi SAKA
|
Professor: Ph.D.
Notes: The new approach is the
Sample structure is shape of micro-wire
ワイヤ創製のサンプルをSampleと言わない．Specimen or setup/device

## Slide 2: Introduction
wire
1
dots
3
particles
2
wall
4
What’re micro/nano-materials?
|
Micro/nano-materials
Properties 5, 6
Mechanical
Electrical
Thermal
etc.
Applications for free-standing materials
3D interconnection
Thermal application
Electrochemical sensor
Microscopy probe
Waveguide
etc.
Morphology
Materials
Metal
Semiconductor
Polymer
etc.
Stability
High aspect-ratio
1. I.R. Musin and M.A. Filler, Nano Lett., 12 (2012) 3363.
2. Z. Li, M. Yoshino and a. Yamanaka, J. Micromech. Microeng., 24 (2014) 045011.
3. X. Dai, G.G. Wildgoose and R.G. Compton, Analyst, 131 (2006) 1241.
4. M.M. Brewster, et al., J. Phys. Chem. Lett., 2 (2011) 1940.
5. J. Sarkar, et al., Bull. Mater. Sci., 30 (2007) 271.
6. R. Dou and B. Derby, Scr. Mater. 59 (2008) 151.
7. S. Steinhauer, et al., Sens. Actuators, B, 186 (2013) 550.
8. M. Motoyama and F.B. Prinz, ACS nano, 8 (2014) 3556.
9. Y. Nagasaki, et al., MRS Commun., 5 (2015) 587.
Fig. 1 Sensor using CuO nanowire7.
Fig. 2 Nanowire probe8.
Fig. 3 Nanowire waveguide9.
Notes: Synthesis
Bottom-up method is the directed growth and elevating ….
Because many applications utilize the surface area
Some reports indicats the characteristics depends on the shape
Typical synthesis technique are VLS as a bottom-up, and template as a top-down methods.

## Slide 3
12. H. Liu, et al., RSC Advances, 6 (2016) 16640.
10. Q. Li, et al., Opt. Express, 20 (2012) 17873.
11. I. Musin and M. Filler, Nano Lett., 12 (2012) 3363.
Motivation
Stability of free-standing micro-materials
|
Mechanism of the irregular structure for metal micro-material is not clear.
Mechanism for Nano-wire is clear11.
Mechanism for micro-wire of polymer have been reported12.
Straight 10
Kink 11
Collapse 12
2 μm
100 μm
400 nm

## Slide 4
Motivation
Bending with time in electromigration technique
|
Bend of Al micro-wire still requires clarification.
Micro-wires bent, kinked and collapsed after growth.
One wire would bend during growth.
50 μm
50 μm
Fig. 8 Micro-wires grown immediately after.
Fig. 9 Micro-wires grown after a while.
Immediately after
After a while (< 5 h @High temp.)

## Slide 5
Aim
The present work
|
Today’s topic
1. Fabrication by electromigration technique
2. Observation
3. Discussion
Target:
Al micro-wires
Electromigration technique
Method:
Scale:
Micrometer
Specimen with 20 wires
Number:
Why?
Investigation of a bending structure of micro-wires

## Slide 6
Electromigration
Atomic diffusion with high-density electron flow
Utilization
Fig. 5 Fabrication of Al thin wire
by EM 15.
Application utilizing electromigration
Micro/nano-wire15
Vacancies 13
Voids
Hillocks
Accumulations 14
Fig. 4 The illustration of the EM principle.
15. M. Saka and R. Nakanishi, Mater. Lett., 60 (2006) 2129.
16. Y. Lu, H. Tohmyoh and M. Saka, J. Phys. D: Appl. Phys., 44 (2011) 045501.
13. A.H. Fischer, A. Abel, M. Lepper, et al., Microelectron. Reliab., 41 (2001) 445.
14. I.A. Blech, J. Appl. Phys., 47 (1976) 1203.
Fig. 6 Fabrication of a micro-belt
by EM 16.
Principle
What’s Electromigration?
|
(EM)
Before
After
Micro/nano-belt16
EM technique is fabrication method

## Slide 7: Fabrication method
Buried structure
|
Schematic illustration
Fig. 7 FE-SEM image of sample: (a) whole image, (b) magnification of a fabrication area,
and (c) magnification of a hole.
a.
b.
c.
b.
e-
Cathode
Anode
c.
Atoms are migrated by electron flows.
Atoms are discharged via a hole.
e-
Notes: Widening planar direction. Simultaneously

## Slide 8: Conclusions
Stability of a structure was investigated.
Time-dependence of varying a shape was observed.
Al micro-wires collapsed with time, due to buckling by gravity.
High temperature and shrinking root induce gravity effect.
Optimum conditions exist to control a shape.
Notes: Demonstration of fabrication of micro-materials using multi-layer is important.
We hope that ….

## Slide 9
Thank you very much
for your kind attention.
Acknowledgements
A part of this work was supported by JSPS KAKENHI Grant-in-Aid for Scientific Research (B) Number 26289001, and Grant-in-Aid for JSPS Fellows Number 15J02134. Also, a part was supported by Tohoku University Institute for International Advanced Research and Education. This work was performed via the Micro/Nano-Machining Research and Education Center of Tohoku University.