## Slide 1
Yibin Xu
National Institute for Materials Science, Japan
Thermal Conductivity of Amorphous Si and Ge Thin Films

## Slide 2
The transport forms of phonons has a great impact on the design of nanostructured thermoelectric materials with reduced thermal conductivity, as well as heat dissipation in electronic and photonic devices.
Thermoelectric devices
Thermal management
Thermal management issue for thin film

## Slide 3
L
z, Cross-Plane
x, In-Plane
Diffuse Phonon Boundary Scattering
Phonon-Phonon Scattering
Ballistic Phonon
Phonon transportation in thin film
r
Phonon-Defect Scattering

## Slide 4
bulk
thin film
Temperature, T
Thermal conductivity, l
Thickness, d
Features of thermal conductivity of thin film
Thermal conductivity, l
Film thickness dependence can be observed when
How is amorphous thin film?
easily synthesized
extreme low thermal conductivity
little knowledge of phonon distribution, transportation, etc.

## Slide 5
[1] Einstein model[1]: heat conduction in amorphous solids is described by a random walk of thermal energy between neighboring atoms vibrating with random phases.
[2] Minimum thermal conductivity model[2]: the minimum thermal conductivity is reached when the distance between collisions of elastic waves equals the wavelength of Debye waves.
Fig. 1 Calculated minimum conductivity at 300 K versus the measured values for amorphous solids[3].
[1] A. Einstein, Ann. Phys. (Leipzig) 35, 679 (1911).
[2] G. A. Slack, in Solid State Physics: Advances in Research and Applications, edited by H. Ehrenreich et al. (Academic, New York, 1979), Vol. 34, p. 1.
[3] D. G. Cahill, S. K. Watson, and R.O. Pohl, Phys. Rev. B 46, 6131 (1992).
Classic models describing heat conduction in amorphous solids
Phonon mean free paths in amorphous solids are several nm.

## Slide 6
Existence of phonons with long mean free path predicted by MD simulation
Effective mean free paths of the vibrational modes of an a-Si in equilibrium MD simulations.
Y. P. He, D. Donadio, and G. Galli, Appl. Phys. Lett. 98, 144101 (2011).

## Slide 7
Purpose of research
Investigate the dependence of thermal conductivity of amorphous Si and Ge films on thickness and deposition conditions, and explore the nature of phonon propagating in amorphous solids.

## Slide 8
Magnetron sputtering
Deposition temperature
25 ℃
300 ℃
500 ℃
600 ℃
Ge(Si) substrate
(single crystal, 0.5 mm)
Si(Ge) thin film (15,100,250 nm)
Au sensing film (150 nm)
Deposition conditions
Synthesis of Si(Ge) thin films

## Slide 9
TEM image of Si and Ge thin film
Ge 300C
Ge 25C
Si 600C

## Slide 10
Ref
T
0
R. Kato, Y. Xu, et. al. , Jpn. J. Appl. Phys, 50, 106602 (2011)
Cross-plane thermal conductivity measurement (FDTR method)
Notes: Enter speaker notes here.

## Slide 11
Thermal resistance of amorphous Si(Ge) films
as a function of thickness and deposition temperature
Si
Ge

## Slide 12
Thermal conductivity of amorphous Si(Ge) film
as a function of thickness and deposition temperature
Si
Ge

## Slide 13
FFT patterns of different area sizes in Ge films
10×10 nm
3×3 nm
2×2 nm
300 ºC
25 ºC

## Slide 14
Conclusion
Thermal conductivity of amorphous Si and Ge films shows thickness dependence. This result proves that long MFP (>100 nm) phonons exist in amorphous Si and Ge.
Thermal conductivity of amorphous Si and Ge films shows dependent on deposition temperature. The nano-scaled structural order is supposed to be the responsible for it.