## Slide 1: Semiconducting SWCNTs: from materials to thin film transistors
Information, data and drawings embodied in this document are strictly confidential and are supplied to the team members of the Printable Electronics Consortium participating in this Project on the understanding that they will be held confidentially and not disclosed to third parties without the prior written consent of the NRC Executive Director responsible for the Printable Electronics Program.
Zhao Li, Patrick R. L. Malenfant, Jianfu Ding, Jacques Lefebvre
Security and Disruptive Technologies Portfolio, National Research
Council Canada, Ottawa, ON, Canada
Nov. 16, 2015, Nanotek San Antonio

## Slide 2: Outline
Single wall carbon nanotubes (SWCNTs)
  Introduction of SWCNTs
  Purification and application
  Our hybrid process: high yield and high purity materials
Fabrication of high performance TFTs with organic SWCNT dispersion
  Substrates surface treatment
  Effect of Polymer/tube ratio
  Multiple soaking process for high density uniform network
Raman microscopy mapping for SWCNTs network purity assessment
  Introduction of the Raman mapping method
  Two samples with different purity

## Slide 3: Structure and electrical properties of SWCNTs
(6,6)
Diverse distribution of chirality and diameter
n-m =3q: metallic; n-m ≠3q: semiconducting
Raw as grown materials contain tubes with sc/m=2/1
Applications:
Metallic: transparent conductor
Semiconductor: TFT

## Slide 4: Purification and Enrichment of SWCNTs
Density Gradient
Ultracentrifugation
Chromatography
Conjugated polymer
extraction
Nat. Nanotechnol., 2006, 1, 60.
Nat. Nanotechnol., 2007, 2, 640.
•
•
•
•
ACS Nano, 2013, 7, 2971
Simple scalable process Low cost
High tube content Organic solvent based

## Slide 5: sc-SWCNTs Enrichment ---- by PFDD Extraction
Raw Plasma CNTs
Enriched CNTs
Nanoscale, 2014, 6, 2328
2000
0.0
0.4
0.8
M
11
S33
Absorbance (a.u.)
Sample
Sediment Raw(x1/20) sc-SWCNT

0.047
0.082
0.406
Filtrate(x1/20) ------
S22
S11
PFDD
400 800 1200 1600
Wavelength (nm)
Single extraction
yield: ~2%
Purity: >99%
0
3000
0
25k
1.2
50k
75k
100k
150
200
250
300
0
100
4k
8k
16k
12k
RBM
M
1000 2000
Wavenumber (cm-1)
Raman intensity (a.u.)
Raw Enriched
1400
1500
800
900
1000
1600 1700Em/nm
Ex/nm
(10,9)

## Slide 6: sc-SWCNTs Enrichment ----Hybrid Processing
+
dispersing
Dispersing
Separating
(2) Mixing
Separating
(1) Adding
SiO2
Conjugated Polymer Extraction
Silica Gel Adsorption
Nanoscale, 2015, 7, 15741

## Slide 7: sc-SWCNTs Enrichment ---- SiO2 Adsorption
Adding SiO2 +
centrifugation
Supernatant (Ex)
Supernatant (Hy)
Sediment (Ad)
For a single extraction
Yield: 10% vs. 2%
Purity: >99%
400
600
800
1800
2000
0.0
0.4
0.8
1.2
Absorbance (a.u.)
1000 1200 1400 1600
Wavelength (nm)
b: PFDD/CNT=8/1
Sample  (%) Ex2 0.356 11.0
Hy2 0.413 10.0
Ad2 0.255 0.72
M11
S
22
100
150
200
250
300
0
200k
400k
600k
Wavenumber (cm-1)
Raman intensity (count)
PFDD/CNT = 8/1 Ex: 785 nm, RBM
Ex2 Hy2 Ad2
b-2
1300
1600
1700
0
200k
400k
600k
G
sc
G

m
Raman intensity (count)
1400 1500
Wavenumber (cm-1)
Ex2 Hy2 Ad2
G+
a-2
PFDD/CNT = 8/1
Ex: 633 nm,
D and G band

## Slide 8: sc-SWCNTs Enrichment by Hybrid Processing---- Commercialized by Raymor NanoIntegris
Patent:
USP 61/867,630.WO 2015024115 A1
IsoSol-S100®:
The highest-ever purity semiconducting carbon nanotube ink that is produced using a simple, cost-effective, truly scalable route,
Award:
Best New Materials Award at IDTechEx’s PE USA 2014.
.

## Slide 9: TFT device fabrication and characterization
For aqueous SWCNT solution, PLL has to be used for adhesion
Nano Lett. 2009, 9, 4285
How to get a high density uniform
network with an organic ink system?
NH2
H N
O
n
PLL
Deposit electrodes

## Slide 10: SWCNT network on SiO2: with or without PLL
With PLL
Without PLL
CSWCNT (mg/L) 2.6
26.4
Clean SiO2 without PLL shows better adhesion to SWCNT/CP organic dispersion, especially at high concentration.

## Slide 11: SWCNT network on SiO2: CP/SWCNTs weight ratio
CP/SWCNTs weight ratio | Solution stability | Adhesion | Network
1:1 | poor | Good | bundles
5:1 | Good | Good | Good
30:1 | Very good | poor | alignment
1:1
30:1
5:1
Choose 5/1 weight ratio in the following study
Organic Electronics, 2015, 26, 15

## Slide 12: SWCNT network on SiO2: concentration and density
SC-SWCNT
SiO2
Gate (Doped Si)
Source
Drain
SWCNT solution (mg/L) | Tube density /μm2 | Mobility cm2/Vs | On/off ratio
1.0 | 3.8 | Under percolation threshold | 
3.0 | 31 | 4.8±1.5 | 7.4x105
9.0 | 68 | 18±1.6 | 1.6x106
27 | 87 | 25±3.8 | 7.3x105
Good control of network density and device performance
5:1
CP:SWCNT

## Slide 13: Network density: higher concentration
CSWCNT = 80 mg/L (5/1 CP/SWCNT), mobility decreased to 10 cm2/Vs
Non-uniform network
Dispersion: gel-like behaviour
Stronger tube-tube interaction
Stacked frame structure

## Slide 14: Network density: multiple layer coating
Soaking, rinsing
annealing
Repeat 3-5 times with 27 mg/L solution

## Slide 15: Multi-layer coating for high density network
On-current distribution of 25 TFTs
covering 5X5 mm2 area: 60±4 µA
Other methods for high density network: Chemical self-assembly
Langmuir-Schaefer assembly
Nat. Nanotechnol. 2012, 7, 787
Nat. Nanotechnol. 2013, 8, 180
55 | 56 | 60 | 58 |  | 58
54 | 56 | 59 | 58 |  | 60
57 | 60 | 53 | 56 |  | 61
64 | 66 | 65 | 63 |  | 60
69 | 64 | 66 | 61 |  | 64

## Slide 16: TFT device performance
Uniform SWCNT network
High purity sc-tubes
• μ= 39 ± 3.7 cm2/Vs
• On/off = 105.0±0.4
2E-9
2E-8
2E-7
2E-6
2E-5
2E-4
0E+0
1E-5
2E-5
3E-5
4E-5
5E-5
6E-5
7E-5
2 4 6 8 10
ISD (A)
-10 -8 -6 -4 -2 0
VG (V)
0E+0
5E-5
1E-4
2E-4
-10
-8
-6
-4
-2
0
ISD (A)
ISD (A)
VSD (V)
VG=-5 V
-4 V
-3 V
-2 V
-1 V
0 V

## Slide 17: SWCNT network: dip-coating without rinsing
CSWCNT=26.5 mg/L, uniform SWCNT network buried in CP matrix (80% wt)
• μ= 35 cm2/Vs, on/off=1.3 x 104
Attractive due to this process is compatible with printing process

## Slide 18: Purity assessment of SWCNT materials
UV absorption spectrum
Qualitative information
Solution samples
Massive device testing
400
600
800
1800
2000
0.0
1.2
Absorbance (a.u.)
1000 1200 1400 1600
Wavelength (nm)
Sample 
Ex2 0.356
Hy2 0.413
Ad2 0.255
(%) 11.0
10.0
0.72
b: PFDD/CNT=8/1
0.8
S
22
M11
0.4
Hard to access instrument
Tedious device fabrication and testing
Nature Nano. 2012, 7, 787

## Slide 19: Raman spectroscopy for SWCNTs
Physics Reports 2005, 409, 47
RBM band: diameter
D band: defects
G band: m or sc

## Slide 20: Kataura plot
514 nm laser:
2.41 eV
E11sc
E22sc
E33
sc
E11m
633 nm laser:
1.96 eV
Plasma or laser tube:
~1.3 nm

## Slide 21: Raman microscopy mapping method
Renishaw inVia confocal Raman microscopy
SEM

## Slide 22: Raman spectra and maps at 514 nm
16 X 16 µm2
Nano Research, 2015, 8, 2179

## Slide 23: Raman spectra and maps at 633 nm
Counted 21 m-tubes
(15, 6)
(16, 4)
(14, 5)

## Slide 24: Two samples with different sc-purity: UV and Raman
UV and regular Raman only give qualitative purity information
0
200
400
600
800
1000
1200
Intensity
1300 1400 1500 1600 1700 1800
Raman Shift (cm-1)
SC1 SC2
0
0.2
0.4
0.6
0.8
1
400
2000
Absorption (a.u.)
800 1200 1600
Wavelength (nm)
SC1
SC2

## Slide 25: Two samples with different sc-purity: Raman G- map
SC1
SC2
 | SC1 | SC2
m-tubes | 135 | 20
m-tube content | 1.0% | 0.2%
sc-purity | 99.0% | 99.8%

## Slide 26: Two samples with different sc-purity: TFT performance
0
5
10
15
20
25
Mobility (cm2/Vs)
SC1SC1
SC1 SC2
2.5 5.0 2.5 5.0
Channel Length (µm)
1E+0
1E+1
1E+2
1E+3
1E+4
1E+5
1E+6
1E+7
1E+8
On/off ratio
SC1 SC2
2.5 5.0 2.5 5.0
Channel Length (µm)

## Slide 27: Conclusion
Conjugated polymer extraction can provide high purity, organic solvent based SWCNT materials. Hybrid process can further improve yield.
High density and uniform SWCNT networks were fabricated on SiO2
surface which shows high TFT performance.
A Raman microscopy mapping method was developed to assess the sc-purity of SWCNT networks.
Thank you, question?