## Slide 1
A study on fluoride removal from aqueous Solutions by using a synthetic aluminum-based adsorbent
Jihane Assaoui, Zineb Hatim, Abdelmoula Kheribech
Chouaïb Doukkali University, Faculty of Science, Biomaterials and Electrochemistry Team, Laboratory “Water and Environment”, El Jadida, Morocco
Jihane Assaoui
Chouaïb Doukkali University
Email: assaoui.j@ucd.ac.ma
Website: www.ucd.ac.ma
Phone: +212(0)523342325
Contact Information
[1] Kaur, B.N. Misra, A. Kohli, Desalination. 139 (2001) 357-365.
[2] Vinati, A., Mahanty, B., Behera, S.K. Applied Clay Science 114, 340-348 (2015)
[3] NF T 90-004: Water quality - Determination of fluoride ion - Potentiometric method, 2002
References
application of adsorption using a synthetic aluminum-based adsorbent for defluoridation of synthetic aqueous solutions was investigated.
The compositional, structural and textural characteristics of the adsorbent were determined using accurate physicochemical and mineralogical characterizations.
The analysis of fluoride ions in the liquid phase was performed using the potentiometric method with a fluoride-specific ion electrode..
Batch adsorption experiments were conducted at room temperature to optimize various operational parameters such as contact time, initial fluoride concentration, adsorbent dose and initial pH solution.
Abstract
Batch Defluoridation Experiments
Kinetic studies
Introduction
The synthetic aluminum-based adsorbent was characterized to determine in one hand, its mineralogical and physicochemical properties, and on the other hand to explore the mechanisms involved in the fluoride adsorption process.
F- concentration was measured by the potentiometric method [3] with a fluoride‑specific ion electrode (WTW F800 Fluoride Combination Electrode) connected to a digital ion analyzer (WTW InoLab pH/Ion 7320).
The batch experiments consisted in analysing the effect of controlling parameters such as contact time, initial F- concentration, adsorbent dose and initial pH solution on F- adsorption onto synthetic aluminum-based adsorbent. All the experiments were conducted at room temperature of 25±2 °C in 500 mL plexiglass reactor.
Methods and Materials
The percentage of F- adsorbed increased with contact time and began to reach equilibrium after 24h.
The maximum defluoridation (84.91%) was obtained for 40 mg L-1and 3 g L-1 of initial F- concentration and adsorbent dose, respectively.
The adsorption of the F- ions on the synthetic adsorbent is thus not dependent on pH.
Kinetic studies revealed that F- adsorption fitted well to pseudo-second-order model, indicating the fluoride adsorption mechanism of aluminum-based adsorbent was of chemisorption type.
Discussion
The contact time of 24h between the adsorbent and the adsorbate was sufficient to achieve equilibrium.
The maximum adsorption capacity was noted to be 43.29 mg g-1, 40 mg L-1 of initial F- concentration, and 3 g L-1 of adsorbent dose.
The experimental data followed pseudo-second-order and fitted well into Langmuir adsorption.
Conclusions
The contamination of wastewater by fluoride ions has been recognized as one of the environmental problems worldwide [1] imposing a serious threat to human health [2].
Aim: evaluation of adsorption capacity of the synthetic aluminum-based adsorbent for fluoride removal from aqueous solutions.
Opportunities: reducing of environmental impact of fluoride, respect of environmental regulation, simple, robust, eco-friendly process and cost-effective method adsorbent.
Results
Modification of this adsorbent by introducing chemicals that aims at developing a low-cost novel adsorbent, presenting a compatible physicochemical properties with fluorine chemistry.
Future Directions
pseudo-first-order kinetic model
pseudo second-order kinetic model
Effect of Adsorbent Dose
Effect of Contact Time
Effect of Initial Fluoride Concentration
Effect of Initial pH Solution
Chart: t (min)
| 0 | 60 | 120 | 210 | 1140 | 1380 | 1440
% | 0 | 12.6 | 24.95 | 47 | 92.5075 | 95.495 | 96.495
Chart: Initial F- concentration (mg L-1)
| 20 | 40 | 80 | 100 | 120 | 160
F- éliminé | 88.95 | 84.905 | 83.8 | 83.32 | 75.0333 | 53.7563
Qe | 8.5529 | 16.3279 | 32.2308 | 40.0577 | 43.2885 | 41.351
Chart: Adsorbent dose (g L-1)
| 1 | 2 | 3 | 4 | 5 | 6
 | 62.375 | 87.2875 | 96.495 | 96.9125 | 97.472 | 97.75
Chart: pH
| 3 | 5 | 7 | 9 | 11
pH | 96.495 | 95.495 | 96.2375 | 96.025 | 96.5025
Chart: t (min)
| 60 | 120 | 210 | 1140 | 1380 | 1440
Log(Qe-Qt) | 1.0487 | 0.97956 | 0.81957 | -0.27354 | -0.87182 | -3
Chart: t (min)
| 60 | 120 | 210 | 1140 | 1380 | 1440
t/Qt | 35.7143 | 36.0721 | 33.5106 | 92.4249 | 108.3826 | 111.9229