Reactive extrusion of Polypropylene-graft–Maleic Anhydride with branched polyethyleneimine as an active packaging material

Authors: Ian P. Kay, Julie M. Goddard

Abstract:

Food waste is a global issue that burdens the world’s economy and its natural resources. Oxidative degradation and microbial growth are two of the most prominent ways food is wasted. Consumer trends towards more clean label foods with fewer preservatives and additives could have an unintended consequence of further reducing product shelf life.  Non-migratory active packaging is a technology that follows the clean label trend while maintaining or improving current shelf life of foods by adding preservative functionality to the packaging material. The active ligands are bonded to the polymer backbone, preventing migration of the preservative into the foodstuff. Here we present the synthesis of a non-migratory active packaging material through the reactive extrusion of the antimicrobial branched polyethyleneimine (PEI) with polypropylene-graft-maleic anhydride (PP-g-MA). The grafting was achieved through a condensation reaction between the primary amines of PEI and the maleic anhydride groups of PP-g-MA. The reaction was confirmed using a colorimetric amine density assay (AO7) and Fourier transform infrared spectroscopy (FTIR). The FTIR data showed a reduction of the maleic anhydride carbonyl peak at 1780 cm-1 and the emergence of the maleimide carbonyl peak at 1702 cm-1. The AO7 amine assay confirmed the reaction through introduction of 7.29 nmol/cm2 primary amine density. Antioxidant activity was confirmed using the ABTS colorimetric assay with .820 nmol Trolox equivalence / cm2 after one hour incubation. These results indicate the condensation reaction was successful during reactive extrusion producing a thermoplastic polymer with antioxidant activity. The reported active packaging material offers industry and consumers another tool for extending the shelf life of foods while addressing clean label market demands. This will help decrease food waste by reducing losses post retail due to oxidative degradation and microbial growth.