Sunset Yellow voltammetric detection with graphene-modified electrodes

Florina Pogacean*, Stela Pruneanu, Valentin Mirel, Maria Coros, Codruta Varodi

National Institute for Research and Development of Isotopic and Molecular Technologies, Donat Street, No. 67-103, RO, 400293, Cluj-Napoca, Romania

Abstract

Graphene-based materials were prepared by exfoliation of graphite rod with pulses of current. After preparation, the materials were used to modify two glassy carbon (GC) electrodes, denoted GC/EGr-1 and GC/EGr-2, respectively. The performances of each electrode toward Sunset Yellow (SY) detection were tested in laboratory solutions (pH 6 PBS) containing increasing concentrations of SY (3×10−7–1×10−4 M). The sensitivities, linear ranges and the limits of detection of the two electrodes were different. Hence, in the case of the electrode covered with graphene prepared in strong acidic solution (GC/EGr-1) the sensitivity was 0.017 A·M−1, the linear range between 6×10−6 and 1×10−4 M, the LOD was 1.8×10−6 M. In contrast, the electrode covered with the material prepared in weak acidic solution (GC/EGr-2) has higher sensitivity (0.021 A·M−1) wider linear range (1×10−6–1×10−4 M) and lower LOD (3×10−7 M).

Keywords— sunset yellow; electrochemical exfoliation; graphene; graphene-modified electrodes;

Professional Biography

Florina Pogacean: her most recent research interests include the development of electrochemical sensors based on nanostructured materials, having significant expertise on fabrication of graphene-modified electrodes, laboratory electrochemical testing methods and data analysis.

E-mail: florina.pogacean@itim-cj.ro

Acknowledgment

This work was supported by a grant of Ministry of Research and Innovation, CNCS-UEFISCDI, project number PN-III-P4-ID-PCCF-2016-0006.