Photograph

Title of the Abstract: Development of new thermosetting oligoimides for use as a matrix for polymer composites

Author Name: Kolesnikov Timofey

Affiliation: Enikolopov Institute of Synthetic Polymeric Materials

University: Moscow State University of Fine Chemical Technologies

Country: Russia

Abstract:

In the previous years the position of PMC (Polymer Matrix Composites), which was already strong, has been highly improved. They are a unique group of materials often applied in the automotive, aerospace, marine and military industry. PCM is much lighter than traditional materials, have good mechanical properties, good corrosion resistance, extremely good formability and damping of mechanical vibrations. In the automotive industry, the relative high specific strength of PMC makes possible the reduction of weight of final elements of car structures. The same tendency is observed as well in the aerospace industry. In this regard, the important task is to find new polymer binders that will be suitable for work in a wide range of temperatures, have good mechanical properties, chemical resistance and high processability of processing.

A series of thermoplastic oligoimides with a propargyl substituent in the side chain was synthesized by the new environmental-friendly method of high-temperature catalytic co-polycondensation in the melt of benzoic acid. High-molecular compounds based on the new monomer - 5- (2-propyn-1-yloxy) benzene-1,3-diamine was observed.

Oligoimides showed good solubility (>20wt% in N-methyl-2-pyrrolidone), wide temperature processing window (>50°C) and also flow well at 220°C. These imide oligomers were successfully converted to cross-linked structures after cross-linking at 300°C. Cross-linked oligomers have a temperature of 5% weight loss >500°C, Tg >200°C and good mechanical properties (Young modulus = 1671MPa). The binders developed in this work have the potential to be used in the transport, military and aerospace industries as a matrix for PCM.

Biography:

Kolesnikov Timofey received his M.S. in chemistry from Moscow State University of Fine Chemical Technologies. In 2019 Timofey began his graduate studies in the laboratory of Professor Kuznetsov A. A. at Enikolopov Institute of Synthetic Polymeric Materials. Currently, Timofey works as junior researcher in the same laboratory.

Research Interests:

Thermal properties, polyimide

References:

Kolesnikov, T. I., et al. "Synthesis and study of the properties of thermoset oligoimides with propargyl fragment." IOP Conference Series: Materials Science and Engineering. Vol. 525. No. 1. p. 012022

Mail Id:

kolesnikov@ispm.ru

Contact Number:

+79652281613

Suggestions of colleagues/Professors/scholars to send invitation (if any)

Suggestions of Sessions in the conference (if any)