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Abstract[footnoteRef:1] [1: ] 

Membrane distillation (MD) is a useful technology for water desalination possible at low temperatures using inexpensive membranes offering high salt rejection. Therefore, in the present study, economically and eco-friendly Saudi red clay, tetraethyl orthosilicate, ammonia, and sodium alginate powder as a binder were used to fabricate a ceramic membrane for membrane distillation using deothermal energy for heating the feed water to 70 oC. The prepared membrane was tested using a vacuum membrane distillation (VMD) process and showed promising permeate flux and salt rejection results. The membrane was characterised by SEM, mechanical testing, contact angle, pore size distribution analysis, and VMD tests were performed using deionised water, magnesium sulphate solution, sodium chloride solutions, and hot raw well water. An average flux of 13.10 kg/(m2∙h) with 98.96% rejection was obtained using raw well water. During continuous well water desalination tests, the membrane exhibited a stable performance for 4 h. The average flux decreased by 16.5% after 10 h, possibly owing to fouling because of salts and suspended solids. The membrane performance was recovered after the saltwater tests by applying a known cleaning procedure.
Keywords: extrusion; membrane distillation; sodium alginate powder; tetraethyl orthosilicate; hot raw well water.
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