Surfactant modified fuller’s earth as adsorbent for removal of fenoxaprop-p-ethyl from water samples; A statistical approach

Mian Muhammad*, 1, Jasmin Shah2, Muhammad Rasul Jan2, Behisht Ara2

1Department of Chemistry, University of Malakand, Khyber Pakhtunkhwa, Pakistan

2Institute of Chemical Sciences, University of Peshawar, Khyber Pakhtunkhwa, Pakistan

Corresponding authors: *mianchem@uom.edu.pk

Abstract-In this study, fuller’s earth modified with sodium dodecylbenzene sulphonic acid was used for adsorptive removal of fenoxaprop-p-ethyl herbicide from water samples and statistical approach was employed to validate the experimental observations. All the adsorption experiments were conducted in batch mode. The effect of solution pH, agitation time, adsorbent dose and initial herbicide concentration were studied. About 98.5% adsorption efficiency was achieved at initial analyte concentration of 1000 mg L-1 at pH 6 within 60 min at adsorbent dose of 0.1 g. The adsorption kinetics were studied and it was observed that pseudo-second-order kinetic model follows the adsorption kinetics with R2=1.00. The isotherm studies show that the adsorption data fit well to the Freundlich isotherms. In statistical evaluation, the individual as well as the interaction effect of various factors on adsorption was investigated and it was observed that concentration, pH and adsorbent dose are the significant factors with p values of 0.0001, 0.004 and 0.006 respectively, while contact time was found statistically insignificant having p value greater than 0.05. The coefficient of determination (R2=0.930) shows that % adsorption is highly dependent on the studied factors and their interactions and under the optimized set of conditions, high absorption capacity of 200.22 mg g-1 was achieved.

Keywords: organo-clay, sodium dodecylbenzene sulphonic acid, fenoxaprop-p-ethyl, adsorption