Reflection loss dependence on length of silicon nanowire-array for photovoltaic devices

Nei-Jan Cheng1, Shang-Chao Hung*2, and Chun-Hao Hsu3

1 Institute of Photonics and Communications, National Kaohsiung University of Applied Sciences, Kaohsiung 807, Taiwan.

2 Department of Information Technology & Communication,

Shih Chien University Kaohsiung Campus, Neimen, Kaohsiung 845, Taiwan.

3 Graduate Institute of Electro-Optical Engineering & Department of Electronic Engineering, National Taiwan University of Science and Technology, Taipei 106, Taiwan.

Abstract

A two-step, metal-assisted, electroless etching technique based on the sputtering of silver particles is described, using phosphorus silicate glass, doping, and screen printing processes to fabricate photovoltaic devices. Si-NW arrays on pyramid surfaces show a low reflectivity of ~1.11%, while the average length of the Si-NW arrays is ~375 nm, with an aspect ratio of ~5.4. Superior photovoltaic characteristics of the PCE (~10.26%) with a Jsc of 28.2 mA/cm2 and a Voc of 540mV are achieved. Power conversion efficiency shows dependence on shunt resistance while the series resistance and the NWs aspect ratio are respectively below 2.41 Ω and 10.

Key words: Si-NW arrays; metal-assisted electroless etching (MAEE); phosphorus silicate glass (PSG); photovoltaic devices