Gas-phase Catalytic Hydrodeoxygenation of Phenolic Compounds Derived from Lignin Pyrolysis for Hydrocarbon Production Using Ni@HZSM-5-γ-Al2O3

Zhiyu Li1, Weiming Yi2, Zhihe Li1, Xiwei Xu1, Enchen Jiang3, Peng Fu3, Chunyan Tian4, Yuchun Zhang1,2

1 School of Agricultural Engineering and Food Science, Shandong University

of Technology, China

2 College of Materials and Energy, South China Agricultural University, China

Abstract:

Global Platform For

Science (Life Science, Medical, Clinical, Pharma), Technology, Engineering &

Management Professionals To Exchange Ideas,

Knowledge And Networking

At 300+ International Conferences

Statement of the Problem: Biomass, as a raw material for future fuels and chemicals, has been put on the agenda to cope with the crisis caused by the increasing depletion of fossil fuels and environmental pollution [1, 2]. The chemical energy contained in biomass can be directly obtained from burning or indirectly obtained by converting it into liquid or gas fuel. The fuel syngas obtained from the gasification of biomass can be burned to generate heat and can be used in engines or turbines to generate electricity. Liquid fuel obtained from biomass pyrolysis or liquefaction can replace traditional fuel oils used in power generation and thermal energy, as well as in the production of fuels and chemicals [3]. Pyrolysis is considered to be an effective method in various biomass utilization technologies, through which high yields of liquid products can be achieved [4]. However, the bio-oil prepared by the pyrolysis of biomass has a high oxygen content and therefore is lacking as a high-quality transportation fuel [5-7]. Our group worked to identify a catalyst that could more efficiently convert biomass pyrolysis oil into high-quality fuel.

Methodology and Theoretical Orientation: An upgraded process was developed to produce high-quality bio-oil or liquid fuel. Currently, hydrodeoxygenation (HDO) is an effective method for upgrading bio-oil to produce high-quality liquid fuels and chemicals because such a process eliminates oxygen and produces a stable product. In this work, the catalyst Ni@HZSM-5-γ-Al2O3 was prepared using an initial impregnation method, and the HDO process was investigated in the gas phase using guaiacol as a model compound. The gas-phase HDO reaction was carried out in a fixed reactor. The flow rate of the model compound was 0.07 g/min, and Ni@HZSM-5-γ-Al2O3 was stored in the middle of the tube. The influence of temperature, hydrogen pressure, flow rate, and WHSV on the HDO of the model compound were studied.

Findings:  First, we found that the catalyst Ni@HZSM-5-γ-Al2O3 exhibited a typical mesoporous structure with a BET surface area of 310.40 m2/g. We then investigated the effects of temperature, pressure, hydrogen flow rate and WHSV on guaiacol HDO activity. And it was determined that the liquid yield, conversion and hydrocarbon content under the optimum conditions were 39.82%, 98.73% and 86.85%, respectively. Based on the above findings, we confirmed that the mixed supported nickel-based catalyst Ni@HZSM-5-γ-Al2O3 has a high efficiency for the removal of oxygen-containing groups in guaiacol.

Conclusion & Significance: Bifunctional catalysts with both an active metal phase and an oxophilic support are the most effective for this HDO process. The metal phase components have the function of dehydrogenation/hydrogenation reactions. In addition, the strong acid sites on the catalysts are favorable for ring-opening or dehydration reactions in HDO.

Biography

Dr. Zhiyu Li has been devoted to the research and development of renewable energy and catalytic conversion of biomass. He received his PhD in Agricultural Bio-Environment and Energy Engineering from South China Agricultural University, under the tutelage of Prof. Enchen Jiang. Currently, Dr. Li is an associate professor at Shandong University of Technology. At the same time, he joined the Qingdao Institute of Bioenergy and Bioprocess Technology, Chinese Academy of Sciences in January 2022 to develop high-value liquid fuels with Professor Li Xuebing. Dr. Zhiyu Li has published nearly 20 SCI papers, one of which has been selected as one of the top 1% ESI highly cited papers in the world (Hydrodeoxygenation of phenols, acids, and ketones as model bio-oil for hydrocarbon fuel over Ni -based catalysts modified by Al, La and Ga).

About Research Topic

Since the first industrial revolution, the world has seen increasing technological advances and improvements in human living standards. However, this has also caused a sharp rise in the global energy demand and climate change, and people are starting to look for good solutions to solve these problems. A fundamental solution to the climate change problemkey. Biomass is the most abundant and least expensive renewable, alternative energy source. The chemical energy contained in biomass can be directly obtained from burning or indirectly obtained by converting it into liquid or gas fuel. The fuel syngas obtained from the gasification of biomass can be burned to generate heat and can be used in engines or turbines to generate electricity. Liquid fuel obtained from biomass pyrolysis or liquefaction can replace traditional fuel oils used in power generation and thermal energy, as well as in the production of fuels and chemicals

About Institution:

The School of Agricultural Engineering and Food Science is one of the schools with the longest history in Shandong University of Technology. The college has a high-level teaching staff led by high-level talents. There are 171 faculty members, including 147 full-time teachers. The full-time teacher doctorate rate is 93.7%. There are 33 professors, 49 associate professors, and 49 doctoral supervisors. The college has a complete talent training system for undergraduates, masters and doctorates. And The college has established close cooperative relations with universities and scientific research institutions in more than ten countries such as the United Kingdom, Spain, and Japan, and established 7 international cooperation platforms such as the Sino-British Intelligent Agriculture Joint Research Center and the International Cooperation Joint Laboratory of Microbial Cell Factory.

References:

- Kwon E E, Kim Y T, Kim H J, Lin K Y A, Kim K H, Lee J, Huber G W. Production of high-octane gasoline via hydrodeoxygenation of sorbitol over palladium-based bimetallic catalysts. J. Environ Manage 2018; 227: 329-334.

- Yao C, Tian H, Hu Z, Yin Y, Chen D, Yan X. Characteristics and kinetics analyses of different genus biomass pyrolysis. Korean J Chem Eng 2018; 35: 511-517.

- Gutierrez A, Kaila R K, Honkela M L,Slioor R, Krause A O I. Hydrodeoxygenation of guaiacol on noble metal catalysts. Catal Today 2009;147(3-4): 239-246.

- Zhang Y, Brown T R, Hu G, Brown R C. Techno-economic analysis of two bio-oil upgrading pathways. Chem Eng J 2013; 225: 895-904.

- Lee J, Ro I, Kim H J, Kim Y T, Kwon E E, Huber G W. Production of renewable C4-C6 monoalcohols from waste biomass-derived carbohydrate via aqueous-phase hydrodeoxygenation over Pt-ReOX/Zr-P. Process Saf Environ 2018; 115: 2-7.

- Kim H, Shafaghat H, Kim J, Kang B S, Jeon J K, Jung S C, Lee I G, Park Y K. Stabilization of bio-oil over a low cost dolomite catalyst. Korean J Chem Eng 2018; 35: 922-925.

- Lee Y, Shafaghat H, Kim J, Jeon J K, Jung S C, Lee I G, Park Y.-K. Upgrading of pyrolysis bio-oil using WO3/ZrO2 and amberlyst catalysts: Evaluation of acid nummber and viscosity. Korean J Chem Eng 2017; 34: 2180-2187.

NOTE: This is a sample abstracts. Conference/Journal name will be changed while publishing respective abstract in supporting journal website.