Interfacial Construction and Multi-scale Structural Evolution in Nanocomposites

Siduo Wu,, Material Science PhD, Peking University Shenzhen Graduate School, China

Abstract (300 word limit)

We first report the construction of hybrid shish-kebab (HSK) superstructure in low-crystallinity elastomer nanocomposites with incorporation of Carbon Nanotube Bundles(CNTBs). With strong interfacial adhesion, the tensile strength of Olefin Block Copolymer(OBC)/CNTBs nanocomposites was tripled from 7.34MPa to 24.11MPa. With in-situ synchrotron small angle X-ray scattering(SAXS) and wide-angle X-ray diffraction(WAXD) as well as in-situ Raman spectra, the multi-scale structural evolution was thoroughly studied. The formation of HSK leads to lower lamellar density, exhibiting remarkably increased long period. Unlike that in neat OBC, the lower density of crystal lamellaes in nanocomposites doesn't dominate the evolution of long range orderness at low strain regions, the long period of nanocomposites exhibit an inversely increasing trend. With addition of CNTBs, the orientation behavior still follows the slip-link theory. With HSK acting as larger but fewer physical junctions, the chain connectivity of the soft and hard segments in OBC chains in nanocomposites is lower than that in neat OBC, it is less necessary for HSK to adjust their orientation status along the stretching direction. Thus the orientation factor of orthorhombic crystals at low strain regions is lower than that of neat OBC. The mesoscopic structural evolution of CNTBs can be directly revealed by the downshift trend of the Raman G’ band of CNTBs in nanocomposites, which reveals the axial deformation of CNTBs. The downshift can reach a maximum of 10.2 cm-1, and the downshift under axial deformation also conform to the slip-link theory and is consistent with the orientation status of HSK superstructure.
Image

Recent Publications (minimum 5)

1. Sheng-Yang Zhou, Ben Niu, Xu-Long Xie, Xu Ji, Gan-Ji Zhong, Benjamin S. Hsiao, and Zhong-Ming Li. (2017) Interfacial Shish-Kebabs Lengthened by Coupling Effect of In Situ Flexible Nanofibrils and Intense Shear Flow: Achieving Hierarchy To Conquer the Conflicts between Strength and Toughness of Polylactide. ACS Applied Materials & Interfaces 9: 10148-10159.

2. Giuseppe Cesare Lama, Pierfrancesco Cerruti, Marino Lavorgna, Cosimo Carfagna, Veronica Ambrogi, and Gennaro Gentile. (2016) Controlled Actuation of a Carbon Nanotube/Epoxy Shape-Memory Liquid Crystalline Elastomer. The Journal of Physical Chemistry C 120: 24417-24426.

3. Jiashu Fan, Qinglong Zhang, Dingding Hu, and Jiachun Feng. (2016) 	Nonreversible Enhanced Crystallization of Olefin Block Copolymer Induced by Preshearing. Industrial & Engineering Chemistry Research 55: 3782-3789.

4. Haoran Yang, Dong Liu, Jianzhu Ju, Jing Li, Zhen Wang, Guanyun Yan, Youxin Ji, Wenhua Zhang, Guangai Sun, and Liangbin Li. (2016) Chain Deformation on the Formation of Shish Nuclei under Extension Flow: An in Situ SANS and SAXS Study. Macromolecules 2016, 49: 9080-9088.

5. Zuo F., Mao Y.M., Li X.W., Burger C., Hsiao B.S. (2011) Effects of Block Architecture on Structure and Mechanical Properties of Olefin Block Copolymers under Uniaxial Deformation. Macromolecules 44:3670.

6.Yu Tian, Caizhen Zhu, Jinghua Gong, Jinghong Ma, Jian Xu. (2015) Transition from shish-kebab to fibrillar crystals during ultra-high hot stretching of ultra-high molecular weight polyethylene fibers: In situ small and wide angle X-ray scattering studies. European Polymer Journal 73: 127-136.

7. Zuo F., Burger C., Chen X.M., Mao Y.M., Hsiao B.S. (2010) An in Situ X-ray Structural Study of Olefin Block and Random Copolymers under Uniaxial Deformation. Macromolecules 2010,43:1922.

Biography (150 word limit)

Dr. Siduo Wu got his PhD. at Sichuan University, majoring material science. Now he is a post-doctor at Peking University Shenzhen Graduate School. His research is mainly focused on interfacial construction, structural evolution, synchrotron techniques and high-performance nanocomposite. He has 10 published papers, and 4 of therm are of first author..

Email: 373970592@qq.com

Notes/Comments: