# Production of Bioplastic by Brazilian bacterium Ralstonia solanacearum

Karine Laste Macagnan, UFPel, Brazil; Mariane Igansi Alves, UFPel, Brazil; Matheus Marques Torres*, UFPel, Brazil; Camila Rios Piecha, UFPel, Brazil; Patrícia Diaz de Oliveira, UFPel, Brazil; Claire Tondo Vendruscolo, UFPel, Brazil; Angelita da Silveira Moreira, UFPel, Brazil *Presenter

### Abstract

### Poly(3-hydroxybutyrate) [P(3HB)] is a biodegradable biopolymer accumulated by some microorganisms as inclusions of polyesters. The cost of production to the P(3HB) can be lower by increasing cellular and polymer concentrations by suitable combinations of nutrients in the culture medium and cheaper raw materials as media components. The purpose of this study was to evaluate the effect of three minerals media with different nitrogen sources (F4 - urea, BEI - yeast extract and MM - ammonium sulfate) and carbon sources (glucose, sucrose) in the P(3HB) production whit Ralstonia solanacearum RS bacterium. The bioprocesses occured in 250 mL Erlenmeyer flasks with 80 mL of mineral medium, containing 40 g.L-1 of carbon source, and 20 mL of inoculum. The incubations occurred at 32 °C with shaking at 250 rpm for 24, 48 and 72 h. Cell growth was evaluated by optical density (OD600nm) and by dry cell weight (DCW) concentration. The DCW and P(3HB) production was determined by gravimetry. P(3HB) recuperation was performed by chemical extraction using chloroform and DCW in the ratio of 40:1 v.m-1. Residual sugars from the cultures was determined by the dinitrosalicylic acid method for reducer sugars. The best results to DCW (5.3 g.L-1) and accumulation of P(3HB) (46.8% or 2.66 g.L-1) were obtained using MM medium with sucrose in 72 h. For the OD600nm, there was no significant difference between 48 and 72 h in MM medium with sucrose or glucose. All cultures presented similar pattern of sugar consumption, with greater variation of the concentration available in the medium in the first 24 h. The lower sugar consumption occurred in F4 medium, which justify the low yields of DCW and OD600nm in this medium. The selected medium for future research is the MM with sucrose, as it presented better results in the analyzes performed. 
Image

Figure 1: Yield of P(3HB) from R. solanacearum culture at the 24, 48 and 72h in the F4, BEI and MM media added with glucose or sucrose.

Recent Publications

- Alves MI, Macagnan KL, Rodrigues AA, Assis DA, Torres, MM, Oliveira PD, Furlan L, Vendruscolo CT, Moreira AS (2017) Poly(3-hydroxybutyrate) – P(3HB): A Review with focus on the production  process. Industrial Biotechnology (in press).

- Torres MM, Alves MI, Macagnan KL, Ratmann CR, Moreira AS., Vendruscolo CT, Oliveira PD. (2017) Micrographical analysis of Poly (3-hydroxybutyrate) after soil degradation test In: Applied Microbiology symposium, São paulo – SP, Brazil.

- Alves M I, Macagnan KL , Rodrigues AA, Torres MM, Oliveira PD, Moreira AS. (2016) Biomass production by Ralstonia solanacearum In bank biorreator under different culture means vising accumulation of  P(3HB). In: XVIII Postgraduate Meeting of the Federal University of Pelotas, 2016, Pelotas - RS. XVIII Postgraduate Meeting of the Federal University of Pelotas.

- Torres MM, Macagnan KL, Alves MI, Dode LB, Kruger YS, Vendruscolo CT, Moreira AS, Oliveira PD. (2016) Exploratory Studies On Poli (3-Hydroxybutyrate) Soil Degradation And Assessment Of Loss Mass Rate. In: XIII Iberoamerican Polymer Congress, 2016, Cancun - Mexico. Proceedings of the XIII Iberoamerican Polymer Congress.

- Macagnan KL, Alves MI, Rodrigues A, Torres MM, Oliveira PD, Furlan L, Moreira AS, Vendruscolo CT. (2016) Complete factorial project to adjust the concentration of pH and sucrose in the inoculous phase of Ralstonia solanacearum for P(3HB) production. In: Latin American Polymer Symposium, 2016, Cancun - Mexico. Proceedings of the Latin American Polymer Symposium.

Biography

Matheus Marques Torres is a student of the sixth semester of bachelor’s degree in biotechnology at the Federal University of Pelotas (UFPel). He’s a scientific initiation student with a scholarship granted by the National Council for Scientific and Technological Development (CNPq). He develops his research activities in the Laboratory of Biopolymers (UFPel) where he works with studies related to the production, characterization and biodegradation of the bioplastic polyhydroxybutyrate [(P(3HB)]

Email: matheus_mmt@hotmail.com