# Comparison of the biostimulating capacity of degradation of Poly(3-hydroxybutyrate) by forage plants and microorganisms in simulated soil

Matheus Marques Torres, UFPel, Brazil; Mariane Igansi Alves, UFPel, Brazil; Karine Laste Macagnan, UFPel, Brazil; Camila Rios Piecha, UFPel, Brazil; Patrícia Diaz de Oliveira, UFPel, Brazil; Claire Tondo Vendruscolo, UFPel, Brazil; Angelita da Silveira Moreira, UFPel, Brazil

### Abstract

### Polyhydroxybutyrate [P(3HB)] is a microbial polyester and possess characteristics adequate to petrochemical plastics substitution as polypropylene. It is completely biodegradable and the speed of degradation depends on environmental characteristics as microbiota, temperature and humidity.So, we measured the degradation rate of P(3HB) synthesized by the bacterium Ralstonia solanacearum RS [P(3HB)RS] in a simulated soil model. The aim of the study was to evaluated the degradation capability effectiveness  of the bacteria Ralstonia solanacearum RS and, Bacillus megaterium CN3, and the bacterial degradation biostimulating capability of the foraging plants Lolium multiflorum (Ryegrass) and Lotus corniculatus (Birdsfoot trefoil). With P(3HB)RS, produced by bacterium Ralstonia solanacearum RS, and commercial P(3HB) Biocycle® (PHB Industrial S.A., Brazil) (control),  films were produced by solubilizing up 1g in 40mL of chloroform for 30min at 58 °C and evaporation in Petry plate to film formation. Samples were cutted, weighed and separated into polyester bags with three samples each and buried in the soil to be removed at intervals of 20, 40, 60, 80 and 100 days.  Trays for plant germination, containing individual cells full with commercial organic soil were used. The soil treatments were: (1) natural soil grown with both plants, (2) natural soil grown with Ryegrass, (3) natural soil grown with Birdsfoot trefoil, (4) natural soil without plants, (5) sterilized soil, (6) sterilized soil inoculated with R. solanacearum, (7) sterilized soil inoculated with B. megaterium, (8) only natural soil. The plants used did not stimulate the biodegradation, but in spite of that, they helped in the fragmentation of the sample. For bacterial treatments, it was possible to affirm that B. megaterium is a more effective polymer degrader. Moreover, we can attest that polymer degradation is more effective in a microbiologically more favorable environment, since the treatment of unsterile soil without plants (trat.8) obtained the highest rate of degradation (100%).

### Image

Figure 1: P (3HB) RS sample from treatment 3 (with inoculum of B. megaterium) at times of 20, 40, 60, 80 and 100 days.

Recent Publications

- Alves MI, Macagnan KL, Rodrigues AA, Assis DA, Torres, MM, Oliveira PD, Furlan L, Vendruscolo CT, Moreira AS (2017) Poly(3-hydroxybutyrate) – P(3HB): A Review with focus on the production  process. Industrial Biotechnology (in press).

- Torres MM, Alves MI, Macagnan KL, Ratmann CR, Moreira AS., Vendruscolo CT, Oliveira PD. (2017) Micrographical analysis of Poly (3-hydroxybutyrate) after soil degradation test In: Applied Microbiology symposium, São paulo – SP, Brazil.

- Alves M I, Macagnan KL , Rodrigues AA, Torres MM, Oliveira PD, Moreira AS. (2016) Biomass production by Ralstonia solanacearum In bank biorreator under different culture means vising accumulation of  P(3HB). In: XVIII Postgraduate Meeting of the Federal University of Pelotas, 2016, Pelotas - RS. XVIII Postgraduate Meeting of the Federal University of Pelotas.

- Torres MM, Macagnan KL, Alves MI, Dode LB, Kruger YS, Vendruscolo CT, Moreira AS, Oliveira PD. (2016) Exploratory Studies On Poli (3-Hydroxybutyrate) Soil Degradation And Assessment Of Loss Mass Rate. In: XIII Iberoamerican Polymer Congress, 2016, Cancun - Mexico. Proceedings of the XIII Iberoamerican Polymer Congress.

- Macagnan KL, Alves MI, Rodrigues A, Torres MM, Oliveira PD, Furlan L, Moreira AS, Vendruscolo CT. (2016) Complete factorial project to adjust the concentration of pH and sucrose in the inoculous phase of Ralstonia solanacearum for P(3HB) production. In: Latin American Polymer Symposium, 2016, Cancun - Mexico. Proceedings of the Latin American Polymer Symposium.

Biography

Matheus Marques Torres is a student of the sixth semester of bachelor’s degree in biotechnology at the Federal University of Pelotas (UFPel). He’s a scientific initiation student with a scholarship granted by the National Council for Scientific and Technological Development (CNPq). He develops his research activities in the Laboratory of Biopolymers (UFPel) where he works with studies related to the production, characterization and biodegradation of the bioplastic polyhydroxybutyrate (P(3HB)

Email: matheus_mmt@hotmail.com