Title: Fuel characteristics of binder free briquettes made at room temperature from blends of oil palm mesocarp fibre and Ceiba pentandra

Stephen Jobson Mitchual1, Patrick Katamani1, Kojo Agyapong Afrifa2

1Department of Construction and Wood Technology Education, University of Education, Winneba, Kumasi Campus, P. O. Box 1277, Kumasi, Ghana

2Department of Wood Science and Technology, Kwame Nkrumah University of Science and Technology, Kumasi, Ghana

Keywords: Ash content: Briquettes, Calorific value, Ceiba pentandra, Elemental composition, Physico-mechanical properties, Oil palm mesocarp fibre, Volatile matter

This study assessed the fuel characteristics of briquettes made from oil palm mesocarp fibre and sawdust of Ceiba pentandra at room temperature, using low compacting pressure without a binder. Properties of briquettes studied included stability in diameter and length, relaxed density, compressive strength, impact resistance index, gross calorific value, volatile matter, ash content and elemental composition. These properties were determined using standard laboratory methods. The results show that briquettes with better relaxed density, compressive strength and impact resistance index could be produced from a blend of C. pentandra sawdust and oil palm mesocarp fibre at low compacting pressure and room temperature without a binder. The relaxed density of briquettes produced ranged from 377 kg/m3 to 586 kg/m3 which could be classified as medium-density briquettes. The result further indicates that compacting pressure 40 MPa or more could be used to produce briquettes with adequate compressive strength in cleft and impact resistance index from the blend of C. pentandra sawdust and oil palm mesocarp fibre at low compacting pressure and room temperature without a binder. At 5% level of significance, the compacting pressure and mixing proportion had significant effect on the physical and mechanical properties of briquettes produced. The gross calorific values of Ceiba pentandra sawdust and oil palm mesocarp fibre were found to be 20.33 MJ/kg and 19.50 MJ/kg respectively. Even though most of the elemental compositions of the oil palm mesocarp fibre were not adequate, a blend with Ceiba pentandra sawdust could make it suitable to be used as an environmental friendly material for biomass briquettes production.

REFERENCES

- OECD/IEA (2014) Africa Energy Outlook - A focus on energy prospects in Sub-saharan Africa. International Energy Agency 9 rue de la Fédération 75739 Paris Cedex 15, France; WEO2014_AfricaEnergyOutlook.pdf

- IEA (2015) Renewables to lead world power market growth to 2020, International Energy Agency. http://www.iea.org/newsroom/news/2015/october/renewables-to-lead-world-power-market-growth-to-2020.html

- EIA (2009) Annual energy outlook with projections to 2030. Energy Information Administration, Washington, DC 20585. http://www.eia.gov/oiaf/aeo.

- Abnisa F, Niya AA. Wan Daud WA, Sahu JN (2013) Bio-oil and bio-char from pyrolysis of palm oil wastes characterization of bio-oil and bio-char from pyrolysis of palm oil wastes. Research Gate 1-12.

- OECD/IEA (2006) Energy for Cooking in Developing Countries, International Energy Agency.

- Furlan Jr. Dendê: manejo e uso dos subprodutos e dos resíduos (2007) Embrapa Amazônia Oriental (Oil palm: management and use of by-products and Waste). Documentos 246, Embrapa Amazônia Oriental, Belém, Brazil.

- Pacheco P, Gnych S, Dermawan A, Komarudin H, Okarda B (2017) The palm oil global value chain: Implications for economic growth and social and environmental sustainability, Working Paper 220. Bogor, Indonesia: CIFOR. DOI: 10.17528/cifor/006405

- Costa AG, Pinheiro GC, Pinheiro FGC, Dos Santos AB, Santaella ST, Leitão RC (2013) Pretreatment strategies to improve anaerobic biodegradability and methane production potential of the palm oil mesocarp fibre. Chemical Engineering Journal 230:158-165.

- Mitchual SJ (2015) Enhancing the physical properties of briquettes from sawdust of Piptadenia africana through combination with Ceiba pentandra. British Journal of Applied Science and Technology 6(4):399-407. DOI: 10.9734/BJAST/2015/12315.

- Mitchual SJ (2013) Densification of sawdust of tropical hardwoods and maize cobs at room temperature using low compacting pressure without a binder. PhD Thesis, School of Graduate Studies, Kwame Nkrumah University of Science and Technology, Kumasi, Ghana.

- Mitchual SJ, Frimpong-Mensah K, Darkwa NA, Akowuah JO (2013) Briquettes from combination of maize cobs and Ceiba pentandra at room temperature and low compacting pressure without a binder, International Journal of Energy and Environmental Engineering, 4(38):7pages. Doi: 10.1186/2251-6832-4-38.

- Mitchual, S. J., Frimpong-Mensah, K., & Darkwa, N. A. (2013). Effect of species, particle size and compacting pressure on relaxed density and compressive strength of fuel briquettes. International Journal of Energy and Environmental Engineering, 4(30), 6 pages. Doi:10.1186/2251-6832-4-30.

- European standard EN 13183–1 (2002) Moisture content of a piece of sawn timber. Determination by oven-dry method, BSI, London.

- ISO: International standard ISO 3131 (1975) Standard test method for density of regular solids. ISO, Geneva.

- ASTM International (2008) Standard test method of compressive strength of wood. ASTM standard D2166-85, West Conshohocken.

- ASTM International (2007) Standard test method of drop shatter test for coal. ASTM standard D440, West Conshohocken.

- ASTM International (2012) ASTM standard E711-87, Standard Test Method for Gross Calorific Value of Refuse-Derived Fuel by the Bomb Calorimeter.. http://ia600806.us.archive.org/23/items/gov.law.astm.e711.1987/astm

- ASTM International (2008) ASTM standard D1102-84, test method for ash in wood. Annual book of ASTM standards, 153-154.

- ASTM International (2008) ASTM standard D3175-11, standard test method for volatile matter  in the analysis sample of coal and coke. Annual book of ASTM standards, 153-154.

- Motsara MR, Roy NR (2008) Guide to Laboratory establishment for plant nutrient analysis. 19th Edition, FAO, Rome, 42-88.

- FAO (2008) FAO Guide to Laboratory Test

- Faizal HM, Latiff ZA, Mazlan AW, Darus AN (2009) Study on characteristics of briquettes contain different mixing ratio of EFB fibre and mesocarp fibre. International meeting on advances in thermo-fluids. Taman Safari, Indonesia. 16-17.

- Lindley J, Vossoughi M (1989) Physical properties of biomass briquettes. Transaction of the ASAE. 32(2):361-366.

- Rahman, ANE, Aziz, MM, Prasad, CSN, Venkatesham, M (1989) Influence of size and shape on the strength of briquettes. Fuel Process Technol. 23:185-195.

- Faizal HM, Latiff ZA, Wahid MA, Darus AN (2010) Physical and combustion characteristics of biomass residues from palm oil mills. New aspects of fluid mechanics, heat transfer and environment. 34-38.

- Tumuluru JS, Wright CT, Kenny KL, Hess R (2011) A review on biomass densification technologies for energy application. U.S. Department of Energy. http://www.inl.aov.

- Kambo HS, Dutta (2014) Strength, storage, and combustion characteristics of densified lignocellulosic biomass produced via torrefaction and hydrothermal carbonization, Appl. Energy 135:182-191.

- Melin S (2011) Quality Certification and Standards for Solid Biofuels, Wood Pellet Association of Canada.

- Demirbas T, Demirbas C (2009) Fuel Properties of Wood Species. Energy Sources 31:1464-1472. http://dx.doi.org/10.1080/15567030802093153

- McKendry P (2002) Energy production from biomass (part 1): Overview of biomass, Bioresource Technology, 83(1), 37–46.

- Hahn B (2004) Existing Guidelines and Quality Assurance for Fuel Pellets—Pellets for Europe Project. UMBERA, Umweltorientierte Betriebsberatungs-, Forschungs- und Entsorgungs-Gesellschaft m.b.H.

- DEPI (2013) ENplus Briquettes, Manual for the Certification of Wood Briquettes, Deutsches Pelletinstitut GmbH (DEPI) Neustädtische Kirchstr. 8 10117 Berlin

- Grover PD, Mishra SK (1996) Biomass Briquetting: Technology and Practice. Regional Wood Energy Development Programme in Asia. Field Document No. 46, Food and Agricultural Organization.

- Akowuah JO, Kemausuor F, Mitchual SJ (2012) Physico-Chemical Characteristics and Market Potential of Sawdust Charcoal Briquettes. International Journal of Energy and Environmental Engineering 3:6p. http://dx.doi.org/10.13031/2013.32359

- Mitchual SJ, Frimpong-Mensah K, Darkwa NA (2014) Evaluation of fuel properties of six tropical hardwood species for briquettes. Journal of Sustainable Bioenergy systems 4(1):1-9. Doi: 10.4236/jsbs.2014.41001

- Jenkins BM, Baxter LL, Miles Jr TR, Miles TR (1998) Combustion properties of biomass. Fuel processing technology 54:17-46 http://dx.doi.org/10.1016/S0378-3820(97)00059-3

- Telmo C, Lousada J, Moreira N (2010) Proximate analysis, backwards stepwise regression between gross calorific value, ultimate and chemical analysis of wood. Bioresource Technology, 101(11):3808-3815.

Biography:

Stephen Jobson Mitchual is an Associate Professor in Wood Science and Technology at the University of Education in Ghana. He holds PhD degree in Wood Science and Technology from the Kwame Nkrumah University of Science and Technology in Ghana. Currently, he is the Dean of the Faculty of Technical Education. He has published more than 24 papers in reputable journals and has been a reviewer for several international journals. He has presented his research findings at various international conferences. He is also an active member of the Society of Wood Science and Technology in the United State of America.

Presenting author’s details

Full Name: Stephen Jobson Mitchual

Contact number: +233 203809967

Session name/number: Biofuels & Biorefinery

Category: Oral presentation