Electrochemical immunosensor based on Manganese oxide nanomaterial for the detection of Aflatoxin B1

Avinash Kumar Singh1,2, Tarun Kumar Dhiman1, GBVS Lakshmi1, Sobhan Sen2 and Pratima R. Solanki1*

1 Special Centre for Nanoscience, Jawaharlal Nehru University (JNU), New Delhi-110067, India

2 School of Physical Sciences, JNU, New Delhi-110067, India

*Corresponding author email: partima@mail.jnu.ac.in; pratimarsolanki@gmail.com

Abstract:

The Aflatoxins (AFB1) are produced mainly by fungi Aspergillus flavus and Aspergillus niger. [1] These toxins mainly affect cereal foods and due to this humans and animals are easily exposed.[2] These have been classified as possible carcinogenic and can also cause liver cancer. Here, manganese oxide nanoparticles (MnO2nps) based electrochemical immunosensor has been proposed for the detection of Aflatoxin-B1. MnO2 nps were synthesized via wet chemical method and further calcined at 450oC and characterized by X- Ray diffraction, Raman spectroscopy, Fourier Transform Infrared spectroscopy, UV- vis absorption, and field effect scanning electron microscopy to study phase, crystallinity, structure, absorption and morphology. Average crystallite size of MnO2nps was observed between 20-30 nm. SEM study confirmed the nps morphology of the material along with average particle size in the range of 40-50 nm. Maximum absorbance of MnO2 was observed around 250 nm. Manganese oxide based MnO2/ITO electrodes were fabricated via drop casting process and further functionalized with antibodies specific to Aflatoxin B1 (anti-AFB1) and non-specific sites were blocked with bovine serum albumin (BSA). Fabricated BSA/anti-AFB1/MnO2/ITO immunoelectrode showed higher sensitivity of (0.032 pg/ml.cm2) for the detection of Aflatoxin-B1. The developed immunosensor showed a linear detection in the range of 0.1pg/mL to 10ng/ml with lower detection of 0.1pg/mL.

Keywords:  Aflatoxin B1, Manganese oxide, Immunoelectrode.

Reference:

[1] U. FDA, Handbook of foodborne pathogenic microorganisms and natural toxins, Bad Bug, (2012).

[2] F. Azri, R. Sukor, J. Selamat, F. Abu Bakar, N. Yusof, R. Hajian, Electrochemical Immunosensor for Detection of Aflatoxin B1 Based on Indirect Competitive ELISA, Toxins, 10(2018) 196.

Biography

Avinash Kumar Singh

Avinash Kumar Singh is currently pursuing his Ph. D. at School of Physical Sciences and Special Center for Nanoscience, Jawaharlal Nehru University. His current   area of research is molecular dynamics and biosensing using various nanomaterials and different techniques. He is currently working in optical, electrochemical and microfluidic nanobiosensors. He has done his M. Sc. in Chemistry from University of Allahabad, Uttar Pradesh. and B. Sc. in chemistry from University of Allahabad, Uttar Pradesh.