The whitening and abrasion effect of bentonite on human tooth enamel

Abstract

Aim: In recent decades, there has been increasing attention towards clays due to their unique properties, as we see them in numerous medical and dental products. Bentonite is an absorbent swelling clay used in many cultures as a natural remedy and has relatively low abrasive properties. This study investigates the whitening effects of bentonite on human tooth enamel.

Materials and Methods: Fifty human tooth specimens were obtained from recently extracted caries-free wisdom teeth, disinfected, polished, and randomly divided into five study groups consisting of bentonite (0.5 and 1.5 and 3 weight percentage), positive control (Close-up Icy White toothpaste) and negative control. A stained film was slowly deposited on specimens using tea and coffee and subsequently removed using a mechanical brushing procedure with toothpaste slurries. The roughness (Ra) and CIELAB colour space () were measured before and after the specimens were submitted to procedures. The data were submitted to one-way ANOVA and Tukey's HSD test (α=0.05).

Results: There were no statistically significant differences in colour alterations after one year equivalent of tooth brushing between five study groups (P>0.05). The positive control group had the most changes in Ra value (P<0.05).

Conclusion: In contrast to previous studies, this study shows that bentonite did not significantly affect teeth whitening. Also, bentonite had relatively low abrasiveness. Further studies seem to be required.

Keywords: Bentonite; Clay; Tooth Abrasion; Tooth Bleaching Agents; Toothpaste

Presenting author details

Full name : Foujan Chitsaz

Mobile Number  / Watsap Number: +989128024496

Linked In account: https://www.linkedin.com/in/foujan-chitsaz-71683b220/

### Session name/ number : International Conference on Dentistry & Oral Health-2021

Category: (Oral presentation/ Poster presentation)

Date of Birth: 3/09/1995

Biography:

I got my DDS from Tehran university of medical sciences, the most prestigious medical university in the nation, Iran, in late 2019, with a flying colour score. I have been working in deprived areas as a full-time dentist while doing academic research since then. I have plenty of articles in the field of cosmetic dentistry which have been in the process of publication in international journals.

Publications:

Foujan Chitsaz, Safoura Ghodsi, Solaleh Amirpour Harehdasht, Bahar Goodarzi, Somayeh Zeighami. Evaluation of the colour and translucency parameter of conventional and Computer-aided design and computer-aided manufacturing (CAD-CAM) feldspathic porcelains after staining and laser-assisted bleaching. The journal of conservative dentistry. Accepted in  2021, September.