Effect of Shade and Light Curing Mode on the Degree of Conversion of Silorane-Based and Methacrylate-Based Resin Composites

Arman  Salehi, Negar  Salehi

Assistant Professor of Rafsanjan University of Medical Sciences, Iran

Statement of Problem: The degree of conversion depends on the material composition, light source properties, distance from light source, light intensity, curing time, and other factors such as shade and translucency.

Objectives: In the present study, we evaluated the effects of different light-curing modes and shades of methacrylate and silorane-based resin composites on the degree of conversion of resin composites (DC).

Materials and Methods: The methacrylate-based (Filtek Z250, 3M, ESPE) and low-shrinkage silorane-based (Filtek P90, 3M, ESPE) resin composites were used in three groups as follows: group 1-Filtek Z250 (shade A3), group 2-Filtek Z250 (shade B2), and group 3-Filtek P90 (shade A3). We used a light-emitting diode (LED) curing unit for photopolymerization. 10 samples were prepared in each group to evaluate the degree of conversion; 5 samples were cured using soft-start curing mode, and the other 5 were cured using standard curing mode. The DC of the resin composites was measured using Fourier Transform Infrared Spectroscopy (FTIR). The data were analyzed using Kruskal Wallis and one-way ANOVA statistical tests.

Results: The degree of conversion of silorane-based resin composite was 70 - 75.8% and that of methacrylate-based resin composites was 60.2 - 68.2% (p = 0.009). The degree of conversion of the composite with brighter colour (B2) was statistically more than the darker composite (A3). Higher degree of conversion was achieved applying the standard curing mode.

Conclusions: The results of the study showed that the colour and type of the resin composite and also the curing mode influence the degree of conversion of resin composites.

References:

1. Randolph LD, Palin WM (2014). Ultra-fast light-curing resin composite with increased conversion and reduced monomer elution. Dental  Materials 30:594-604.

2. Giorgi MC, Hernandes NM (2014). Influence of an intermediary base on the microleakage of simulated class II composite resin restorations. Operative Dentistry 39:301-307.

3. Porto IC, de Aguiar FH (2013). Mechanical and physical properties of silorane and methacrylate based composites. Journal of  Dentistry 41:732-739.

4. Gao BT, Lin H, Zheng G (2012). Comparison between a silorane-based composite and methacrylate-based composites: shrinkage characteristics, thermal properties, gel point and vitrification point. Dent al Matererials  31:76-85.

5. Yoon TH, Lee YK, Lim BS (2002). Degree of polymerization of resin composites by different light sources. J Oral Rehabil 29:1165-1173.

Biography

Arman Salehi obtained his Doctorate of Dental Surgery (DDS) from Kerman Dental School (2007), Iran. He obtained his PhD degree from Department of Operative Dentistry, School of Dentistry, Isfahan University of Medical Sciences, Iran, He is working as an Assistant Professor for the same department, Rafsanjan University of Medical Sciences, Iran. He has around five national and international publications and has attended various conferences. He has his own private practice in Rafsanjan city.

Contact number: 00989133405149
Email: armansalehi1984@gmail.com