AJMAN UNIVERSITY

COLLEGE OF DENTISTRY

EFFECT OF OCCLUSAL STAMP MATERIAL ON THE SURFACE HARDNESS AND ROUGHNESS OF NANOHYBRID COMPOSITE RESIN RESTORATION [IN VITRO STUDY]

AMANY LAHAM

DUAA IMAD AKRAMA

SARA GHORBAN

MAY 2017

TABLE OF CONTENTS

CONTENTS								      Page Number

i. Declaration                                                                     				   3

ii. Acknowledgements		 							   4

iii. Abstract										   5

iv. List of Figures									   6

v. List of Tables									   7

-------------------------------------------------------------------------------------------------------

CHAPTER 1. INTRODUCTION							   8

-------------------------------------------------------------------------------------------------------

CHAPTER 2. LITERATURE REVIEW						  10

- 2.1 COMPOSITE TYPES							  11

- 2.2. OCCLUSAL STAM TECHNIQUE & MATERIALS			  19

- 2.3. SURFACE HARDNESS							  26

- 2.4. SURFACE ROUGHNESS						  29

-------------------------------------------------------------------------------------------------------

CHAPTER 3. METHODOLOGY							  33

- 3.1. MATERIALS								  34

- 3.2. METHODOLOGY							  37

- 3.3. DISCUSSION								  44

-------------------------------------------------------------------------------------------------------

CHAPTER 4. REFERENCES							  46

- 4.1. REFERENCES								  47

- 4.2. APPENDIX [LIST OF TABLES AND FIGURES]

DECLARATION

We declare that this assignment is our own work and that we have correctly acknowledged the work of others. This assignment is in accordance with Ajman University guidance on good academic conduct and integrity.

Amany Laham

Duaa Imad Akrama

Sara Delkhoon Joband

ACKNOWLEDGEMENT

To thank the generous help we received from Mr. Marwan Dia, the Regional Manager of Heraeus Kulzer-Mitsui Chemicals Group [Middle East & Africa] who has helped us get materials that we tested in this study.

To thank Dr. Mazin Hamdi for his support, guidance and constant feedback for the entire literature review throughout the year.

To thank our parents…

To thank the Dean of Dentistry…

ABSTRACT

The aim of the study was to determine the effectiveness of materials commonly used in the occlusal stamp technique on the surfaces of composite. Thirty specimens of a specific nanohybrid composite were evenly organized in groups according to the material that will be placed on top of the discs and then each were polymerized using a specific LED light cure. They were then further tested on the Vickers hardness and the surface roughness using a Vickers microhardness tester and a profilometer respectively. The results revealed that while two of the three materials provided with adequate hardness, the upper surfaces of the discs were very rough compared to the lower surface that had an acceptable Ra value. Therefore, the occlusal stamp technique is not more efficient than the conventional technique.