# Ta2O5-nanoparticle-modified graphite felt as a high-performance electrode for vanadium redox flow battery

Anteneh Wodaje Bayeh, Daniel Manaye Kabtamu, Yu-Chung Chang, Guan-Cheng Chen, Hsueh-Yu Chen, Guan-Yi Lin, Ting-Ruei Liu, Tadele Hunde Wondimu, Kai-Chin Wang and Chen-Hao Wang*

Department of Materials Science and Engineering, National Taiwan University of Science and Technology, 10607, Taipei, Taiwan.

### Abstract

To increase the electrocatalytic activity of graphite felt (GF) electrodes in vanadium redox flow batteries (VRFBs) toward the VO2+/VO2+ redox couple, we prepared stable, high catalytic activity, and uniformly distributed hexagonal Ta2O5 nanoparticles on the surface of GF by varying the Ta2O5 contents. Scanning electron microscopy (SEM) revealed the amount and distribution uniformity of the electrocatalyst on the surface of GF. It was found that the optimum amount and uniformly immobilized Ta2O5 nanoparticles on GF surface provided the active sites, enhanced hydrophilicity and electrolyte accessibility, thus remarkably improved electrochemical performance of GF. In particular, cyclic voltammetry (CV) and electrochemical impedance spectroscopy (EIS) results showed that the Ta2O5-GF nanocomposite electrode with weight percentage of Ta2O5 to GF of 0.75 wt% exhibited the best electrochemical activity and reversibility toward the VO2+/VO2+ redox reaction, when compared with the other electrodes. The corresponding energy efficiency was enhanced by ~ 9% at a current density of 80 mA cm−2, as compared with untreated GF. Furthermore, the charge–discharge

stability test with 0.75 wt% Ta2O5-GF electrode at 80 mA cm−2 showed that after 100 cycles, there was no obvious attenuation of efficiencies signifying, the best stability of Ta2O5 nanoparticles which strongly adhered on the GF surface.

### Image

Recent Publications

- Ponce de León, C.; Frías-Ferrer, A.; González-García, J.; Szánto, D. A.; Walsh, F. C., Redox flow cells for energy conversion. J. Power Sources 2006, 160 (1), 716-732.

- Yang, Z.; Zhang, J.; Kintner-Meyer, M. C.; Lu, X.; Choi, D.; Lemmon, J. P.; Liu, J., Electrochemical energy storage for green grid. Chem Rev 2011, 111 (5), 3577-613.

- Larcher, D.; Tarascon, J. M., Towards greener and more sustainable batteries for electrical energy storage. Nat Chem 2015, 7 (1), 19-29.

- Lin, K.; Gómez-Bombarelli, R.; Beh, E. S.; Tong, L.; Chen, Q.; Valle, A.; Aspuru-Guzik, A.; Aziz, M. J.; Gordon, R. G., A redox-flow battery with an alloxazine-based organic electrolyte. Nature Energy 2016, 1, 16102.

- Brushett, F. R.; Vaughey, J. T.; Jansen, A. N., An All-Organic Non-aqueous Lithium-Ion Redox Flow Battery. Advanced Energy Materials 2012, 2 (11), 1390-1396.

Biography

Anteneh Wodaje is a lecturer in the School of Chemical and Bio Engineering at Addis Ababa Institute of Technology, Ethiopia. He obtained his MSC degree from Addis Ababa University in 2010 for the studies on Photoelectrochemical Solar Energy Conversion based on Conjugated Polymers. He moved to the National Taiwan University of Science and Technology in 2016 till now for PhD study and extended research work on Redox Flow Battery Systems. His research interests are in nanostructured electrode materials for energy systems and electrochemical engineering for energy materials.

Email: antenehwodaje@gmail.com