Highly efﬁcient and durable phosphine reduced iron-doped tungsten oxide/reduced graphene oxide nanocomposites for the hydrogen evolution reaction

Tadele Hunde Wondimu, Guan-Cheng Chen, Daniel Manaye Kabtamu, Hsueh-Yu Chen, Anteneh Wodaje Bayeh, Hsin-Chih Huang,Chen Hao Wang*

Department of Materials Science and Engineering, National Taiwan University of Science and Technology, 10607,

Taipei, Taiwan, ROC

### Abstract

### The design and development of inexpensive and highly efﬁcient electrocatalysts for hydrogen production from water splitting are highly crucial for green energy and the hydrogen economy. Herein, we report phosphine reduced an iron-doped tungsten oxide nanoplate/reduced graphene oxide nanocomposite (Fe-WOxP/rGO) as an excellent electrocatalyst for the hydrogen evolution reaction. This electrocatalyst was synthesized using a hydrothermal method, followed by reduction with phosphine (PH3), which was generated from sodium hypophosphite. The catalyst onset potential, Tafel slope, and stability were investigated. Accordingly, Fe-WOxP/rGO exhibited impressively high electrocatalytic ac- tivity with a low overpotential of 54.60 mV, which is required to achieve a current density of 10mAcm-2. The Tafel slope of 41.99 mV dec-1 and the linear sweep voltammetry curve is almost the same as 2000 cycles and electrolysis under static overpotential (54.60 mV) is remain for more than 24 h in 0.5 M H2SO4. The catalytic activity and conductivity of Fe-WOxP/rGO were higher than WOXP, Fe-WOxP and WOxP/rGO. Such an outstanding performance of the Fe-WOxP/rGO nanocomposite is attributed to the coupled synergic effectbetween high oxygen vacancies formation on tungsten oxide in the nanoplate-like structure of Fe-WOxP and rGO nanosheet, making it as an excellent electrocatalyst for hydrogen evolution reaction.

### Image

Recent Publications

- Xing Z, Liu Q, Asiri AM, Sun X. High-Efficiency Electrochemical Hydrogen Evolution Catalyzed by Tungsten Phosphide Submicroparticles. ACS Catalysis. 2015;5:145-9.

- Wang D, Zhang D, Tang C, Zhou P, Wu Z, Fang B. Hydrogen evolution catalyzed by cobalt-promoted molybdenum phosphide nanoparticles. Catal Sci Technol. 2016;6:1952-6.

- Chen J, Yu D, Liao W, Zheng M, Xiao L, Zhu H, et al. WO3-x Nanoplates Grown on Carbon Nanofibers for an Efficient Electrocatalytic Hydrogen Evolution Reaction. ACS Appl Mater Interfaces. 2016;8:18132-9.

- Ramireddy T, Xing T, Rahman MM, Chen Y, Dutercq Q, Gunzelmann D, et al. Phosphorus–carbon nanocomposite anodes for lithium-ion and sodium-ion batteries. J Mater Chem A. 2015;3:5572-84.

- ingh T, Müller R, Singh J, Mathur S. Tailoring surface states in WO3 photoanodes for efficient photoelectrochemical water splitting. Applied Surface Science. 2015;347:448-53

Biography

Tadele Hunde is a lecturer at Mekelle University in College of Computational and Natural Science in Department of Chemistry , Ethiopia. He obtained his MSc degree from Addis Ababa University in 2011 for the studies on Simultaneous determination of N-acetyl-p-aminophenol and p-aminophenol with poly(3,4-ethylenedioxythiophene) modified glassy carbon electrode . He moved to the National Taiwan University of Science and Technology in 2016 till now for PhD study and extended research work on water splitting on hydrogen evolution reaction and fuel cell. His research interests are in nanostructured electrode materials for energy systems and electrochemical engineering for energy materials.

Email: tadechem@gmail.com