Synthesis and Characterization of Carbon Dots Coated Al2O3 Nanofibers Nanocomposite for Pb2+ ion Adsorption and Reuse for Latent Fingerprint Detection.

BG Fouda-Mbanga, E. Prabakaran, and K. Pillay*

*Department of Chemical science, University of Johannesburg, Johannesburg, South Africa

*Corresponding author: Tel: +27 11 5596128, Fax: +27 11 5596425 (NB)

Email address: kriveshinip@uj.ac.za (KP).

Abstract

This study reports a new approach of preparation of carbon dots coated aluminum oxide nanofibers (CDs/Al2O3NFs) nanocomposite and reusing the spent adsorbent of Pb2+-CDs/Al2O3NFs nanocomposite for latent fingerprint detection (LFP) after removing Pb2+ ions from aqueous solution. CDs/Al2O3NFs nanocomposite was prepared by using CDs and Al2O3NFs with adsorption processes. The prepared nanocomposite was then characterized by using UV-visible spectroscopy (UV-visible), Fourier transforms infrared spectroscopy (FTIR), Fluorescence, X-ray diffraction pattern (XRD), scanning electron microscope (SEM), Transmission electron microscopy (TEM), Energy-dispersive X-ray spectroscopy (EDS), Zeta potential, X-ray photoelectron spectroscopy (XPS). The size of the CDs average was 51.18 nm. The synthesized CDs/Al2O3NFs nanocomposite has proven to be a good adsorbent in Pb2+ removal from water with optimum pH 6, dosage 0. 2 g / L.  The results were suited by Freundlich models rather than the Langmuir, which was indicated the linear fit of Freundlich models with (R2 = 0.9896). This adsorption was related to the multilayer adsorption processes of Pb2+ ions on the CDs/Al2O3NFs nanocomposite surface. The adsorption capacity of CDs/Al2O3NFs nanocomposite showed the best removal of Pb2+ ions with qm = (177. 83 mg/g), when compared to the previous reports. This adsorption followed the pseudo-second order kinetics and intra particle diffusion processes. ∆G and ∆H values indicated spontaneity and the endothermic nature of the adsorption process. CDs/Al2O3NFs nanocomposite therefore showed potential as an effective adsorbent. Furthermore, the metal loaded on the adsorbent Pb2+-CDs/Al2O3NFs has proven to be sensitive and selective for LFP detection on various porous substrates. Hence Pb2+-CDs/Al2O3NFs nanocomposite can be reused as a good fingerprint labelling agent in LFP detection so as to avoid secondary environmental pollution by disposal of the spent adsorbent.

Keyword: CDs/Al2O3NFs nanocomposite, Lead adsorption, Isotherm, kinetics, Thermodynamics, Reusable for latent fingerprint detection.

Biography

Dr Bienvenu Gael Fouda Mbanga is researcher at the University of Johannesburg currently work as a research assistant. He completed his PhD in 2020 and has intrest in nanotechnology, water treatment and forensic. He worked also as a facilitator at Soweto sciences at the same university. He has published part of his work on international peer reviewed articles and is dedicated to see young people to achieve their goals by encouraging them to think critically and be problem solvers in their communities where they found themselves.

Presenting Author details

Full name: Bienvenu Gael Fouda Mbanga

Contact: 0734178887

Category: Oral presentation

Email: patsonp46@gmail.com