Title: Antibacterial activity on newly developed nanotechnological coatings approved for food contact

NAME: Alessandro Di Cerbo1, Roberto Canton2, Giuseppe Rosace3, Carla Sabia4, Antonio Scarano5, Roberta Stocchi1, Anna Rita Loschi1, Stefano Rea1

1 School of Biosciences and Veterinary Medicine, University of Camerino, 62024 Matelica, Italy;

2 Moma Nanotech Srl, 20861 Brugherio, Italy

3 Department of Engineering and Applied Sciences, University of Bergamo, 24044 Dalmine, Italy;

4 Department of Life Sciences, University of Modena and Reggio Emilia, 41125 Modena, Italy

5 Department of Medical, Oral and Biotechnological Sciences, University of Chieti-Pescara, 66100 Chieti, Italy

Aims and Objectives:

One of the main concerns of the food industry is microbial adhesion to food contact surfaces and consequent contamination. Stainless steel and aluminum, widely present in food industry, are frequently exposed to bacterial colonization with possible consequences on consumers’ health. We aimed to evaluate the potential bacteriostatic/bactericidal efficacy of aluminum and stainless-steel surfaces with different large-scale roughness before and after the surface coating with two different nanotechnological coatings approved for food contact.

Methods:

Fifty hundred seventy-six disks of both stainless-steel (n = 288) and aluminum (n = 288) with different roughness (0.25, 0.5 and 1 μm) were challenged with four Gram-negative (Escherichia coli ATCC 25922, Salmonella typhimurium ATCC 1402, Yersinia enterocolitica ATCC 9610 and Pseudomonas aeruginosa ATCC 27588) and four Gram-positive (Staphylococcus aureus ATCC 6538, Enterococcus faecalis ATCC 29212, Bacillus cereus ATCC 14579 and Listeria monocytogenes NCTT 10888) bacteria and underwent 3 different sanitizing treatments, e.g., UV, alcohol and a natural product named Gold lotion.

After the first challenge all disks were then coated with two different nanotechnological coatings approved for food contact according to NSF and MOCA 1935/2004 named DURALTI® and NanoXHAM® D, respectively, and underwent the same sanitizing treatments.

Results:

As far as concerns aluminum surfaces without nanotechnological surface treatment, an overall bacteriostatic effect was observed for all strains with respect to the initial inoculum that was 106 CFU/mL. Conversely, an overall bactericidal effect was observed both for Gram-negative and -positive bacteria on DURALTI®-treated aluminum disks, regardless of roughness and sanitizing treatment. Conversely, on stainless-steel surfaces, a significant bactericidal effect was exerted by all of sanitizing treatments against all bacterial strains regardless of roughness and surface coating. The nanoXHAM D coating itself induced an overall bactericidal effect as well as in synergy with all sanitizing treatments regardless of roughness.

Conclusions:

Results are innovative in terms of the great potential of the antibacterial activity of nanotechnologically treated food contact surfaces and their combination with some sanitizing agents that might be exploited in the food industry. Moreover, since most of sanitizing treatments are toxic and corrosive causing the onset of crevices able to facilitate bacterial nesting and growth, nanoXHAM D was also able to reduce bacterial adhesion, nesting and growth.

Biography

- Di Cerbo, A.; Mescola, A.; Rosace, G.; Stocchi, R.; Rossi, G.; Alessandrini, A.; Preziuso, S.; Scarano, A.; Rea, S.; Loschi, A.R.; et al. Antibacterial Effect of  Stainless-Steel Surfaces Treated with a Nanotechnological Coating Approved for Food Contact. Microorganisms 2021, 9 (in press)

- Di Cerbo, A.; Pezzuto, F.; Scarano, A. Cytotoxic and Bacteriostatic Activity of Nanostructured TiO2 Coatings. Pol. J. Microbiol. 2016, 65, 225–229, doi:10.5604/17331331.1204484.

- Rosace, G.; Canton, R.; Colleoni, C. Plasma enhanced CVD of SiOxCyHz thin film on different textile fabrics: Influence of exposure time on the abrasion resistance and mechanical properties. Appl. Surf. Sci. 2010, 256, 2509–2516, doi:10.1016/j.apsusc.2009.10.097.

- Iannitti, T.; Di Cerbo, A.; Loschi, A.R.; Rea, S.; Suzawa, M.; Morales-Medina, J.C. Repeated administration of a flavonoid-based formulated extract from citrus peels significantly reduces peripheral inflammation-induced pain in the rat. Food Sci. Nutr. 2020, 8, 3173–3180, doi:10.1002/fsn3.1566

- Di Cerbo, A.; Mescola, A.; Iseppi, R.; Canton, R.; Rossi, G.; Stocchi, R.; Loschi, A.R.; Alessandrini, A.; Rea, S.; Sabia, C. Antibacterial Effect of Aluminum Surfaces Untreated and Treated with a Special Anodizing Based on Titanium Oxide Approved for Food Contact. Biology 2020, 9, 456, doi:10.3390/biology9120456.

- Seeger, H.M.; Di Cerbo, A.; Alessandrini, A.; Facci, P. Supported lipid bilayers on mica and silicon oxide: Comparison of the main phase transition behavior. J. Phys. Chem. B 2010, 114, 8926–8933, doi:10.1021/jp1026477.

- Di Cerbo, A.; Mescola, A.; Iseppi, R.; Canton, R.; Rossi, G.; Stocchi, R.; Loschi, A.R.; Alessandrini, A.; Rea, S.; Sabia, C. Antibacterial Effect of Aluminum Surfaces Untreated and Treated with a Special Anodizing Based on Titanium Oxide Approved for Food Contact. Biology 2020, 9, 456, doi:10.3390/biology9120456

- MOMA Nanotech SRL. nanoXHAM®D. Available online: https://www.nanotech.it/bundles/datadeo/images/materiale/4183/nanoXham%20D_ita_2018.pdf (accessed on 19/12/2020).

Presenting author details Full name: Dr. Alessandro Di Cerbo

MS.c. (Medical Biotechnology), Ph.D. (Nanoscience and Nanotechnology), Postgraduate Dipl. (Clinical Biochemistry)

Email Address: alessandro.dicerbo@unicam.it Contact number: +39 3923731318

Linked In account: https://www.linkedin.com/in/alessandro-di-cerbo-0072791b3/

Session name/number: Category: (Oral presentation)