# Nano encapsulation of catechin in starch nanoparticles: Characterization, release behavior and bioactivity retention during in-vitro digestion.

# Sajid Maqsood1, Mudasir Ahmad1,2, Priti Mudgil, Fathalla Hamed3, Adil Gani2*

1Department of Food Science, College of Food and Agriculture, United Arab Emirates University, 15551 Al Ain, United Arab Emirates

2Department of Food Science and Technology, University of Kashmir, Srinagar, India, 190006.

3Department of Physics, College of Science, United Arab Emirates University, 15551 Al Ain, United Arab Emirates

### Abstract (300 word limit)

The novel starch-based nanoparticles from three different sources viz: horse chestnut (HSC), water chestnut (WSC) and lotus stem (LSC) were prepared for nano-encapsulation of bioactive catechin molecules. Average particle size of nano-particles produced from HSC, WSC and LSC were found to be 322, 559 and 615 nm with encapsulation efficiency of 59.09, 48.30, and 55.00% and negative zeta potential of -18.05, -21.5 and -18.05mv were observed, respectively. The structural, physical and thermal properties were characterized by fourier transform infrared spectroscopy (FTIR), scanning electron microscopy (SEM), X-ray diffraction (XRD) and differential scanning calorimetry (DSC). The SEM analysis revealed capsule formation with entrapped catechin, while the broad characteristic peaks at 3479, 1683, 1283, 1144, 1070 and 860 cm -1 depicts the encapsulation of catechin in starch nanoparticles without any evident interaction. DSC thermogram reveals the thermal protection of catechin while XRD showed loss of crystallinity after encapsulation. The higher content of catechin in intestinal juice ensured controlled release in the intestine. Bioactivities like lipase, cholesteryl esterase and DPP-IV inhibition were higher in encapsulated catechin than free catechin upon simulated gastric and intestinal digestion.

### Recent publications (minimum 5)

- Nongonierma, A.B., Paolella Sara, Mudgil, P., Maqsood*, S & FitzGerald, R.J*. (2017). Dipeptidyl peptidase IV (DPP-IV) inhibitory properties of camel milk protein hydrolysates generated with trypsin. Journal of Functional Foods, 34, 49–58.

- Ahmad, M., Qureshi, S., Maqsood*, S, Gani, A., and Masoodi, F.A. (2017). Micro-encapsulation of folic acid using horse chestnut starch and β-cyclodextrin: Microcapsule characterization, release behavior & antioxidant potential during GI tract conditions. Food Hydrocolloids, 66, 154–160.

- Al-Shamsi, K.A., Mudgil, P., Hassan, H.M., Maqsood, S*. (2018). Camel milk protein hydrolysates with improved technofunctional properties and enhanced antioxidant potential in in vitro and in food model systems. Journal of Dairy Science, 101, 47-60.

- Nongonierma, A.B., Paolella Sara, Mudgil, P., Maqsood*, S. & FitzGerald, R.J*. (2018). Identification of novel dipeptidyl peptidase IV (DPP-IV) inhibitory peptides in camel milk protein hydrolysates. Food Chemistry, 244, 340-348.

- S. Mad‐Ali, S. Benjakul, T. Prodpran, Maqsood, S. (2016). Interfacial properties of gelatin from goat skin as influenced by drying methods. LWT - Food Science and Technology 73 (2016) 102e107

Biography

Dr. Sajid is an Associate Professor in Department of Food Science, College of Food and Agriculture, UAEU. He teaches advance courses in food science. He has been awarded Gold medal for bachelor’s and master’s degree and was awarded with Altech’s Young Scientist award. He is currently exploring an innovative research program at UAEU which focus on bioactive molecules in camel milk and dates, investigating their functional and nutraceutical properties, and their encapsulation at micro and nano level. He has published his research in leading refereed journals and presented his research results in both national and international conferences. He has published more than 50 articles and edited 2 books. He is member of editorial board for four International journals as well as serving a potential reviewer for many international journals.

Email: sajid.m@uaeu.ac.ae

Notes/Comments: